Anodic  solution

 Feed solution
  Liquid membrane
Cathodic solution

















Scheme of membrane extraction during electrodialysis

 
[image: image1.wmf]0

20

40

60

80

100

0

20

40

60

80

100

t (min)

Cobalt content (%)


Kinetics of cobalt(II) removal  from the feed solution (1), accumulation in the liquid membrane (2), in the cathodic solution (3) and electrodeposition (4). i = 2.8 mА∙сm-2 ; СD2EHPA = 20 vol.%; СTOA = 0.1 mol∙L-1; cathodic  solution: 0.025 M  HClO4


[image: image2.wmf]0

20

40

60

80

100

0

0.02

0.04

0.06

0.08

0.1

c

co

 (mol L

-1

)

 J (

m

mol m

-2

s

-1

)

E, S (%)


Dependence of the extraction degree (1), stripping degree (2) and  flux  into the cathodic  solution (3)  on the CoSO4 initial concentration
i = 2.8 mА∙сm-2; t  = 60 min; CD2EHPA = 32 vol.%; CTOA = 0.1 mol∙L-1; cathodic  solution:  0.025 M HClO4
[image: image3.jpg]



Scanning electron microscopy image of the cobalt  coating deposited from

0.025 M  HClO4  on the copper cathode at the current density of 6.0 mА∙сm-2
 
[image: image4.wmf]0

40

80

120

160

200

0

30

60

90

120

150

180

t (min)

U (V)


Change in voltage during electrodialysis for various  current densities

CD2EHPA = 20 vol.%;  CTOA = 0.1 mol∙L-1 ;  cathodic  solution: 0.025 M  HClO4;

i (mА∙сm-2) = 5.7 (1); 4.2 (2); 2.8 (3); 2.1 (4)

Effect of the current density i on the cobalt(II) extraction degree E, stripping degree S, electrodeposition degree D and flux Ja
	i /mА∙сm-2
	t / min
	Cathodic  solution
	Е
	S
	D
	J∙105 / mol∙m-2∙s-1

	
	
	
	%
	

	2.1
	175
	2.5∙10-2 M HClO4
	99.7
	32
	45
	1.3

	2.8
	98
	2.5∙10-2 M HClO4
	99.7
	41
	27
	2.1

	4.2
	55
	2.5∙10-2 M HClO4
	99.0
	36
	6
	2.4

	5.7
	40
	2.5∙10-2 M HClO4
	98.4
	30
	2
	2.4

	2.8
	107
	2∙10-2 M H2SO4
	100.0
	64
	15
	2.3

	1.4
	33
	1∙10-2 M H2SO4
	15.0
	3.5
	-
	0.3

	2.8
	33
	1∙10-2 M H2SO4
	34.0
	9.0
	-
	0.9

	4.2
	33
	1∙10-2 M H2SO4
	76.0
	26
	1.5
	2.5

	4.2
	46
	1∙10-2 M H2SO4
	99.1
	44
	9
	3.6

	5.7
	33
	1∙10-2 M H2SO4
	98.0
	50
	6
	5.2

	5.7
	34
	0.1 M H2SO4
	98.0
	25
	3
	2.5


a  CCo = 0.01 mol∙L-1; cD2EHPA = 20 vol.%;  cTOA = 0.1 mol∙L-1
Effect of the D2EHPA and TOA concentration in the liquid membrane on the cobalt(II) transporta

	cD2EHPA / vol.%
	cTOA  / mol∙L-1
	Е
	S
	J / (mol∙m-2∙s-1

	
	
	%
	

	5
	0.1
	68
	17
	9

	20
	0.1
	54
	14
	7

	32
	0.1
	59
	17
	9

	50
	0.1
	69
	15
	8

	32
	0.05
	65
	17
	9

	32
	0.2
	59
	13
	7

	32
	0.4
	61
	14
	7


a  CCo = 0.01 mol∙L-1; i = 2.8 mA∙cm-2; CHClO4 = 0.025 M;  t = 60 min

Effect of the cathodic   solution composition  on the cobalt(II) transport and electrodepositiona

	t / min
	Cathodic  solution

(C = 0.01 M) 
	Е
	S
	D
	J∙105 / mol∙m-2∙s-1

	
	
	%
	

	45
	HClO4
	52
	3
	7
	0.7

	45
	HCl
	57
	12
	3
	1

	45
	H2SO4
	59
	15
	-
	1

	45
	HNO3
	58
	10
	-
	0.7

	60
	H2SO4b
	88
	Organic phase in the cathodic solution

	60
	H2SO4
	83
	39
	9
	2.5

	60
	HCl
	77
	28
	8
	1.8

	60
	HClO4c
	54
	14
	-
	0.7


a CCo = 0.01 mol∙L-1; i = 2.8 mA∙cm-2; CD2EHPA = 20 vol.%;  CTOA = 0.1 mol∙L-1
b C = 1∙10-3 M; c C = 2.5∙10-2 M

4





	O2										 2A−					    H2


        													           											Co2+				Co2+			     Co2+


   				          												(				 	    	         					CoA2	       				


	 H+ 												


		 H2O					  		


     		  									HA


							H+						  	     H+  					  						   	   			


      	  										 A− 							


			  		      											ClO4−


     						     R3NHA				  


	H+	     SO42−	  		 SO42−	  	   R3N		      HA			ClO4−	


				   						       R3NH+				  									ClO4−						       ClO4−


									    	   R3NHClO4


																	








			  		 


       ClO4−						         ClO4−				   		  Oct3NHClO4





	NO3−		  Oct3NH+		      ClO4−














				   				





  +


			


























—





  −























3





2





1





3





2





1





4





3





2





1








_1458122827.xls
Диаграмма1

		7		3		2		3

		12		10		10		10

		20		18		19		26

		24		24		26		37

		30		30		34		49

		34		35		44		60

		37		40		51		96

		39		44		60		113

		40		48		66		122

				53		75		129

				54		81		136

				55		87		145

						92		152

						95		163

						97		171

						98		173

								175



t (min)

U (V)

42

32

23

18

45

31

23

17

58

37

25

19.6

72

46

28

23

88.5

67

34.5

27.5

100

76

42

31.4

119

84

45

37.4

142

95

50

48

200

115

56

50

136

66

56

153

70

69

200

83

80

95

89

113

102

131

133

200

154

200



Диаграмма2

		0		0		80		0

		40		40		98		40

		60		60				60

		80		80				80

		98		98				98



t (min)

Cobalt content (%)

100

0

0

0

64.6

6

27

30

45.6

12

41

12.6

29

58

0.3

40.5

32



Диаграмма3

		0.001		0.001		0.001

		0.01		0.01		0.01

		0.05		0.05		0.05

		0.1		0.1		0.1



cco (mol L-1)

J (mmol m-2s-1)
E, S (%)

94.4

39.1

2.5

58.8

17.4

8.8

20.8

10.7

27.3

10.8

4.1

20.9



Диаграмма4

		-3		-3		-3

		-2		-2		-2

		-1		-1		0.1



lgCH2SO4

J / mmol m-2s-1
E, S / %

80.5

28.9

14.7

58.8

17.4

0.88

6.2

2.1



Диаграмма6

		2		2		2		2		3

		8		8		5		5		8

		13		13		10		13		15

		20		23		15		20		20

		30		32		20		22		25

		35		44		25		27		30

		41		57		31		35		37

		45		60		38		39		43

		50				45		45		47

		56				55		50		54

		58				60		55		60

								60



t / min

U / V

47

41

17

14

12.6

45

40

17.6

17.4

13.5

45

40

17.6

21.4

14

45

40

18

25

14.6

46

42

19

27

15.4

49

42.4

20

31.4

16.6

51

50

22

40.5

18.6

52

50.4

25

46.6

21

54

26.6

53

21.4

57

27

56

22.4

58

27.4

53

22.6

52



Диаграмма5

		2		2		2

		8		6		5

		13		10		15

		24		15		25

		32		20		43

		37		30		52

		42		37		60

		43		43

		44		51

		44.5		55

				59



t

U

27

28

26

27

28

26

28

28

24.5

31.5

28

23.5

41

31

21.6

55

33

21

82

35

20.6

100

34.5

144

33

200

34

36.4



Диаграмма7

		1.5		2		2		2

		5		11		7		11

		7		20		15		20

		16		25		25		33

		19		30		30		42

		24		35		35		50

		27		37		41		60

		32		42		46		70

		36		45		57		85

		39		47		70		95

		41		49		76		105

		45		51		85		115

				53		95		120

				54		101

						103

						105

						107



t / min

U / V

76.4

32

25

27

66

32

24

25

62

35.5

25

26.5

68.4

40.4

33

33

80

47

39

34

92.6

57

47.5

32

106

66

57

34

125

85

61.5

31

140

99

66.5

28

168

116

76

22

184

137

86

18

200

154

83

18

171

81

18

200

94

110

132

200



Лист1

		

																Fig1

				40 мА				30mA						20mA						15mA

		t		U				t		U				t		U				t		U

		7		42				3		32				2		23				3		18

		12		45				10		31				10		23				10		17

		20		58				18		37				19		25				26		19.6

		24		72				24		46				26		28				37		23

		30		88.5				30		67				34		34.5				49		27.5

		34		100				35		76				44		42				60		31.4

		37		119				40		84				51		45				96		37.4

		39		142				44		95				60		50				113		48

		40		200				48		115				66		56				122		50

								53		136				75		66				129		56

								54		153				81		70				136		69

								55		200				87		83				145		80

														92		95				152		89

														95		113				163		102

														97		131				171		133

														98		200				173		154

																				175		200

																Fig2

										t		c1		c2		c3		c4-org

										0		100		0		0		0

										40		64.6		6		0		30

										60		45.6		12		0		41

										80		12.6		29		0		58

										98		0.3		40.5		27		32

						Fig3						Fig3b

		Cco		E		R		J*106				lgCh2so4		E		R		J*106

		0.001		94.4		39.1		2.5				-3		80.5		28.9		14.7

		0.01		58.8		17.4		8.8				-2		58.8		17.4		0.88

		0.05		20.8		10.7		27.3				-1		6.2		2.1		0.1

		0.1		10.8		4.1		20.9

						Fig4

		0.0001Co						0.01Co						0.1Co

		t		u				t		u				t		u

		2		27				2		28				2		26

		8		27				6		28				5		26

		13		28				10		28				15		24.5

		24		31.5				15		28				25		23.5

		32		41				20		31				43		21.6

		37		55				30		33				52		21

		42		82				37		35				60		20.6

		43		100				43		34.5

		44		144				51		33

		44.5		200				55		34

								59		36.4

								Fig5

						50%D2				0.05MTOA						0.2MTOA						5%D2						0.4MTOA

				t		U				t		U				t		U				t		U				t		U

				2		47				2		41				2		17				2		14				3		12.6

				8		45				8		40				5		17.6				5		17.4				8		13.5

				13		45				13		40				10		17.6				13		21.4				15		14

				20		45				23		40				15		18				20		25				20		14.6

				30		46				32		42				20		19				22		27				25		15.4

				35		49				44		42.4				25		20				27		31.4				30		16.6

				41		51				57		50				31		22				35		40.5				37		18.6

				45		52				60		50.4				38		25				39		46.6				43		21

				50		54										45		26.6				45		53				47		21.4

				56		57										55		27				50		56				54		22.4

				58		58										60		27.4				55		53				60		22.6

																						60		52

								Fig6

						10-4MHS						10-3MHS						0/02MHS						0.1MHS

						t		u				t		u				t		u				t		u

						1.5		76.4				2		32				2		25				2		27

						5		66				11		32				7		24				11		25

						7		62				20		35.5				15		25				20		26.5

						16		68.4				25		40.4				25		33				33		33

						19		80				30		47				30		39				42		34

						24		92.6				35		57				35		47.5				50		32

						27		106				37		66				41		57				60		34

						32		125				42		85				46		61.5				70		31

						36		140				45		99				57		66.5				85		28

						39		168				47		116				70		76				95		22

						41		184				49		137				76		86				105		18

						45		200				51		154				85		83				115		18

												53		171				95		81				120		18

												54		200				101		94

																		103		110

																		105		132

																		107		200





Лист2

		





Лист3

		






_1458125759.xls
Диаграмма1

		7		3		2		3

		12		10		10		10

		20		18		19		26

		24		24		26		37

		30		30		34		49

		34		35		44		60

		37		40		51		96

		39		44		60		113

		40		48		66		122

				53		75		129

				54		81		136

				55		87		145

						92		152

						95		163

						97		171

						98		173

								175



t (min)

U (V)

42

32

23

18

45

31

23

17

58

37

25

19.6

72

46

28

23

88.5

67

34.5

27.5

100

76

42

31.4

119

84

45

37.4

142

95

50

48

200

115

56

50

136

66

56

153

70

69

200

83

80

95

89

113

102

131

133

200

154

200



Диаграмма2

		0		0		80		0

		40		40		98		40

		60		60				60

		80		80				80

		98		98				98



t (min)

Cobalt content (%)

100

0

0

0

64.6

6

27

30

45.6

12

41

12.6

29

58

0.3

40.5

32



Диаграмма3

		0.001		0.001		0.001

		0.01		0.01		0.01

		0.05		0.05		0.05

		0.1		0.1		0.1



Cco / mol L-1

J / mmol m-2s-1
E, S / %

94.4

39.1

2.5

58.8

17.4

8.8

20.8

10.7

27.3

10.8

4.1

20.9



Диаграмма4

		-3		-3		-3

		-2		-2		-2

		-1		-1		0.1



lgCH2SO4

J / mmol m-2s-1
E, S / %

80.5

28.9

14.7

58.8

17.4

0.88

6.2

2.1



Диаграмма6

		2		2		2		2		3

		8		8		5		5		8

		13		13		10		13		15

		20		23		15		20		20

		30		32		20		22		25

		35		44		25		27		30

		41		57		31		35		37

		45		60		38		39		43

		50				45		45		47

		56				55		50		54

		58				60		55		60

								60



t / min

U / V

47

41

17

14

12.6

45

40

17.6

17.4

13.5

45

40

17.6

21.4

14

45

40

18

25

14.6

46

42

19

27

15.4

49

42.4

20

31.4

16.6

51

50

22

40.5

18.6

52

50.4

25

46.6

21

54

26.6

53

21.4

57

27

56

22.4

58

27.4

53

22.6

52



Диаграмма5

		2		2		2

		8		6		5

		13		10		15

		24		15		25

		32		20		43

		37		30		52

		42		37		60

		43		43

		44		51

		44.5		55

				59



t

U

27

28

26

27

28

26

28

28

24.5

31.5

28

23.5

41

31

21.6

55

33

21

82

35

20.6

100

34.5

144

33

200

34

36.4



Диаграмма7

		1.5		2		2		2

		5		11		7		11

		7		20		15		20

		16		25		25		33

		19		30		30		42

		24		35		35		50

		27		37		41		60

		32		42		46		70

		36		45		57		85

		39		47		70		95

		41		49		76		105

		45		51		85		115

				53		95		120

				54		101

						103

						105

						107



t / min

U / V

76.4

32

25

27

66

32

24

25

62

35.5

25

26.5

68.4

40.4

33

33

80

47

39

34

92.6

57

47.5

32

106

66

57

34

125

85

61.5

31

140

99

66.5

28

168

116

76

22

184

137

86

18

200

154

83

18

171

81

18

200

94

110

132

200



Лист1

		

																Fig1

				40 мА				30mA						20mA						15mA

		t		U				t		U				t		U				t		U

		7		42				3		32				2		23				3		18

		12		45				10		31				10		23				10		17

		20		58				18		37				19		25				26		19.6

		24		72				24		46				26		28				37		23

		30		88.5				30		67				34		34.5				49		27.5

		34		100				35		76				44		42				60		31.4

		37		119				40		84				51		45				96		37.4

		39		142				44		95				60		50				113		48

		40		200				48		115				66		56				122		50

								53		136				75		66				129		56

								54		153				81		70				136		69

								55		200				87		83				145		80

														92		95				152		89

														95		113				163		102

														97		131				171		133

														98		200				173		154

																				175		200

																Fig2

										t		c1		c2		c3		c4-org

										0		100		0		0		0

										40		64.6		6		0		30

										60		45.6		12		0		41

										80		12.6		29		0		58

										98		0.3		40.5		27		32

						Fig3						Fig3b

		Cco		E		R		J*106				lgCh2so4		E		R		J*106

		0.001		94.4		39.1		2.5				-3		80.5		28.9		14.7

		0.01		58.8		17.4		8.8				-2		58.8		17.4		0.88

		0.05		20.8		10.7		27.3				-1		6.2		2.1		0.1

		0.1		10.8		4.1		20.9

						Fig4

		0.0001Co						0.01Co						0.1Co

		t		u				t		u				t		u

		2		27				2		28				2		26

		8		27				6		28				5		26

		13		28				10		28				15		24.5

		24		31.5				15		28				25		23.5

		32		41				20		31				43		21.6

		37		55				30		33				52		21

		42		82				37		35				60		20.6

		43		100				43		34.5

		44		144				51		33

		44.5		200				55		34

								59		36.4

								Fig5

						50%D2				0.05MTOA						0.2MTOA						5%D2						0.4MTOA

				t		U				t		U				t		U				t		U				t		U

				2		47				2		41				2		17				2		14				3		12.6

				8		45				8		40				5		17.6				5		17.4				8		13.5

				13		45				13		40				10		17.6				13		21.4				15		14

				20		45				23		40				15		18				20		25				20		14.6

				30		46				32		42				20		19				22		27				25		15.4

				35		49				44		42.4				25		20				27		31.4				30		16.6

				41		51				57		50				31		22				35		40.5				37		18.6

				45		52				60		50.4				38		25				39		46.6				43		21

				50		54										45		26.6				45		53				47		21.4

				56		57										55		27				50		56				54		22.4

				58		58										60		27.4				55		53				60		22.6

																						60		52

								Fig6

						10-4MHS						10-3MHS						0/02MHS						0.1MHS

						t		u				t		u				t		u				t		u

						1.5		76.4				2		32				2		25				2		27

						5		66				11		32				7		24				11		25

						7		62				20		35.5				15		25				20		26.5

						16		68.4				25		40.4				25		33				33		33

						19		80				30		47				30		39				42		34

						24		92.6				35		57				35		47.5				50		32

						27		106				37		66				41		57				60		34

						32		125				42		85				46		61.5				70		31

						36		140				45		99				57		66.5				85		28

						39		168				47		116				70		76				95		22

						41		184				49		137				76		86				105		18

						45		200				51		154				85		83				115		18

												53		171				95		81				120		18

												54		200				101		94

																		103		110

																		105		132

																		107		200





Лист2

		





Лист3

		






_1458121729.xls
Диаграмма1

		7		3		2		3

		12		10		10		10

		20		18		19		26

		24		24		26		37

		30		30		34		49

		34		35		44		60

		37		40		51		96

		39		44		60		113

		40		48		66		122

				53		75		129

				54		81		136

				55		87		145

						92		152

						95		163

						97		171

						98		173

								175



t (min)

U (V)

42

32

23

18

45

31

23

17

58

37

25

19.6

72

46

28

23

88.5

67

34.5

27.5

100

76

42

31.4

119

84

45

37.4

142

95

50

48

200

115

56

50

136

66

56

153

70

69

200

83

80

95

89

113

102

131

133

200

154

200



Диаграмма2

		0		0		80		0

		40		40		98		40

		60		60				60

		80		80				80

		98		98				98



t (min)

Cobalt content (%)

100

0

0

0

64.6

6

27

30

45.6

12

41

12.6

29

58

0.3

40.5

32



Диаграмма3

		0.001		0.001		0.001

		0.01		0.01		0.01

		0.05		0.05		0.05

		0.1		0.1		0.1



Cco / mol L-1

J / mmol m-2s-1
E, S / %

94.4

39.1

2.5

58.8

17.4

8.8

20.8

10.7

27.3

10.8

4.1

20.9



Диаграмма4

		-3		-3		-3

		-2		-2		-2

		-1		-1		0.1



lgCH2SO4

J / mmol m-2s-1
E, S / %

80.5

28.9

14.7

58.8

17.4

0.88

6.2

2.1



Диаграмма6

		2		2		2		2		3

		8		8		5		5		8

		13		13		10		13		15

		20		23		15		20		20

		30		32		20		22		25

		35		44		25		27		30

		41		57		31		35		37

		45		60		38		39		43

		50				45		45		47

		56				55		50		54

		58				60		55		60

								60



t / min

U / V

47

41

17

14

12.6

45

40

17.6

17.4

13.5

45

40

17.6

21.4

14

45

40

18

25

14.6

46

42

19

27

15.4

49

42.4

20

31.4

16.6

51

50

22

40.5

18.6

52

50.4

25

46.6

21

54

26.6

53

21.4

57

27

56

22.4

58

27.4

53

22.6

52



Диаграмма5

		2		2		2

		8		6		5

		13		10		15

		24		15		25

		32		20		43

		37		30		52

		42		37		60

		43		43

		44		51

		44.5		55

				59



t

U

27

28

26

27

28

26

28

28

24.5

31.5

28

23.5

41

31

21.6

55

33

21

82

35

20.6

100

34.5

144

33

200

34

36.4



Диаграмма7

		1.5		2		2		2

		5		11		7		11

		7		20		15		20

		16		25		25		33

		19		30		30		42

		24		35		35		50

		27		37		41		60

		32		42		46		70

		36		45		57		85

		39		47		70		95

		41		49		76		105

		45		51		85		115

				53		95		120

				54		101

						103

						105

						107



t / min

U / V

76.4

32

25

27

66

32

24

25

62

35.5

25

26.5

68.4

40.4

33

33

80

47

39

34

92.6

57

47.5

32

106

66

57

34

125

85

61.5

31

140

99

66.5

28

168

116

76

22

184

137

86

18

200

154

83

18

171

81

18

200

94

110

132

200



Лист1

		

																Fig1

				40 мА				30mA						20mA						15mA

		t		U				t		U				t		U				t		U

		7		42				3		32				2		23				3		18

		12		45				10		31				10		23				10		17

		20		58				18		37				19		25				26		19.6

		24		72				24		46				26		28				37		23

		30		88.5				30		67				34		34.5				49		27.5

		34		100				35		76				44		42				60		31.4

		37		119				40		84				51		45				96		37.4

		39		142				44		95				60		50				113		48

		40		200				48		115				66		56				122		50

								53		136				75		66				129		56

								54		153				81		70				136		69

								55		200				87		83				145		80

														92		95				152		89

														95		113				163		102

														97		131				171		133

														98		200				173		154

																				175		200

																Fig2

										t		c1		c2		c3		c4-org

										0		100		0		0		0

										40		64.6		6		0		30

										60		45.6		12		0		41

										80		12.6		29		0		58

										98		0.3		40.5		27		32

						Fig3						Fig3b

		Cco		E		R		J*106				lgCh2so4		E		R		J*106

		0.001		94.4		39.1		2.5				-3		80.5		28.9		14.7

		0.01		58.8		17.4		8.8				-2		58.8		17.4		0.88

		0.05		20.8		10.7		27.3				-1		6.2		2.1		0.1

		0.1		10.8		4.1		20.9

						Fig4

		0.0001Co						0.01Co						0.1Co

		t		u				t		u				t		u

		2		27				2		28				2		26

		8		27				6		28				5		26

		13		28				10		28				15		24.5

		24		31.5				15		28				25		23.5

		32		41				20		31				43		21.6

		37		55				30		33				52		21

		42		82				37		35				60		20.6

		43		100				43		34.5

		44		144				51		33

		44.5		200				55		34

								59		36.4

								Fig5

						50%D2				0.05MTOA						0.2MTOA						5%D2						0.4MTOA

				t		U				t		U				t		U				t		U				t		U

				2		47				2		41				2		17				2		14				3		12.6

				8		45				8		40				5		17.6				5		17.4				8		13.5

				13		45				13		40				10		17.6				13		21.4				15		14

				20		45				23		40				15		18				20		25				20		14.6

				30		46				32		42				20		19				22		27				25		15.4

				35		49				44		42.4				25		20				27		31.4				30		16.6

				41		51				57		50				31		22				35		40.5				37		18.6

				45		52				60		50.4				38		25				39		46.6				43		21

				50		54										45		26.6				45		53				47		21.4

				56		57										55		27				50		56				54		22.4

				58		58										60		27.4				55		53				60		22.6

																						60		52

								Fig6

						10-4MHS						10-3MHS						0/02MHS						0.1MHS

						t		u				t		u				t		u				t		u

						1.5		76.4				2		32				2		25				2		27

						5		66				11		32				7		24				11		25

						7		62				20		35.5				15		25				20		26.5

						16		68.4				25		40.4				25		33				33		33

						19		80				30		47				30		39				42		34

						24		92.6				35		57				35		47.5				50		32

						27		106				37		66				41		57				60		34

						32		125				42		85				46		61.5				70		31

						36		140				45		99				57		66.5				85		28

						39		168				47		116				70		76				95		22

						41		184				49		137				76		86				105		18

						45		200				51		154				85		83				115		18

												53		171				95		81				120		18

												54		200				101		94

																		103		110

																		105		132

																		107		200





Лист2

		





Лист3

		






