

Catholyte
Feed

Liquid


Strip


Anolyte






solution

membrane

solution




















Scheme of the membrane extraction during electrodialysis

 
[image: image1.wmf]0

2

4

6

8

10

0

4

8

12

16

Current density, mA cm

-2

Flux 10

5

, mol m

-2 

s

-1


Dependence of the chromium(VI) flux into the strip solution on the current density for various membrane systems 

(CТОА  (mol L-1) = 0.2 (1, 2); 0.1 (3); CD2EHPA (vol. %) = 10 (1, 3); 0 (2); CHCl  (mol L-1) = 0.01 (1); 0.1 (2, 3))


[image: image2.wmf]0

25

50

75

100

0

60

120

180

Time, min

Cr  content, %


Kinetics of chromium(VI) removal  from the feed solution (1), accumulation in the liquid membrane (2) and in the strip solution (3) 

(i = 10.6 mА сm-2; CTOA = 0.1 mol L-1; CD2EHPA = 10 vol. %; CHCl = 0.1 mol L-1)

 
[image: image3.wmf]0

25

50

75

100

0

0.025

0.05

0.075

0.1

Cr  concentration, mol L

-1

Flux 10

5

, mol m

-2

 s

-1

 E, S, %


Dependence of the chromium(VI)  extraction degree (1), stripping degree (2) and flux into the strip solution (3) on the K2Cr2O7   initial concentration (i = 10.6 mА сm-2; t = 100 min; CTOA = 0.2 mol L-1; CD2EHPA = 10 vol.%)

 
[image: image4.wmf]0

50

100

150

200

0

60

120

180

240

Time, min

Voltage, V


Change in voltage during electrodialysis for various  membrane systems (i (mА сm-2) = 6.4 (3, 5, 6); 12.7 (1, 2, 4); 

CТОА (mol L-1) = 0.1 (4, 6); 0.2 (1, 2, 3, 5); CD2EHPA (vol. %) = 10 (1, 3, 4, 6); 0 (2, 5); CHCl (mol L-1)  = 0.01 (1, 3); 0.1 (2, 4, 5, 6))

Effect of the current density on the chromium(VI) extraction degree E, stripping degree S and flux J for various HCl, D2EHPA and TOA concentrations in the system.a 

	i 

(mА сm-2)
	t 

(min)
	cHCl 

 (mol L-1)

	Liquid membrane
	E
	S


	JCr∙105 
(mol m-2 s-1)

	
	
	
	CTOA  (M)
	CD2EHPA,(vol.%)
	(%)
	

	0
	120
	0.1
	0.1
	10
	25.7
	0
	0

	4.2
	173
	0.01
	0.2
	10
	99.8
	85
	3.0

	6.4
	109
	0.01
	0.2
	10
	99.7
	84
	4.6

	8.5
	86
	0.01
	0.2
	10
	99.4
	86
	6.0

	10.6
	73
	0.01
	0.2
	10
	99.0
	84
	7.0

	12.7
	53
	0.01
	0.2
	10
	98.4
	80
	9.0

	4.2
	216
	0.1
	0.2
	0
	99.6
	70
	2.0

	6.4
	157
	0.1
	0.2
	0
	99.3
	72
	2.8

	8.5
	122
	0.1
	0.2
	0
	99.2
	67
	3.4

	10.6
	109
	0.1
	0.2
	0
	98.9
	65
	3.6

	12.7
	90
	0.1
	0.2
	0
	98.7
	66
	4.4

	6.4
	235
	0.1
	0.1
	10
	100.0
	85
	2.2

	8.5
	159
	0.1
	0.1
	10
	99.8
	80
	3.0

	10.6
	168
	0.1
	0.1
	10
	99.6
	89
	3.2

	12.7
	132
	0.1
	0.1
	10
	99.2
	85
	3.8

	14.9
	122
	0.1
	0.1
	10
	99.3
	83
	4.0


a  CCr = 0.01 mol L-1; strip solution – 0.1 mol L-1   HCl

Effect of the strip  solution composition, D2EHPA and TOA concentration in the liquid membrane on the chromium(VI) transport.a

	CTOA 

 (mol L-1)

	CD2EHPA

 (vol.%)
	Strip solution

(C = 0.1 mol L-1)
	Е
	S
	JCr∙105 
(mol m-2 s-1)

	
	
	
	(%)
	

	0.05
	10
	 HCl
	64
	49
	3.0

	0.1
	10
	 HCl
	66
	46
	2.8

	0.2
	10
	 HCl
	74
	55
	3.4

	0.3
	10
	 HCl
	80
	55
	3.4

	0.4
	10
	 HCl
	79
	55
	3.4

	0.2
	  0
	 HCl
	93
	64
	4.0

	0.2
	  5
	 HCl
	77
	60
	3.6

	0.2
	20
	 HCl
	66
	46
	2.8

	0.2
	40
	 HCl
	62
	47
	2.8

	0.1
	10
	H2O
	74
	73
	4.4

	0.1
	10
	 H3PO4
	70
	55
	3.4

	0.1
	10
	 H2SO4
	71
	49
	3.0

	0.1
	10
	 HClO4
	70
	48
	3.0


a   CCr = 0.01 mol L-1; i = 10.6 mА сm-2; t = 100 min.

2





3





 −























 +























2





1





3





1








								   HA							        	


         H2				H+			    			          H+			 	  O2


			                			     A(							 


        					    	         									


     	  H+		  	H+  				R3NHA			   H+    	     	H+	


       			     			 	 HA		 R3N															       2R3NH+


    				   Cr2O72‒		 Cr2O72‒		     Cr2O72‒


  	H+			H+  			   (R3NH)2Cr2O7		      H+  		H+  	      SO42(


R3NH+


   	SO42(		 Cl(						      Cl(			


					    			R3NHCl


        													           																		     


   				          										H+  		(				 H+	    	         						       				


	 H2O												


							  		


     		  									


													  	       					  						   	   			


      	  																	


			  		      											ClO4−


     						     				  


	H+		  	  	   		      				


				   						      				  																


									    	   


																	








			  		 


       ClO4−						         ClO4−				   		  Oct3NHClO4





	NO3−		  Oct3NH+		      ClO4−














				   				





2





3





6





5





4





3





2





1




















1








_1608029454.xls
Chart2

		0		0		0

		35		35		35

		70		70		70

		100		100		100

		130		130		130

		168		168		168



Feed solution

Strip solution

Liquid membrane

Time, min

Cr  content, %

100

0

0

71.5

19.3

9.2

51.7

31.6

16.7

33.6

45.9

20.5

19.4

60.9

19.7

0.4

88.9

10.7



Sheet1

		0,1T+10D										0,2M TOA												0,2T+10D

		45mA				90mA						45mA						90mA						45mA						90mA

		t		U		t		U				t		U				t		U				t		U				t		U

		3		33		7		62				4		75				10		102				4		24				6		43

		15		29		14		57				10		49				15		74				15		26				20		55

		35		29		23		52				22		35				26		38				31		29				30		54

		53		27		31		19				42		25										56		31				40		54.5

		68		26		43		22.5				53		23.5				50		24				84		32				48		68

		81		15.5		55		21				75		21				60		24				95		43				50		78

		97		15		66		21.5				107		23.6				75		29				100		52				51		89

		117		14		77		23.5				122		27				84		47				103		68				52		107

		145		15		90		27				132		27				89		89				105		80				53		150

		160		16		100		31.5				140		32				91		200				107		103				54		200

		180		18.6		107		39				146		39										108		128

		198		23		115		48				150		49										109		163

		214		37		120		53				153		62										110		200

		225		60		125		62				154		74

		229		84.5		128		74				155		94

		231		104		130		90				156		128

		232		133		131		111				157		200

		233		145		132		151

		234		165		133		200

		235		200

								Fig.2

				0,2T+10D				0,2M TOA						0,1T+10D

		i		j*105				i		j*105				i		j*105

		0		0				0		0				0		0

		4.2		2.94				4.2		1.99				6.4		2.22

		6.4		4.64				6.4		2.82				8.5		2.78

		8.5		6				8.5		3.38				10.6		3.16

		10.6		7				10.6		3.66				12.7		3.84

		12.7		9				12.7		4.48				14.9		4.04

								Fig.3				Fig.4a										Fig.4b

		t		исх.р-р		прин.р-р		жд.ммб.				CCr *10-1 M		E, %		R, %		j*105				CHCl, M		E, %		R, %		J*106

		0		100		0		0				0.0043		79.6		58.7		1.55				0.01		99		84		66

		35		71.5		19.3		9.2				0.0099		74		55.1		3.38				0.05		92		79.8		48.2

		70		51.7		31.6		16.7				0.049		59.1		46.9		14				0.1		74		55.1		33.8

		100		33.6		45.9		20.5				0.099		45		30.9		18.8				0.5		39.5		17.8		10.2

		130		19.4		60.9		19.7														1		38		21.3		12.2

		168		0.4		88.9		10.7

								Fig.5

		0,01MHCl						0,1MHCl						0,1MCr						1MHCl

		t		U				t		U				t		U				t		U

		6		36				6		30				6		29				7		23

		12		39				14		33				13		28				13		21

		16		41				21		36				22		28				24		19

		20		43				28		38.4				25		13.6				31		18

		25		46				38		39				34		13				40		16.5

		30		49				45		39				42		12				45		16

		40		44.5				61		39				55		12				58		14.5

		53		42				71		33				70		10.4				64		13.5

		60		51				77		32				80		10.4				69		5.3

		65		61				86		31				90		10.7				76		5.5

		67		71				95		27				95		10.6				88		5.5

		70		93				100		27										99		5.6

		72		120

								Fig.6

						0,05MTOA						0,4MTOAc						0,4MTOA						0D2						40D2

						t		U				t		U				t		U				t		U				t		U

						10		119				8		41				7		25				8		112				7		68

						17		95				20		40				21		24.6				13		77.5				14		42

						21		12.5				32		42				40		27				23		42				33		38

						27		12.5				40		47.5				60		28				36		32				50		37.6

						35		13.4				49		55.4				90		27				53		25				67		19

						47		13.4				55		74				100		26				77		27				88		19

						56		14.2				58		104										93		37				100		20

						61		14.6				60		134										100		44

						75		16.8				61		169

						81		17.4				62		200

						100		19

				CHCl

				0.01		99

				0.05		92

				0.1		74

				0.5		Feb-00

				1		38





Sheet1

		



Feed solution

Strip solution

Liquid membrane

Time, min

Cr  content, %



Sheet2

		



Time, min

Voltage, V



Sheet3

		



Current density, mA cm-2

Flux 105, mol m-2 s-1



		



Cr  concentration, mol L-1

Flux 105, mol m-2 s-1
 E, S, %



		



HCl concentration, mol/L

Flux, mmol/m2s
 E, S, %



		



t

U



		



t

U



		

		1





		






_1608030227.xls
Chart3

		0.0043		0.0043		0.0043

		0.0099		0.0099		0.0099

		0.049		0.049		0.049

		0.099		0.099		0.099



Cr  concentration, mol L-1

Flux 105, mol m-2 s-1
 E, S, %

79.6

58.7

1.55

74

55.1

3.38

59.1

46.9

14

45

30.9

18.8



Sheet1

		0,1T+10D										0,2M TOA												0,2T+10D

		45mA				90mA						45mA						90mA						45mA						90mA

		t		U		t		U				t		U				t		U				t		U				t		U

		3		33		7		62				4		75				10		102				4		24				6		43

		15		29		14		57				10		49				15		74				15		26				20		55

		35		29		23		52				22		35				26		38				31		29				30		54

		53		27		31		19				42		25										56		31				40		54.5

		68		26		43		22.5				53		23.5				50		24				84		32				48		68

		81		15.5		55		21				75		21				60		24				95		43				50		78

		97		15		66		21.5				107		23.6				75		29				100		52				51		89

		117		14		77		23.5				122		27				84		47				103		68				52		107

		145		15		90		27				132		27				89		89				105		80				53		150

		160		16		100		31.5				140		32				91		200				107		103				54		200

		180		18.6		107		39				146		39										108		128

		198		23		115		48				150		49										109		163

		214		37		120		53				153		62										110		200

		225		60		125		62				154		74

		229		84.5		128		74				155		94

		231		104		130		90				156		128

		232		133		131		111				157		200

		233		145		132		151

		234		165		133		200

		235		200

								Fig.2

				0,2T+10D				0,2M TOA						0,1T+10D

		i		j*105				i		j*105				i		j*105

		0		0				0		0				0		0

		4.2		2.94				4.2		1.99				6.4		2.22

		6.4		4.64				6.4		2.82				8.5		2.78

		8.5		6				8.5		3.38				10.6		3.16

		10.6		7				10.6		3.66				12.7		3.84

		12.7		9				12.7		4.48				14.9		4.04

								Fig.3				Fig.4a										Fig.4b

		t		исх.р-р		прин.р-р		жд.ммб.				CCr *10-1 M		E, %		R, %		j*105				CHCl, M		E, %		R, %		J*106

		0		100		0		0				0.0043		79.6		58.7		1.55				0.01		99		84		66

		35		71.5		19.3		9.2				0.0099		74		55.1		3.38				0.05		92		79.8		48.2

		70		51.7		31.6		16.7				0.049		59.1		46.9		14				0.1		74		55.1		33.8

		100		33.6		45.9		20.5				0.099		45		30.9		18.8				0.5		39.5		17.8		10.2

		130		19.4		60.9		19.7														1		38		21.3		12.2

		168		0.4		88.9		10.7

								Fig.5

		0,01MHCl						0,1MHCl						0,1MCr						1MHCl

		t		U				t		U				t		U				t		U

		6		36				6		30				6		29				7		23

		12		39				14		33				13		28				13		21

		16		41				21		36				22		28				24		19

		20		43				28		38.4				25		13.6				31		18

		25		46				38		39				34		13				40		16.5

		30		49				45		39				42		12				45		16

		40		44.5				61		39				55		12				58		14.5

		53		42				71		33				70		10.4				64		13.5

		60		51				77		32				80		10.4				69		5.3

		65		61				86		31				90		10.7				76		5.5

		67		71				95		27				95		10.6				88		5.5

		70		93				100		27										99		5.6

		72		120

								Fig.6

						0,05MTOA						0,4MTOAc						0,4MTOA						0D2						40D2

						t		U				t		U				t		U				t		U				t		U

						10		119				8		41				7		25				8		112				7		68

						17		95				20		40				21		24.6				13		77.5				14		42

						21		12.5				32		42				40		27				23		42				33		38

						27		12.5				40		47.5				60		28				36		32				50		37.6

						35		13.4				49		55.4				90		27				53		25				67		19

						47		13.4				55		74				100		26				77		27				88		19

						56		14.2				58		104										93		37				100		20

						61		14.6				60		134										100		44

						75		16.8				61		169

						81		17.4				62		200

						100		19

				CHCl

				0.01		99

				0.05		92

				0.1		74

				0.5		Feb-00

				1		38





Sheet1

		0		0		0

		0		0		0

		0		0		0

		0		0		0

		0		0		0

		0		0		0



Feed solution

Strip solution

Liquid membrane

Time, min

Cr  content, %

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0



Sheet2

		0		0		0		0		0		0

		0		0		0		0		0		0

		0		0		0		0		0		0

		0		0		0		0		0		0

		0		0		0		0		0		0

		0		0		0		0		0		0

		0		0		0		0		0		0

		0		0		0		0		0		0

		0		0		0		0		0		0

		0		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0

		0		0		0		0

		0		0		0		0

		0		0		0

		0		0

		0		0

		0		0

		0		0

		0		0

		0		0

		0		0

		0		0

		0		0

		0



Time, min

Voltage, V

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0



Sheet3

		0		0		0

		0		0		0

		0		0		0

		0		0		0

		0		0		0

		0		0		0



Current density, mA cm-2

Flux 105, mol m-2 s-1

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0



		0		0		0

		0		0		0

		0		0		0

		0		0		0



Cr  concentration, mol L-1

Flux 105, mol m-2 s-1
 E, S, %

0

0

0

0

0

0

0

0

0

0

0

0



		0		0		0

		0		0		0

		0		0		0

		0		0		0

		0		0		0



HCl concentration, mol/L

Flux, mmol/m2s
 E, S, %

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0



		0		0		0		0

		0		0		0		0

		0		0		0		0

		0		0		0		0

		0		0		0		0

		0		0		0		0

		0		0		0		0

		0		0		0		0

		0		0		0		0

		0		0		0		0

		0		0		0		0

		0		0				0

		0

		0

		0



t

U

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0



		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0						0

		0		0

		0

		0



t

U

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0



		

		1





		






_1608030982.xls
Chart4

		3		7		4		10		4		6

		15		14		10		15		15		20

		35		23		22		26		31		30

		53		31		42				56		40

		68		43		53		50		84		48

		81		55		75		60		95		50

		97		66		107		75		100		51

		117		77		122		84		103		52

		145		90		132		89		105		53

		160		100		140		91		107		54

		180		107		146				108

		198		115		150				109

		214		120		153				110

		225		125		154

		229		128		155

		231		130		156

		232		131		157

		233		132

		234		133

		235



Time, min

Voltage, V

33

62

75

102

24

43

29

57

49

74

26

55

29

52

35

38

29

54

27

19

25

31

54.5

26

22.5

23.5

24

32

68

15.5

21

21

24

43

78

15

21.5

23.6

29

52

89

14

23.5

27

47

68

107

15

27

27

89

80

150

16

31.5

32

200

103

200

18.6

39

39

128

23

48

49

163

37

53

62

200

60

62

74

84.5

74

94

104

90

128

133

111

200

145

151

165

200

200



Sheet1

		0,1T+10D										0,2M TOA												0,2T+10D

		45mA				90mA						45mA						90mA						45mA						90mA

		t		U		t		U				t		U				t		U				t		U				t		U

		3		33		7		62				4		75				10		102				4		24				6		43

		15		29		14		57				10		49				15		74				15		26				20		55

		35		29		23		52				22		35				26		38				31		29				30		54

		53		27		31		19				42		25										56		31				40		54.5

		68		26		43		22.5				53		23.5				50		24				84		32				48		68

		81		15.5		55		21				75		21				60		24				95		43				50		78

		97		15		66		21.5				107		23.6				75		29				100		52				51		89

		117		14		77		23.5				122		27				84		47				103		68				52		107

		145		15		90		27				132		27				89		89				105		80				53		150

		160		16		100		31.5				140		32				91		200				107		103				54		200

		180		18.6		107		39				146		39										108		128

		198		23		115		48				150		49										109		163

		214		37		120		53				153		62										110		200

		225		60		125		62				154		74

		229		84.5		128		74				155		94

		231		104		130		90				156		128

		232		133		131		111				157		200

		233		145		132		151

		234		165		133		200

		235		200

								Fig.2

				0,2T+10D				0,2M TOA						0,1T+10D

		i		j*105				i		j*105				i		j*105

		0		0				0		0				0		0

		4.2		2.94				4.2		1.99				6.4		2.22

		6.4		4.64				6.4		2.82				8.5		2.78

		8.5		6				8.5		3.38				10.6		3.16

		10.6		7				10.6		3.66				12.7		3.84

		12.7		9				12.7		4.48				14.9		4.04

								Fig.3				Fig.4a										Fig.4b

		t		исх.р-р		прин.р-р		жд.ммб.				CCr *10-1 M		E, %		R, %		j*105				CHCl, M		E, %		R, %		J*106

		0		100		0		0				0.0043		79.6		58.7		1.55				0.01		99		84		66

		35		71.5		19.3		9.2				0.0099		74		55.1		3.38				0.05		92		79.8		48.2

		70		51.7		31.6		16.7				0.049		59.1		46.9		14				0.1		74		55.1		33.8

		100		33.6		45.9		20.5				0.099		45		30.9		18.8				0.5		39.5		17.8		10.2

		130		19.4		60.9		19.7														1		38		21.3		12.2

		168		0.4		88.9		10.7

								Fig.5

		0,01MHCl						0,1MHCl						0,1MCr						1MHCl

		t		U				t		U				t		U				t		U

		6		36				6		30				6		29				7		23

		12		39				14		33				13		28				13		21

		16		41				21		36				22		28				24		19

		20		43				28		38.4				25		13.6				31		18

		25		46				38		39				34		13				40		16.5

		30		49				45		39				42		12				45		16

		40		44.5				61		39				55		12				58		14.5

		53		42				71		33				70		10.4				64		13.5

		60		51				77		32				80		10.4				69		5.3

		65		61				86		31				90		10.7				76		5.5

		67		71				95		27				95		10.6				88		5.5

		70		93				100		27										99		5.6

		72		120

								Fig.6

						0,05MTOA						0,4MTOAc						0,4MTOA						0D2						40D2

						t		U				t		U				t		U				t		U				t		U

						10		119				8		41				7		25				8		112				7		68

						17		95				20		40				21		24.6				13		77.5				14		42

						21		12.5				32		42				40		27				23		42				33		38

						27		12.5				40		47.5				60		28				36		32				50		37.6

						35		13.4				49		55.4				90		27				53		25				67		19

						47		13.4				55		74				100		26				77		27				88		19

						56		14.2				58		104										93		37				100		20

						61		14.6				60		134										100		44

						75		16.8				61		169

						81		17.4				62		200

						100		19

				CHCl

				0.01		99

				0.05		92

				0.1		74

				0.5		Feb-00

				1		38





Sheet1

		0		0		0

		0		0		0

		0		0		0

		0		0		0

		0		0		0

		0		0		0



Feed solution

Strip solution

Liquid membrane

Time, min

Cr  content, %

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0



Sheet2

		0		0		0		0		0		0

		0		0		0		0		0		0

		0		0		0		0		0		0

		0		0		0		0		0		0

		0		0		0		0		0		0

		0		0		0		0		0		0

		0		0		0		0		0		0

		0		0		0		0		0		0

		0		0		0		0		0		0

		0		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0

		0		0		0		0

		0		0		0		0

		0		0		0

		0		0

		0		0

		0		0

		0		0

		0		0

		0		0

		0		0

		0		0

		0		0

		0



Time, min

Voltage, V

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0



Sheet3

		0		0		0

		0		0		0

		0		0		0

		0		0		0

		0		0		0

		0		0		0



Current density, mA cm-2

Flux 105, mol m-2 s-1

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0



		0		0		0

		0		0		0

		0		0		0

		0		0		0



Cr  concentration, mol L-1

Flux 105, mol m-2 s-1
 E, S, %

0

0

0

0

0

0

0

0

0

0

0

0



		0		0		0

		0		0		0

		0		0		0

		0		0		0

		0		0		0



HCl concentration, mol/L

Flux, mmol/m2s
 E, S, %

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0



		0		0		0		0

		0		0		0		0

		0		0		0		0

		0		0		0		0

		0		0		0		0

		0		0		0		0

		0		0		0		0

		0		0		0		0

		0		0		0		0

		0		0		0		0

		0		0		0		0

		0		0				0

		0

		0

		0



t

U

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0



		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0						0

		0		0

		0

		0



t

U

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0



		

		1





		






_1608029100.xls
Chart1

		0		0		0

		4.2		4.2		6.4

		6.4		6.4		8.5

		8.5		8.5		10.6

		10.6		10.6		12.7

		12.7		12.7		14.9



Current density, mA cm-2

Flux 105, mol m-2 s-1

0

0

0

2.94

1.99

2.22

4.64

2.82

2.78

6

3.38

3.16

7

3.66

3.84

9

4.48

4.04



Sheet1

		0,1T+10D										0,2M TOA												0,2T+10D

		45mA				90mA						45mA						90mA						45mA						90mA

		t		U		t		U				t		U				t		U				t		U				t		U

		3		33		7		62				4		75				10		102				4		24				6		43

		15		29		14		57				10		49				15		74				15		26				20		55

		35		29		23		52				22		35				26		38				31		29				30		54

		53		27		31		19				42		25										56		31				40		54.5

		68		26		43		22.5				53		23.5				50		24				84		32				48		68

		81		15.5		55		21				75		21				60		24				95		43				50		78

		97		15		66		21.5				107		23.6				75		29				100		52				51		89

		117		14		77		23.5				122		27				84		47				103		68				52		107

		145		15		90		27				132		27				89		89				105		80				53		150

		160		16		100		31.5				140		32				91		200				107		103				54		200

		180		18.6		107		39				146		39										108		128

		198		23		115		48				150		49										109		163

		214		37		120		53				153		62										110		200

		225		60		125		62				154		74

		229		84.5		128		74				155		94

		231		104		130		90				156		128

		232		133		131		111				157		200

		233		145		132		151

		234		165		133		200

		235		200

								Fig.2

				0,2T+10D				0,2M TOA						0,1T+10D

		i		j*105				i		j*105				i		j*105

		0		0				0		0				0		0

		4.2		2.94				4.2		1.99				6.4		2.22

		6.4		4.64				6.4		2.82				8.5		2.78

		8.5		6				8.5		3.38				10.6		3.16

		10.6		7				10.6		3.66				12.7		3.84

		12.7		9				12.7		4.48				14.9		4.04

								Fig.3				Fig.4a										Fig.4b

		t		исх.р-р		прин.р-р		жд.ммб.				CCr *10-1 M		E, %		R, %		j*105				CHCl, M		E, %		R, %		J*106

		0		100		0		0				0.0043		79.6		58.7		1.55				0.01		99		84		66

		35		71.5		19.3		9.2				0.0099		74		55.1		3.38				0.05		92		79.8		48.2

		70		51.7		31.6		16.7				0.049		59.1		46.9		14				0.1		74		55.1		33.8

		100		33.6		45.9		20.5				0.099		45		30.9		18.8				0.5		39.5		17.8		10.2

		130		19.4		60.9		19.7														1		38		21.3		12.2

		168		0.4		88.9		10.7

								Fig.5

		0,01MHCl						0,1MHCl						0,1MCr						1MHCl

		t		U				t		U				t		U				t		U

		6		36				6		30				6		29				7		23

		12		39				14		33				13		28				13		21

		16		41				21		36				22		28				24		19

		20		43				28		38.4				25		13.6				31		18

		25		46				38		39				34		13				40		16.5

		30		49				45		39				42		12				45		16

		40		44.5				61		39				55		12				58		14.5

		53		42				71		33				70		10.4				64		13.5

		60		51				77		32				80		10.4				69		5.3

		65		61				86		31				90		10.7				76		5.5

		67		71				95		27				95		10.6				88		5.5

		70		93				100		27										99		5.6

		72		120

								Fig.6

						0,05MTOA						0,4MTOAc						0,4MTOA						0D2						40D2

						t		U				t		U				t		U				t		U				t		U

						10		119				8		41				7		25				8		112				7		68

						17		95				20		40				21		24.6				13		77.5				14		42

						21		12.5				32		42				40		27				23		42				33		38

						27		12.5				40		47.5				60		28				36		32				50		37.6

						35		13.4				49		55.4				90		27				53		25				67		19

						47		13.4				55		74				100		26				77		27				88		19

						56		14.2				58		104										93		37				100		20

						61		14.6				60		134										100		44

						75		16.8				61		169

						81		17.4				62		200

						100		19

				CHCl

				0.01		99

				0.05		92

				0.1		74

				0.5		Feb-00

				1		38





Sheet1

		0		0		0

		0		0		0

		0		0		0

		0		0		0

		0		0		0

		0		0		0



Feed solution

Strip solution

Liquid membrane

Time, min

Cr  content, %

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0



Sheet2

		



Time, min

Voltage, V



Sheet3

		



Current density, mA cm-2

Flux 105, mol m-2 s-1



		0		0		0

		0		0		0

		0		0		0

		0		0		0



Cr  concentration, mol L-1

Flux 105, mol m-2 s-1
 E, S, %

0

0

0

0

0

0

0

0

0

0

0

0



		0		0		0

		0		0		0

		0		0		0

		0		0		0

		0		0		0



HCl concentration, mol/L

Flux, mmol/m2s
 E, S, %

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0



		0		0		0		0

		0		0		0		0

		0		0		0		0

		0		0		0		0

		0		0		0		0

		0		0		0		0

		0		0		0		0

		0		0		0		0

		0		0		0		0

		0		0		0		0

		0		0		0		0

		0		0				0

		0

		0

		0



t

U

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0



		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0						0

		0		0

		0

		0



t

U

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0



		

		1





		






