[image: image1.png]Anolyte CEM  Feed solution  Liquid membrane Catholyte

R;NHA

Pb> / R;NH\ Pb*

\PhA, 7

H0
RNHA
-
H , H . JRNH H*
HA

|

clos A clos
sNHCIO,





Scheme of the membrane extraction of Pb(II) ions during electrodialysis

(CEM: cation-exchange membrane)

[image: image2.png]o o =3 =]
% o < Q

ul
S urouny

% /d°s‘d

=3
S

15

12.5

5 75 2 10
i/mA cm”

25




Effect of current density on the extraction degree E, stripping degree S, electrodeposition degree D and  flux J of lead(II)

(catholyte: 0.2 M HClO4; t  = 100 min)
[image: image3.png]u/v

40

30

20

—+-3.5 =71 —+10.6 + 14.1 mA cm-2

20 40 60 80
t/min

100




Change in potential difference during electrodialysis for different current densities (catholyte: 0.2 M  HClO4)

[image: image4.png]100

_ 80
.,\°Z;
Q_EGO
v £
m’\i40
20

—~E S —+D =]

0

0.02

0.04 0.06
Cpp, /M

0.08

0.1




Effect of the initial lead(II) ion concentration on the extraction degree E, stripping degree S, electrodeposition degree D and flux  J (i = 10.6 mА∙сm-2; t  = 100 min)
[image: image5.png]100

80

E.S.D/%

«E +S «D

.

.

20
Cpagnpa / vol %

30

40




Effect of D2EHPA concentration in the liquid membrane on the lead(II) extraction degree E, stripping degree  S and electrodeposition degree D

(i = 10.6 mА∙сm-2; t = 100 min; CTOA = 0.1 M)

[image: image6.png]100 + Feed + Strip + Deposition





Kinetics of lead(II) removal  from the feed solution, accumulation in the strip solution and electrodeposition (i = 10.6 mА∙сm-2; catholyte: 0.2 M  HClO4)

[image: image7.png]



Light microscopy image of the lead coating deposited from 0.2 M HClO4  on the platinum cathode at the current density of 10.6 mА∙сm-2
Effect of the stripping solution (catholyte) composition on the Pb(II) extraction degree E, stripping degree S, electrodeposition degree D and flux J a
	С (M) 
	Catholyte
	Е (%)
	S (%)
	D (%)
	S+D (%)
	J (μmol∙m-2∙s-1)

	0.05
	HClO4
	88
	4
	21
	25
	8

	0.1
	HClO4
	89
	7
	33
	40
	12

	0.2
	HClO4
	81
	12
	27
	39
	12

	0.3
	HClO4
	74
	13
	24
	37
	11

	0.5
	HClO4
	69
	10
	27
	37
	11

	1.0
	HClO4
	62
	9
	28
	37
	11

	0.2
	HNO3
	80
	16
	17
	33
	10

	0.2
	CH3COOH
	96
	16
	22
	38
	12


a   i = 10.6 mA∙cm-2; t = 100 min.

