##### Supporting Information

##### DENDRONIZED AZOCHROMOPHORES WITH AROMATIC AND PERFLUOROAROMATIC FRAGMENTS: SYNTHESIS AND PROPERTIES DEMONSTRATING Ar-ArF INTERACTIONS

Lauma Laipniece,a Valdis Kampars,a Sergey Belyakov,a,b Andrejs Tokmakovs,c Edgars Nitiss,c and Martins Rutkisc

a Institute of Applied Chemistry, Faculty of Materials Science and Applied Chemistry, Riga Technical University, P. Valdena 3/7, Riga, LV-1048, Latvia

b Latvian Institute of Organic Synthesis, Aizkraukles 21, Riga, LV-1006, Latvia

c Institute of Solid State Physics, University of Latvia, Kengaraga 8, Riga, LV-1063, Latvia

Figure S1. Experimental set up for second harmonic intensity (SHI) investigations: BS - beam splitter; GP - Glan polarizer, L - lens, HPF - high past filter, SM - selective mirror, LPF - low past filter, IF - interference filter (λ = 532 nm), SH - shutter, λ/2 - half-wave plate (λ = 1064 nm), STM - step motor, ADL - alignment diode laser, NDF - neutral density filter, A - analyzer, PMT - photo multiplier tube.

Figure S2. Structures of synthesized new dendronized azochromophores.

Tg = 37 oC

Tg = 44 oC

Tg = 53 oC

Tg = 60 oC

Tg = 58 oC

Tg = 46 oC

Tg = 60 oC

Figure S3. DSC curves of synthesized azochromophores recorded during the second heating. The glass transition temperatures (Tg) are indicated for each compound.

Figure S4. DSC curves of chromophore blends recorded during the second heating. The glass transition temperature is indicated.

Figure S5. TGA curves of synthesized azochromophores.

Figure S6. 1H NMR spectrum of compound 11.

Figure S7. 1H NMR spectrum of compound 12.

Figure S8. 1H NMR spectrum of compound 13.

Figure S9. 1H NMR spectrum of compound 14.

Figure S10. 1H NMR spectrum of compound 16.

Figure S11. 1H NMR spectrum of compound 17.

Figure S12. 13C NMR spectrum of compound 12.

Figure S13. 13C NMR spectrum of compound 14.

Figure S14. 13C NMR spectrum of compound 16.

Figure S15. 13C NMR spectrum of compound 17.