The whiteness degree and colour properties of recycled

Polyethylene terephthalate fibres

Population, economic growth and industrialization in the world increase the amount of waste. A waste policy should be developed and the studies of the waste management should be carried out, especially in the environment causing landfill problems.

Recycled polyethylene terephthalate (r-PET) is a widely recycled plastic employed for new textile production in the world. It reduces environmental impact and lowers cost of the production [1].

The influence of the anionic detergent Felosan FOX (CHT/Bezema Group) on the whitness degree and the colour properties of r-PET fibres was determined.

Research steps

- Pre treating  of r-PET fibres

- Testing of whiteness

- Testing of colour properties

# Materials and methods

# Material

# For pre treating  the recycled polyethylene terephthalate fibres (designation r-PET; length 60±2 mm, Starlinger, Uzbekistan [2]) with density of 6den, 15 den, 20 den and 40 den were used.

# Chemical

# For r-PET fibres the pre-treatment in the solution (2 g/L)  the anionic detergent Felosan FOX (CHT/Bezema Group [2]) at 73 ± 3°C for 60 min was applied. The rinse in warm running water and drying at room temperature (20 ±2°C ) followed.

## Testing

## Whiteness degree. For assessing the pre-treatment effect of r-PET fibres whiteness degree before and after washing was determined with Novo-Shade Duo reflectometer (Rhopoint, USA). Equipment indicates a shade of surface colour based on lightness / darkness, where 0 – corresponds to a completely black and 100 - totally white. 10 measurements were read and the average value of whiteness degree was calculated.

## Colour properties. Colour parameters of samples were carried out in the spectral width of 400 to 700 nm with Easy Colour QA device (Pocket Spec. Technologies Inc. USA), using RGB (red, green and blue light) system in CIELAB-76 colour space, which allows to determine the coordinates of colour vectors a*, b* and L*- the degree of lightness in the colour space. The differences in lightness (ΔL*ab) between sample and standard (r-PET fibres without pre treating), the common colour diference (ΔE*ab), the saturation diference (ΔC*ab) and hue (h ab) were calculated following the ISO 105-JO3:2009 [4].

# Results

# Table 1 Whiteness degree of r-PET fibres before and after pretreating with the anionic detergent

| Sample | Without pre-treatment | With pre-treatment |
| --- | --- | --- |
| 40 den | 25,24 | 28,78 |
| 20 den | 27,94 | 28,54 |
| 15 den | 23,32 | 26,26 |
| 6 den | 26,56 | 29,34 |

# Table 2 Colour properties of r-PET fibres before (-) and after (+) pretreating with the anionic detergent

| Sample | 40 den |  | 20 den |  | 15 den |  | 6 den |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Pre- treatment | - | + | - | + | - | + | - | + |
| L* | 64,84 | 69,07 | 67,73 | 70,33 | 70,27 | 71,21 | 74,29 | 74,91 |
| a* | 2,3 | 1,39 | 2,71 | 2,54 | 2,69 | 2,87 | 3,47 | 2,83 |
| b* | -4,04 | -3,22 | -5,15 | -5,48 | -5,7 | -4,91 | -5,4 | -4,28 |
| S | 4,65 | 3,51 | 5,82 | 6,04 | 6,3 | 5,69 | 6,42 | 5,13 |
| ∆L* |  | 4,23 |  | 2,6 |  | 0,94 |  | 0,62 |
| ∆a* |  | -0,91 |  | -0,17 |  | 0,18 |  | -0,64 |
| ∆b* |  | 37,18 |  | -0,33 |  | 0,79 |  | 1,12 |
| ∆E*ab |  | 37,43 |  | 2,63 |  | 1,24 |  | 1,43 |
| ∆C*ab |  | 32,54 |  | -5,44 |  | -5,49 |  | -5,13 |
| hab |  | -1,55 |  | 1,09 |  | 1,39 |  | -1,05 |

# References

# [1] E. Sariuglu, H. K. Kaynax, PET Bottle Recycling for Sustainable Textiles, In Tech OpenAccess (2018) 6-20.

# [2] https://www.starlinger.com/en/recycling/, rewie 02.12.2020.

# [3] Felosan FOX specification

# https://www.cht.com/cht/web.nsf/id/pa_promo_felosan_fox_en.html,

# rewie 02.12.2020.

# [4] ISO 105-JO3:2009  Textiles- Tests for colour fastness – Part J- 03: Calculation of colour differences