Colour fastness to washing of  recycled polyethylene terephthalate fibres dyed with disperse dye Itosperse Blue

In presented research the recycled polyethylene terephthalate fibres were dyed with disperse dyes Itosperse Blue (concentration 2 Wt. %) and the influence of the intensifier of a salicylic acid (with concentration of 4 g/L, 6 g/L, 8 g/L  and 10 g/L) in dye bath was investigated. The colour fastness to washing (5 cycles using anionic liquor) of r-PET fibres were tested.

Materials and methods

Material. For dyeing recycled polyethylene terephthalate fibres (length 60±2 mm, density of 6 den, 15 den, 20 den and 40 den, Starlinger, Uzbekistan [1]) were used.

# Chemicals.

# Detergent. The non- ionic detergent Felosan FOX (CHT/Bezema Group [2]) suitable for all fibres in discontinuous and continuous washing and bleaching processes was used for pre treating of fibres before dyeing.

Disperse dye. Itoperse Blue (Producer LJ Specialities LTD, UK) powder dispersible colouring agents was used for dyeing. The most important colouring agent class for the dyeing of chemical fibres and, above all, polyester fibres, as well as acetate, triacetate and polyamide fibres. It covers the whole colour gamut and provides high levels of colour resilience. It is valid for periodic and continuous dyeing method and printing [3].

Dispersor. Itosolt LJ 557LJ Specialities LTD (Producer LJSpecialities LTD, UK) was used. The dispersor makes easier for colorants to penetrate in deep layers of fibres, reduces diffusion time. Dispergator has low foaming, which eliminates problems resulting from foam formation in the dyeing process. The highest dispersive effect prevents discoloration from coagulation at elevated temperatures. Prevents uneven dyeing, staining and shading problems [4] stabilising a dispersion or solution.

Intensifier. Salicylic acid (C7H6O3) Sigma – Aldrich) acts as an intensifier in the dyeing bath [5]. Adding salicylic acid to the dye- bath speeds up the dyeing rate and then gained higher paint strength. An intensifier (salicylic acid) of polyester fibres absorb and swell as well as enhances colour penetration in the fibre.

Methods

Pre-treating technology. Pre-treating or washing of  r-PET fibres with solution of Felosan FOX (2 g/l) at  temperature 72  ±  2 °C for 60 min before dyeing was done. The rinse in warm running water and drying at room temperature ( 20 ±  2 °C ) folowed.

Dyeing technology. The dyeing was prepared using the following technology:

- The required amount of distilled water (bath ratio = 50) was warmed up to 40 °C. 10 g of each r-PET fibres for dyeing were used.

- The 2% wt  of dye by weight of the textile material and disperator 10 g/l was added in hot distilled water 50-60 °C (of the total amount of distilled water) and very carefully sacked. Add the remaining amount of distilled water. At this stage, the dyeing bath is for the start  of dyeing.

- For part of sample after the above, an intensifier (salicylic acid) with a specified concentration (4 g/L, 6 g/L, 8 g/L or 10 g/L) was added. Dyeing was started at 40 °C, the temperature and lifted to 95± 2°C and dyed for 60 min. The fibres were rinsed in hot running water after dyeing to remove unfixed dyes.

Colour fastness to washing. Determination of colour fastness to washing of dyed r-PET fibres, the adapted standard ISO 105-C10:2006 [6] with using anionic liquor Felosan FOX (2 g/L), 5 washing cycles at temperature 45± 2 °C for 15 min was applied.

Testing of colour properties. Colour parameters of samples were carried out in the spectral width of 400 to 700 nm with Easy Colour QA device (Pocket Spec. Technologies Inc. USA), using RGB (red, green and blue light) system in CIELAB-76 colour space, which allows to determine the coordinates of colour vectors a*, b* and L*- the degree of lightness in the colour space. The differences in lightness (ΔL*ab) between sample and standard (dyed with Itoperse Blue r-PET fibres before washing), the common colour diference (ΔE*ab), the saturation diference (ΔC*ab) and hue (h ab) were calculated following the ISO 105-JO3:2009 [7].

Results

Table 1 Colour properties of recycled polyethylene terephthalate fibres dyed with disperse dye Itosperse Blue after 5 washing cycles

| Density of fibres | 40 den | 20 den |  | 15 den | 6 den |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Salicylic acid [g/L] in dye bath | 0 | 0 | 6 | 0 | 0 | 4 | 6 | 8 | 10 |
| L* | 46,16 | 44,88 | 41,00 | 48,02 | 47,76 | 36,80 | 38,67 | 47,69 | 39,86 |
| a* | -0,26 | 1,68 | 3,04 | 1,08 | 2,00 | 6,42 | 5,15 | 0,60 | 4,34 |
| b* | -28,56 | -31,87 | -34,03 | -31,46 | -33,47 | -38,95 | -37,65 | -32,28 | -36,88 |
| ∆L* | 6,18 | 4,5 | 2,87 | 6,53 | 5,00 | 5,72 | 6,02 | 11,23 | 7,44 |
| ∆a* | -2,68 | -0,14 | -1,82 | -1,67 | -2,86 | -5,72 | -5,04 | -7,05 | -4,35 |
| ∆b* | 2,45 | -1,36 | 1,67 | 1,19 | 1,12 | 1,17 | 2,36 | 2,59 | -0,10 |
| ∆E*ab | 7,17 | 4,70 | 3,79 | 6,84 | 5,87 | 8,17 | 8,20 | 13,51 | 8,62 |
| ∆C*ab | -9,58 | -0,50 | -3,63 | -2,15 | -6,36 | -28,25 | -25,41 | -48,9 | -14,58 |
| h ab | -0,74 | 1,47 | -0,74 | -0,62 | -0,37 | -0,20 | -0,44 | -0,35 | 0,02 |

References

# [1] https://www.starlinger.com/en/recycling/

# [2] Felosan FOX specification https://www.cht.com/cht/web.nsf/id/pa_promo_felosan_fox_en.html

[3] LJSpecialities LTD, UK Itosperse Blue Rap specification.

[4] J. Shore, Colorants and auxiliaries, Vol. 2. Auxilaries, Ed. J.Shore, pp. 191, 2002.

[5] M. Joshi Rashmi, V. Dhanabaln, S. K. Laga, Carrier dyeing: pros and cons., Textile Today, pp. 1-24, 2013.

# [6] ISO 105-C10:2006 Textiles -Tests for colour fastness - Part C10: Colour fastness to washing with soap or soap  and  soda

[7] ISO 105-JO3:2009  Textiles- Tests for colour fastness – Part J- 03: Calculation of colour differences