Cardolite Ultra Lite 513 (Cardanol-type material) modified with the silane Dynasylan 1189, forming a silyl-terminated prepolymer

- Color of prepolymer bright yellow

- Density of prepolymer 0.97 g/cm3

- Viscosity of prepolymer 48 mPa*s

Cardolite Ultra Lite 513 (Cardanol-type material) modified with the silane Dynasylan 1122, forming a silyl-terminated prepolymer

- Color of prepolymer orange

- Density of prepolymer 0.96 g/cm3

- Viscosity of prepolymer 54 mPa*s