Supplementary Materials

Analysis of bio-based acrylate accelerated weathering: A study of nanocellulose impact on the bulk durability of 3D-printed nanocomposites

Anda Barkane1*, Oskars Platnieks1, Jana Vecstaudza2, Sergejs Gaidukovs1

1Institute of Polymer Materials, Faculty of Materials Science and Applied Chemistry, Riga Technical University, P. Valdena 3/7, Riga LV-1048, Latvia

2Rudolfs Cimdins Riga Biomaterials Innovations and Development Centre of RTU, Institute of General Chemical Engineering, Faculty of Materials Science and Applied Chemistry, Riga Technical University, Pulka 3, Riga LV-1007, Latvia

Figure S.1. UV-VIS reflectance and transmittance spectra of the samples at 0 h (a), 250 h (b), 500 h (c), 750 h (d), and 1000 h (e) UV weathering

Table S1. UV-VIS measurement data at 500 nm

| Time | 0% |  |  | 0.1% |  |  | 0.5% |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | T, (%) | R, (%) | S, (%) | T, (%) | R, (%) | S, (%) | T, (%) | R, (%) | S, (%) |
| 0 h | 78.0 | 6.3 | 15.7 | 76.0 | 7.5 | 16.5 | 60.5 | 10.0 | 29.5 |
| 250 h | 62.0 | 5.7 | 32.3 | 56.0 | 5.0 | 39.0 | 45.5 | 8.7 | 45.8 |
| 500 h | 60.6 | 5.3 | 34.1 | 49.8 | 4.8 | 45.4 | 38.6 | 7.5 | 53.9 |
| 750 h | 48.3 | 5.7 | 46.0 | 50.0 | 5.7 | 42.3 | 36.8 | 7.0 | 56.2 |
| 1000 h | 49.0 | 5.5 | 45.5 | 47.8 | 5.0 | 47.2 | 37.0 | 8.2 | 54.8 |

Figure S2. FTIR spectra of 0% sample resin and TPO photoinitiator.

Figure 3. Photodegradation chemical changes evaluation: 0.1% sample FTIR spectra (a), and peak intensity ratios (b) and 0.5% sample FTIR spectra (c), and peak intensity ratios (d) during UV weathering.