Cotton Fabric Surface Modification by Sol-Gel Deposition of ZnO Thin Films
Svetlana Vihodceva1, Silvija Kukle2
1,2 Institute of Textile Materials Technology and Design, Riga Technical University, Latvia
e-mail: Svetlana.Vihodceva@rtu.lv
[image: image1.png]SEM MAG: 5.00 kx  Vac: HiVac
SEM HV: 15.00 kV WD: 11.0920 mm 20 um MIRA\ TESCAN g/
Date(m/d/y): 02/20/12 Det: BSE Detector Riga Technical University




Zinc oxide show high absorption in the ultraviolet (UV) region of the light spectrum, while absorption of visible light is quite low. In comparison with organic absorbers conventionally used in the textile industry, inorganic materials show no significant degradation and are therefore extremely stable and the oxides are classified as non-toxic materials. [1] Sols were prepared using sol-gel technology. Ethanol, tetraetoxysilane, distilled water and hydrochloric acid was stirred for 30 minutes, after stirring was added Zn acetate and for second variant ZnSO4. The fabric samples were immersed in the prepared sols, after samples was dried at 50ºC and cured in an oven at 120ºC. Experiment results show that a moderate thermal treatment at 120°C after the sol is applied to the cotton textile is appropriate. In this work comparison of coatings of samples prepared using Zn acetate or ZnSO4 was made (Fig.1.). 
SEM and laser laboratory complex were used to examine the nature of the surface modification with ZnO coating by the sol-gel technique as also after exploitation of samples; energy dispersive X-ray spectroscopy was used for the analysis of chemical composition of coated fabric samples. 
This work has been supported by the European Social Fund within the project «Support for the implementation of doctoral studies at Riga Technical University». 
References

1. Q. Weu, Surface modification of textiles. Woodhead Publ. in Textiles. 97 (2009)
�


Fig.1 SEM image of transparent ZnO coating on natural cotton textile fibers received with sol-gel technology used ZnSO4








