[image: image1.jpg]Maria S. Konsta-Gdoutos
Editor

Nanotechnology
in Construction

4™ International
Symposium

Co-sponsored by ACI

Agios Nikolaos, Crete, Greece
May 20-22, 2012



[image: image2.jpg]Post-Cracking Behaviour of High Strength (Nano-Level Designed) Fiber
Concrete Prediction and Validation
A. Krasnikovs, O. Kononova, A. az, E. Machanovsky, and A.Machanovsky

Graphene Nanoreinforcement for Cement-Based Composites
N. Zohhadi, N. Aich, F. Matta, N. Sale, and P. Ziehl

Carbon Nanofiber Cementitious Composites: Effect of Debulking Procedure
on Dispersion and Reinforcing Ability 64

Z.S. Metaxa, M.S. Konsta-Gdoutos, and S.P. Shah

Nanomaterials in Cultural Heritage

Physico-Chemical and Mechanical Characterization of Hydraulic Mortars
P. Maravelaki-Kalaitzaki, Z. Agioutantis, E. LmnalusCKaprldaAlSMayngranak:sM
Stavroulaki, V. Perdikatsis, A. Verganelaki, N. Kallithrakas-Kontos

Microbiologically Induced Cementation of CaCO; Nanoparticles for

Limestone Conservation 68
W. De Muynck, A.M. Kaczmarek, L. Fontaine, R. Van Deun, H. De Clercq,
W. Verstraete, and N. De Belie

Distribution of Nanosilica-based Consolidants in a Carbonatic Matrix__
E. Zendri, L. Falchi, L. Agostinetto, E. Balliana, G. Biscontin, and F.C.

M. Stefanidou

Applications of Nanomaterials in Construction

Tailor-Made Nano Materials for Corrosion Control and Improved Matrix
Characteristics in Cement-Based Systems _
D.A. Koleva, K. van Breugel, and J. Hu

Nanoporous Thin Films to Improve Precast Concrete Grout Bonding in Bridge Decks . 74
J.M. Sanfilippo Silva, M. Oliva and M.A. Anderson

Nano-engineered Cements With Improved Early Strength ¥3
Z. Lin, LF. Vivian and K. Sobolev

Investigation on Hydraulic Conductivity and Desiccation Crack Behaviour
of Compacted Soil-Neno Alumisa Mixtare. . (.. . oo 76
MR. Taha and O.M. Eldeen Taha

Adaptation of Aerospace Advanced Technology to Nano-Composite
Evbanced Concrete INMOaSMChmes, .. . .. ... s 7
C.C. Chamis

xi



[image: image3.jpg]1h . . > . 7
4" International Symposium on Nanotechnology in Construction

POST-CRACKING BEHAVIOUR OF HIGH STRENGTH
(NANO-LEVEL DESIGNED) FIBER CONCRETE
PREDICTION AND VALIDATION

A. Krasnikovs, O. Kononova, A. Khabbaz, E. Machanovsky, A. Machanovsky

Riga Technical University, Mechanical institute
Ezermalas street 6, Riga LV-1006, Latvia
akrasn@lametlv olga.kononovawzgmail.com khabbaz966@hotmail.com
edgars.macanovskis@rtuly artursmacanovskis@inbox.lv

Summary

Fracture process in mechanically loaded steel fiber reinforced high-strength (SFRHSC) concrete is
characterized by fibers bridging the crack providing resistance to its opening. Important role in con-
crete matrix mechanical behavior (stiffness, friction properties to steel, bond to steel) is playing nano-
level mix design and granulometry. Structural SFRHSC fracture model was created; material fracture
process was modeled, based on single fiber pull-out laws (See FIGURE 1), which were determined
experimentally (for straight fibers, fibers with end hooks (Dramix), and corrugated fibers (Tabix)) as
well as obtained numerically (using FEM simulations) Armelin and Banthia [1], Robins and et al. [2].
For this purpose experimental program was realized and pull-out force versus pull-out fiber length
was obtained (for fibers embedded into concrete at different depth and under different angle). Model
predictions were validated by 15x15x60cm prisms 4 point bending tests. Fracture surfaces analysis
was realized for broken prisms with the goal to improve elaborated model assumptions. Optimal
SFRHSC structures were recognized.

800
600 - :
- ~
“:400 e TN T S T e e T Fa
£ % -2
g s .
i % ss——
2oof \ . Fl
i

o
¢
2
lx
e

100 150 20.0 25.0

@
=1
w
o

d, mm

FIGURE 1. Pull-out curves ( L=25 mm, & = 0°) for: F1 - straight (lower curve); F2 — hooked-
end (middle curve); F3 — corrugated (upper curve).

References

1. Armelin, H.S., Banthia, N., Predicting the flexural post cracking performance of steel fiber
reinforced concrete from the pullout of single fibers, 4C/ Mater J 94:18-31.
2. Robins, P., Austin, S. and Jones, P., Pull-out behavior of hooked steel fibers, Material Structures

35:434-442,
62




