APPLICATION OF TEXTILE WASTE FOR COMPOSITE MATERIALS PROCESSING
TEKSTILATKRITUMU IZMANTOŠANAS IESPĒJAS KOMPOZĪTMATERIĀLU VEIDOŠANAI 
Skaidrīte Reihmane, Jānis Kajaks

RTU Polimērmateriālu institūts

Summary: A series of composites were made with textile waste and low density polyethylene as matrix material. The mechanical, technological and water sorption properties were examined. The results suggest that presence of synthetic fibers waste increases mechanical properties and decreases melting index and water sorption of composites. Recyclability is the major attraction of composites with thermoplastic matrix and thermoplastic reinforcement therefore use of waste textile helps to solve the environmental and recycling problems.
The awareness of the relationship between the textile production and use and healthy and safe environment is growing. As a result, consumers purchase products they believe are environmentally friendly. During textile materials manufacturing processes a lot of waste forms. Much of the textile waste has been buried in landfills to biodegrade. Solid waste materials that require disposal are many and varied. Manufactured fibers are often cheaper than natural fibers, but synthetic materials are not as easily biodegraded. The investigation of recycling of textile waste is area of significant research and development. The experience of Polymer materials institute researchers shows that  waste wood and linen fibers could be used for reinforcement of primary and secondary low-density polyethylene (1-3(.
In this work natural (wool) and man-made (rayon, acrylic, polyamide 6, polyamide 6.6, polyester, polyurethane) fibers waste from Ogresjarns and Lauma Lingerie were used for reinforcement of virgin low density polyethylene grade 15813-020 (PE). Content of fibers 30 wt. - % and 50 wt. - %.  Composites were compounded in rolling mills at 150 0C and compression moulded at 150 0C.
Tensile tests of composites specimens (length of basis 10 mm, width of basis 5 mm) were carried out on dynamometer UTS -100 (deformation rate 20 mm/min, estimating of tensile modulus at region of deformation 0,1-0,2 mm). Fixation of melting index at      190 0C, water sorption experiment according to ASTM - D – 3201 - 94.
The obtained results indicate the influence of kind and content of fibers waste on melting index, main mechanical properties and water sorption of composites.
References

1. G. Bakradze, J. Kajaks, S. Reihmane, J. Lejnieks Correlation Between the Mechanical Properties and the Amount of Desorpted Water for Composites Based on Recycled Low - Density Polyethylene and Linen Yarn Production Waste. Mech. Comp. Mat. Vol. 43, No 5, p. 427- 432, (2007).

2. S. Reihmane, J. Kajaks Waste Wood Fibers for Low Density Polyethylene Composites. RTU Zinātniskie raksti. Materiālzinātne un lietišķā ķīmija, sērija1, sējums 15, Rīga, 2007, 58-62 lpp.
3. S. Reihmane, J. Kajaks The Application of Hybrid Fibers for Thermoplastic Polymers Reinforcement. Materials of 6th Global Wood and Natural Fibre Composites Symposium, April 05-06, 2006 in Kassel/Germany, p. P5-1 – P5-4.
Skaidrīte Reihmane

RTU Polimērmateriālu institūts
Āzenes14/24, Rīga, LV 1048

e-pasts:reihmane@ktf.rtu.lv
