Supporting Information

Synthesis of fluorescent C-C bonded

triazole-purine conjugates

Aleksejs Burcevs,a Armands Sebris,a Kaspars Traskovskis,b Han-Wei Chu,c

Huan-Tsung Chang,c, d, e, f Justina Jovaišaitė,g Saulius Juršėnas,g

Māris Turks,a Irina Novosjolovaa, *

a Institute of Technology of Organic Chemistry, Faculty of Materials Science and Applied Chemistry, Riga Technical University, P. Valdena Str. 3, LV-1048, Riga, Latvia

b Institute of Applied Chemistry, Faculty of Materials Science and Applied Chemistry, Riga Technical University, P. Valdena Str. 3, LV-1048, Riga, Latvia

c Department of Biomedical Sciences, Chang Gung University, Taoyuan, 33302, Taiwan

d Graduate Institute of Biomedical Sciences, Chang Gung University, Taoyuan 33302, Taiwan

e Center for Advanced Biomaterials and Technology Innovation, Chang Gung University, Taoyuan 33302, Taiwan

f Division of Breast Surgery, Department of General Surgery, Chang-Gung Memorial Hospital, Linkou, Taoyuan 33305, Taiwan

g Institute of Photonics and Nanotechnology, Faculty of Physics, Vilnius University, Saulėtekis av. 3, LT-10257 Vilnius, Lithuania

Table of Contents

Experimental	S3

1. General information	S3

2. Synthesis of alkynylpurines	S4

3. Synthesis of 2-chloro-6-triazolylpurines	S13

4. Synthesis of 2,6-bistriazolylpurines	S33

5. Synthesis of 2-piperidinyl-6-triazolylpurines	S48

6. Synthesis of C-N conjugated triazolylpurines	S68

7. TBS group cleavage	S75

8. Photophysical data	S82

9. In vitro cytotoxic experiments	S84

References	S86

# Experimental

# 1. General information

Analytical thin-layer chromatography (TLC) was performed on Merck 60 Å silica gel F254 plates. Column chromatography was performed on Merck 40–60 μm 60 Å silica gel or Licroprep C18 (25–40 μm) silica gel.

NMR spectra were recorded on Bruker Avance 500 spectrometers. 1H NMR spectra were recorded at 500 MHz with internal references from nondeuterated solvents (δ = 7.26 for CDCl3, δ = 2.50 for DMSO-d6). 13C NMR spectra were recorded at 125.7 MHz with internal references from nondeuterated solvents (δ = 77.16 for CDCl3, δ = 39.52 for DMSO-d6). Coupling constants are reported in Hz, chemical shifts of signals are given in ppm, and standard abbreviations were used for multiplicity assignments.

The IR spectra were recorded in hexachlorobutadiene (4000–2000 cm-1) with an FTIR PerkinElmer Spectrum 100 spectrometer.

HPLC analysis were performed using Agilent Technologies 1200 Series system equipped with XBridge C18 column, 4.6×150 mm, particle size 3.5 μm, with flow rate of 1 mL/min, using 0.1% TFA/H2O and MeCN for mobile phase. Wavelength of detection was 260 nm. Eluent A – 0.1% TFA aqueous solution with 5% v/v MeCN, eluent B1 – MeCN, eluent B2 – MeOH. Eluent E1 – gradient 30–95% B1 5 min, 95% B1 5 min, 95–30% B1 2 min. Eluent E2 – gradient 95% B1 12 min, 95–80% B1, 2 min. Eluent E3 – gradient 30–95% B1 5 min, 95% B1 10 min, 95–30% B1 2 min. Eluent E4 – gradient 50–95% B2 5 min, 95% B2 5 min, 95–50% B2 2 min.

HRMS analysis was performed on an Agilent 1290 Infinity series UPLC system, connected to Agilent 6230 TOF LC/MS mass spectrometer; column Extend C18 RRHD 2.1 × 50 mm, particle size 1.8 µm. Eluents: formic acid in CH3CN (0.1 %) and aq. 0.1 formic acid.

Optical measurements of solutions were carried out at a typical material concentration of 1 × 10–5 mol L–1. The UV–vis absorption spectra were recorded with a PerkinElmer Lambda 35 spectrometer. Films for optical measurements were prepared using a spin-coating technique with a Laurell WS-400B-6NPP/LITE spin-coater on glass slides, using CHCl3 solutions with a material concentration of 30 mg/mL. After the preparation, all films were dried in an oven at 100 °C for 2 h.

Emission spectra, ΦFL in solutions or thin films were measured using a QuantaMaster 40 steady-state spectrofluorometer (Photon Technology International, Inc.) equipped with a 6-inch integrating sphere by LabSphere, using the software package provided by the manufacturer.

# 2. Synthesis of alkynylpurines

## 2-{2-Chloro-6-[(trimethylsilyl)ethynyl]-9H-purin-9-yl}ethyl 3,3,3-triphenylpropanoate (3a)

General method A for preparation of alkynylpurines: To a solution of 2a [1] (2.0 g, 3.86 mmol, 1.0 eq.), Ph3P (203 mg, 0.77 mmol, 0.2 eq.), CuI (74 mg, 0.39 mmol, 
0.1 eq.) and PdCl2 (68 mg, 0.39 mmol, 0.1 eq.) in dry THF (45 mL) Et3N (5.38 mL, ρ = 0.73 g/cm3, 38.6 mmol, 10.0 eq.) was added and the reaction mixture was stirred at 25 oC for 5 minutes. Trimethylsilylacetylene (2.20 mL, ρ = 0.69 g/cm3, 15.44 mmol, 4.0 eq.) was added and the reaction mixture was stirred at 50 oC for 30 minutes. Then it was evaporated and dried in vacuum. Silica gel column chromatography (DCM/MeCN, gradient 0% → 3%) provided product 3a (yield: 1.50 g, 67%) as an orange amorphous solid. Rf = 0.52 (DCM/MeCN = 20:1). HPLC: tR = 7.98 min, eluent E1. IR (KBr) ν (cm-1): 3060, 2960, 1742, 1574, 1463, 1378, 1346,1251, 1209, 1147. 1H-NMR (500 MHz, CDCl3) δ (ppm): 7.80 (s, 1H, H-C(8)), 7.31–7.21 (m, 15H, 15×H-C(Ph)), 4.24–4.14 (m, 4H, 2×(-CH2-)), 3.74 (s, 2H, (-CH2-)), 0.39 (s, 9H, 3×(-CH3)). 13C-NMR (126 MHz, CDCl3) δ (ppm): 170.4, 154.2, 153.4, 146.3, 146.2, 142.8, 133.6, 129.1, 128.0, 126.6, 108.1, 97.5, 61.7, 55.9, 46.0, 42.9, -0.4. HRMS (ESI) m/z: [M+H]+Calcd for C33H32ClN4O2Si 579.1978; Found 579.1975 (0.52 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 3a:

13C-NMR (126 MHz, CDCl3) spectrum of compound 3a:

## 2-{2,6-Bis[(trimethylsilyl)ethynyl]-9H-purin-9-yl}ethyl 3,3,3-triphenylpropanoate (4a)

Prepared according to general method A: Compound 2a [1] (100 mg, 0.19 mmol, 1.0 eq.), Ph3P (20 mg, 0.08 mmol, 0.4 eq.), CuI (7 mg, 0.04 mmol, 0.2 eq.), PdCl2 (21 mg, 0.04 mmol, 0.2 eq.), Et3N (0.26 mL, ρ = 0.73 g/cm3, 1.93 mmol, 10.0 eq.) and trimethylsilylacetylene (0.27 mL, ρ = 0.69 g/cm3, 1.9 mmol, 10.0 eq.), DMF (3 mL), 100 oC, 30 min. Silica gel column chromatography (DCM/MeCN, gradient 0% → 4%) provided product 4a (yield: 84 mg, 68%) as a brown amorphous solid. Rf = 0.64 (DCM/MeCN = 20:1). HPLC: tR = 8.70 min, eluent E1. IR (KBr) ν (cm-1): 3059, 2960, 1743, 1568, 1463, 1377, 1354, 1251, 1207, 1141. 1H-NMR (500 MHz, CDCl3) δ (ppm): 7.82 (s, 1H, H-C(8)), 7.30–7.21 (m, 15H, 15×H-C(Ph)), 4.27–4.22 (m, 2H, (-CH2-)), 4.19–4.15 (m, 2H, (-CH2-)), 3.73 (s, 2H, (-CH2-)), 0.38 (s, 9H, 3×(-CH3)), 0.33 (s, 9H, 3×(-CH3)). 13C-NMR (126 MHz, CDCl3) 
δ (ppm): 170.4, 151.7, 146.6, 146.2, 146.0, 141.7, 133.6, 129.1, 128.0, 126.6, 106.5, 102.6, 98.0, 93.5, 61.9, 55.9, 46.0, 42.7, -0.2, -0.3. HRMS (ESI) m/z: [M+H]+Calcd for C38H41N4O2Si2 641.2763; Found 641.2750 (2.03 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 4a:

13C-NMR (126 MHz, CDCl3) spectrum of compound 4a:

## 2-Chloro-9-heptyl-6-[(trimethylsilyl)ethynyl]-9H-purine (3b)

Prepared according to general method A: Compound 2b [2] (3.31 g, 11.53 mmol, 1.0 eq.), Ph3P (0.61 g, 2.31 mmol, 0.2 eq.), CuI (0.22 g, 1.15 mmol, 0.1 eq.), PdCl2 (0.21 g, 1.15 mmol, 0.1 eq.), Et3N (8.00 mL, ρ = 0.73 g/cm3, 57.66 mmol, 5.0 eq.) and trimethylsilylacetylene (6.6 mL, ρ = 0.69 g/cm3, 46.13 mmol, 4.0 eq.), THF (75 mL), 50 oC, 1 h. Silica gel column chromatography (DCM/MeCN, gradient 0% → 5%) provided product 3b (yield: 3.22 g, 80%) as a brown oil. Rf = 0.85 (DCM/MeCN = 20:1). HPLC: tR = 8.25 min, eluent E1. IR (KBr) ν (cm-1): 3098, 2957, 1568, 1356, 1250, 1011, 980, 840, 759, 633. 1H-NMR (500 MHz, CDCl3) δ (ppm): 8.08 (s, 1H, H-C(8)), 4.23 (t, 2H, 3J = 7.5 Hz, (-CH2-)), 1.89 (quintet, 2H, 
3J = 7.5 Hz, (-CH2-)), 1.34–1.22 (m, 8H, 4×(-CH2-)), 0.81 (t, 3H, 3J = 7.5 Hz, (-CH3-)), 0.32 (s, 9H, 3×(-CH3)). 13C-NMR (126 MHz, CDCl3) δ (ppm): 154.1, 153.6, 141.6, 142.6, 133.7, 107.7, 97.6, 44.4, 31.7, 29.9, 28.7, 26.6, 22.6, 14.1, -0.4. HRMS (ESI) m/z: [M+H]+Calcd for C17H26ClN4Si 349.1610; Found 349.1606 (1.1 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 3b:

13C-NMR (126 MHz, CDCl3) spectrum of compound 3b:

## 9-Heptyl-2,6-bis[(trimethylsilyl)ethynyl]-9H-purine (4b)

Prepared according to general method A: Compound 2b [2] (500 mg, 1.74 mmol, 1.0 eq.), Ph3P (184 mg, 0.70 mmol, 0.4 eq.), CuI (66 mg, 0.35 mmol, 0.2 eq.), PdCl2 (62 mg, 0.35 mmol, 0.2 eq.), Et3N (2.43 mL, ρ = 0.73 g/cm3, 17.42 mmol, 10.0 eq.) and trimethylsilylacetylene (2.48 mL, ρ = 0.69 g/cm3, 17.42 mmol, 10.0 eq.), DMF (10 mL), 100 oC, 30 min. Silica gel column chromatography (DCM/MeCN, gradient 0% → 2%) provided product 4b (yield: 320 mg, 45%) as a brown amorphous solid. Rf = 0.76 (DCM/MeCN = 20:1). HPLC: tR = 9.21 min, eluent E1. IR (KBr) ν (cm-1): 3095, 2928, 1566, 1356, 1250, 1011, 978, 840, 759, 633. 1H-NMR (500 MHz, CDCl3) δ (ppm): 8.10 (s, 1H, H-C(8)), 4.23 (t, 2H, 3J = 7.4 Hz, (-CH2-)), 1.84 (quintet, 2H, 3J = 7.4 Hz, (-CH2-)), 1.30–1.15 (m, 8H, 4×(-CH2-)), 0.81 (t, 3H, 3J = 7.4 Hz, (-CH3-)), 0.26 (s, 9H, 3×(-CH3)), 0.24 (s, 9H, 3×(-CH3)). 13C-NMR (126 MHz, CDCl3) δ (ppm): 151.9, 146.3, 145.8, 141.4, 133.6, 106.0, 102.8, 98.1, 92.8, 44.1, 31.6, 29.9, 28.6, 26.5, 22.5, 14.0, -0.3, -0.4.  HRMS (ESI) m/z: [M+H]+Calcd for C22H35N4Si2 411.2395; Found 411.2376 (4.6 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 4b:

13C-NMR (126 MHz, CDCl3) spectrum of compound 4b:

## 9-[2-(Tert-butyldimethylsilaniloxy)-1-(tert-butyldimethylsilaniloxymethyl)ethyl]-2-chloro-6-[(trimethylsilyl)ethynyl]-9H-purine (3c)

Prepared according to general method A: Compound 2c [3] (2.00 g, 4.07 mmol, 1.0 eq.), Ph3P (213 mg, 0.81 mmol, 0.2 eq.), CuI (78 mg, 0.41 mmol, 0.1 eq.), PdCl2 (72 mg, 0.41 mmol, 0.1 eq.), Et3N (2.83 mL, ρ = 0.73 g/cm3, 20.34 mmol, 5.0 eq.) and trimethylsilylacetylene (2.30 mL, ρ = 0.69 g/cm3, 16.27 mmol, 4.0 eq.), THF (60 mL), 50 oC, 1 h. Silica gel column chromatography (Hex/EtOAc, gradient 0% → 15%) provided product 3c (yield: 1.87 g, 83%) as a beige amorphous solid. Rf = 0.75 (Hex/EtOAc = 5:1). HPLC: tR = 8.11 min, eluent E2. IR (KBr) ν (cm-1): 2954, 2932, 1574, 1362, 1250, 1126, 1100, 994, 921, 833, 776. 1H-NMR (500 MHz, CDCl3) δ (ppm): 8.34 (s, 1H, H-C(8)), 4.80 (quintet, 1H, 3J = 5.3 Hz, (-CH-)), 4.06 (dd, 2H, 
2J = 10.3 Hz, 3J = 5.3 Hz, 2×(Ha-C)), 3.98 (dd, 2H, 2J = 10.3 Hz, 3J = 5.3 Hz, 2×(Hb-C)), 0.84 (s, 18H, 2×C(CH3)3), 0.33 (s, 9H, Si-(CH3)3), 0.01 (s, 6H, Si-(CH3)2), 0.00 (s, 6H, Si-(CH3)2). 
13C-NMR (126 MHz, CDCl3) δ (ppm): 153.9, 153.8, 146.3, 142.4, 133.3, 107.4, 97.8, 61.2 (2C), 58.1, 25.8, 18.2, -0.3, -5.4, -5.5. HRMS (ESI) m/z: [M+H]+Calcd for C25H46ClN4O2Si3 553.2612; Found 553.2623 (2.0 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 3c:

13C-NMR (126 MHz, CDCl3) spectrum of compound 3c:

## 9-[2-(Tert-butyldimethylsilaniloxy)-1-(tert-butyldimethylsilaniloxymethyl)ethyl]-2,6-bis[(trimethylsilyl)ethynyl]-9H-purine (4c)

Prepared according to general method A: Compound 2c [3] (3.00 g, 6.10 mmol, 1.0 eq.), Ph3P (640 mg, 2.44 mmol, 0.4 eq.), CuI (232 mg, 1.22 mmol, 0.2 eq.), PdCl2 (216 mg, 1.22 mmol, 0.2 eq.), Et3N (8.5 mL, ρ = 0.73 g/cm3, 61.03 mmol, 10.0 eq.) and trimethylsilylacetylene (8.7 mL, ρ = 0.69 g/cm3, 61.03 mmol, 10.0 eq.), DMF (70 mL), 100 oC, 40 min. Silica gel column chromatography (Hex/EtOAc, gradient 0% → 15%) provided product 4c (yield: 1.39 g, 37%) as a brown amorphous solid. Rf = 0.64 (Hex/EtOAc = 5:1). HPLC: tR = 11.98 min, eluent E2. IR (KBr) ν (cm-1): 2958, 2936, 1568, 1355, 1250, 1135, 1104, 990, 920, 840, 774. 1H-NMR (500 MHz, CDCl3) δ (ppm): 8.36 (s, 1H, H-C(8)), 4.89 (quintet, 1H, 3J = 5.3 Hz, (-CH-)), 4.03 (dd, 2H, 2J = 10.3 Hz, 3J = 5.3 Hz, 2×(Ha-C)), 3.96 (dd, 2H, 2J = 10.3 Hz, 3J = 5.3 Hz, 2×(Hb-C)), 0.84 (s, 18H, 2×C(CH3)3), 0.33 (s, 9H, Si-(CH3)3), 0.28 (s, 9H, Si-(CH3)3), 0.00 (s, 12H, 2×Si-(CH3)2). 13C-NMR (126 MHz, CDCl3) δ (ppm): 152.2, 146.4, 145.7, 141.3, 133.3, 105.8, 102.9, 98.3, 92.8, 61.1 (2C),1 57.4, 25.9, 18.2, -0.2, -0.3, -5.45, -5.54. HRMS (ESI) m/z: [M+H]+Calcd for C30H55N4O2Si4 615.3397; Found 615.3397 (0 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 4c:

13C-NMR (126 MHz, CDCl3) spectrum of compound 4c:

# 3. Synthesis of 2-chloro-6-triazolylpurines

## 2-[2-Chloro-6-(1-phenyl-1H-1,2,3-triazol-4-yl)-9H-purin-9-yl]ethyl 3,3,3-triphenylpropanoate (5a)

General method B for preparation of triazolylpurines: To a solution of 3a (350 mg, 0.60 mmol, 1.0 eq.), CuI (18 mg, 0.10 mmol, 0.16 eq.), AcOH (38 µL, ρ = 1.05 g/cm3, 0.66 mmol, 1.1 eq.) and Et3N (92 µL, ρ = 0.73 g/cm3, 0.66 mmol, 1.1 eq.) in DCM (7 mL) azidobenzene [4] (4.30 mL, C = 0.21 M (in DCM), 0.90 mmol, 1.5 eq.) was added and the reaction mixture was stirred isolated from the daylight for 30 min at 25 °C. Then the reaction mixture was poured into water (20 mL) and extracted with DCM (3×10 mL). Combined organic phase was washed with aqueous NaHS (10 mL) and sat. NaCl (10 mL), dried over anhydrous Na2SO4, filtered and evaporated. Silica gel column chromatography (DCM/MeCN, gradient 0% → 8%) provided product 5a (yield: 248 mg, 66%) as a white amorphous solid. Rf = 0.42 (DCM/MeCN = 10:1). HPLC: tR = 7.40 min, eluent E1. IR (KBr) ν (cm-1): 1735, 1593, 1501, 1213, 1142, 939, 856, 765, 705, 690. 1H-NMR (500 MHz, CDCl3) δ (ppm): 9.17 (s, 1H, H-C(triazole)), 7.91 (d, 2H, 3J = 7.3 Hz, 2×H-C(Ph)), 7.85 (s, 1H, H-(C8)), 7.61 (t, 2H, 3J = 7.3 Hz, 2×H-C(Ph)), 7.53 (t, 1H, 3J = 7.3 Hz H-C(Ph)), 7.30–7.17 (m, 15H, 15×H-C(Ph)), 4.28–4.24 (m, 2H, (-CH2-)), 4.23–4.18 (m, 2H, (-CH2-)), 3.76 (s, 2H, (-CH2)). 13C-NMR (126 MHz, CDCl3) δ (ppm): 170.5, 154.7, 153.9, 149.0, 146.2, 146.0, 143.8, 136.7, 130.0, 129.4, 129.1, 128.9, 128.0, 126.5, 125.1, 121.0, 61.9, 55.9, 46.1, 42.9. HRMS (ESI) m/z: [M+H]+Calcd for C36H29ClN7O2 648.1885; Found 648.1899 (2.16 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 5a:

13C-NMR (126 MHz, CDCl3) spectrum of compound 5a:

## 2-{2-Chloro-6-[1-(4-cyanophenyl)-1H-1,2,3-triazol-4-yl]-9H-purin-9-yl}ethyl 3,3,3-triphenylpropanoate (5b)

Prepared according to general method B: Compound 3a (300 mg, 0.52 mmol, 1.0 eq.), CuI (16 mg, 0.08 mmol, 0.16 eq.), AcOH (36 µL, ρ = 1.05 g/cm3, 0.57 mmol, 1.1 eq.), Et3N (79 µL, ρ = 0.73 g/cm3, 0.57 mmol, 1.1 eq.) and 4-azidobenzonitrile [4] (2.68 mL, C = 0.29 M (in DCM), 0.78 mmol, 1.5 eq.), DMF (6 mL), 25 °C, 30 min. Silica gel column chromatography (DCM/MeCN, gradient 0% → 7%) provided product 5b (yield: 278 mg, 82%) as a beige amorphous solid. Rf = 0.52 (DCM/MeCN = 5:1). HPLC: tR = 7.01 min, eluent E1. IR (KBr) ν (cm-1): 2282, 1743, 1594, 1513, 1328, 1146, 1040, 848, 746, 705. 
1H-NMR (500 MHz, DMSO-d6) δ (ppm): 9.80 (s, 1H, H-C(triazole)), 8.59 (s, 1H, H-C(8)), 8.35 (d, 2H, 3J = 8.7 Hz, 2×H-C(Ar)), 8.14 (d, 2H, 3J = 8.7 Hz, 2×H-C(Ar)), 7.19–7.12 (m, 6H, 
6×H-C(Ph)), 7.11–7.05 (m, 9H, 9×H-C(Ar)), 4.35 (t, 2H, 3J = 4.8 Hz, (-CH2-)), 4.15 (t, 2H, 
3J = 4.8 Hz, (-CH2-)), 3.75 (s, 2H, (-CH2-)). 13C-NMR (126 MHz, DMSO-d6) δ (ppm): 170.0, 154.1, 152.7, 148.1, 147.5, 146.2, 143.1, 139.2, 134.3, 128.9, 128.7, 127.6, 126.3, 125.9, 121.3, 118.1, 111.6, 61.6, 55.2, 45.1, 42.6. HRMS (ESI) m/z: [M+H]+Calcd for C37H28ClN8O2 651.2018; Found 651.2033 (2.3 ppm).

1H-NMR (500 MHz, DMSO-d6) spectrum of compound 5b:

13C-NMR (126 MHz, DMSO-d6) spectrum of compound 5b:

## 2-(2-Chloro-6-{1-[4-(dimethylamino)phenyl]-1H-1,2,3-triazol-4-yl}-9H-purin-9-yl)ethyl 3,3,3-triphenylpropanoate (5c)

To a solution of 3a (567 mg, 0.98 mmol, 1.0 eq.), CuSO4·5H2O (13 mg, 0.08 mmol, 0.08 eq.) and sodium ascorbate (31 mg, 0.16 mmol, 0.16 eq.) in DMF (15 mL) 10 w-% AcOH solution (4.8 mL) and 4-azido-N,N-dimethylaniline [5] (9.8 mL, C = 0.15 M (in DCM), 1.47 mmol, 1.5 eq.) was added and the reaction mixture was stirred isolated from the daylight for 1 h at 70 °C. Then it was evaporated and dried in vacuum. Water (20 ml) was added and organic phase was extracted with DCM (2×15 mL). Combined organic phase was washed with aqueous NaHS (2×30 mL) and sat. NaCl (2×30 mL), dried over anhydrous Na2SO4, filtered and evaporated. Reverse phase silica gel column chromatography (MeOH/H2O, gradient 70% → 95%) provided product 5c (yield: 365 mg, 56%) as a yellow amorphous solid. Rf = 0.52 (Tol/EtOH = 6:1). HPLC: tR = 7.19 min, eluent E1. IR (KBr) ν (cm-1): 1725, 1606, 1529, 1331, 1216, 1147, 1039, 857, 700, 640. 1H-NMR (500 MHz, CDCl3) δ (ppm): 8.99 (s, 1H, H-C(triazole)), 7.81 (s, 1H, H-C(8)), 7.67 (d, 2H, 3J = 9.0 Hz, 2×H-C(Ph)), 7.23 (d, 2H, 3J = 9.0 Hz, 2×H-C(Ph)), 7.25–7.19 (m, 12H, 12×H-C(Ph)), 7.19–7.15 (m, 3H, 3×H-C(Ph)), 4.22 (t, 2H, 3J = 5.0 Hz, (-CH2-)), 4.16 (t, 2H, 3J = 5.0 Hz, (-CH2-)), 3.72 (s, 2H, (-CH2-)), 3.04 (s, 6H, 2×(-CH3)). 13C-NMR (126 MHz, CDCl3) δ (ppm): 170.5, 154.7, 153.8, 151.0, 149.5, 146.2, 145.9, 143.4, 129.2, 128.8, 128.0, 126.5, 126.3, 124.8, 122.3, 112.4, 61.9, 55.9, 46.1, 42.8, 40.6. HRMS (ESI) m/z: [M+H]+Calcd for C38H34ClN8O2 669.2488; Found 669.2470 (2.7 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 5c:

13C-NMR (126 MHz, CDCl3) spectrum of compound 5c:

## 2-{2-Chloro-6-[1-(4-methoxyphenyl)-1H-1,2,3-triazol-4-yl]-9H-purin-9-yl}ethyl 3,3,3-triphenylpropanoate (5d)

Prepared according to general method B: Compound 3a (350 mg, 0.60 mmol, 1.0 eq.), CuI (18 mg, 0.10 mmol, 0.16 eq.), AcOH (38 µL, ρ = 1.05 g/cm3, 0.66 mmol, 1.1 eq.), Et3N (93 µL, ρ = 0.73 g/cm3, 0.66 mmol, 1.1 eq.) and 
1-azido-4-methoxybenzene [4] (3.2 mL, C = 0.28 M (in DCM), 0.90 mmol, 1.5 eq.), DCM (3 mL), 25 °C, 30 min. Silica gel column chromatography (DCM/MeCN, gradient 0% → 18%) provided product 5d (yield: 354 mg, 89%) as a red amorphous solid. Rf = 0.41 (DCM/MeCN = 5:1). HPLC: tR = 7.27 min, eluent E1. IR (KBr) ν (cm-1): 1720, 1590, 1518, 1328, 1251, 1149, 1032, 830, 799, 702. 
1H-NMR (500 MHz, CDCl3) δ (ppm): 9.08 (s, 1H, H-C(triazole)), 7.84 (s, 1H, H-C(8)), 7.80 (d, 2H, 3J = 8.9 Hz, 2×H-C(Ar)), 7.30–7.22 (m, 15H, 15×H-C(Ph)), 7.09 (d, 2H, 3J = 8.9 Hz, 
2×H-C(Ar)), 4.26 (t, 2H, 3J = 4.8 Hz,  (-CH2-)), 4.20 (t, 2H, 3J = 4.8 Hz,  (-CH2-)), 3.92 (s, 3H, 
(-CH3)), 3.75 (s, 2H, (-CH2-)). 13C-NMR (126 MHz, CDCl3) δ (ppm): 170.5, 160.4, 154.7, 153.9, 149.2, 146.2, 146.0, 143.6, 130.1, 129.1, 128.9, 128.0, 126.5, 125.1, 122.6, 115.0, 61.9, 55.9, 55.8, 46.1, 42.8. HRMS (ESI) m/z: [M+H]+Calcd for C37H31ClN7O3 656.2171; Found 656.2174 (0.46 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 5d:

13C-NMR (126 MHz, CDCl3) spectrum of compound 5d:

## 2-Chloro-9-heptyl-6-(1-phenyl-1H-1,2,3-triazol-4-yl)-9H-purine (5e)

Prepared according to general method B: Compound 3b (890 mg, 2.55 mmol, 1.0 eq.), CuI (78 mg, 0.41 mmol, 0.16 eq.), AcOH (0.16 mL, ρ = 1.05 g/cm3, 2.81 mmol, 1.1 eq.), Et3N (0.39 mL, ρ = 0.73 g/cm3, 2.81 mmol, 1.1 eq.) and azidobenzene [4] (10.1 mL, C = 0.38 M (in DCM), 3.83 mmol, 1.5 eq.), DCM (18 mL), 25 °C, 1 h. Silica gel column chromatography (DCM/MeCN, gradient 0% → 10%) provided product 5e (yield: 864 mg, 86%) as a beige amorphous solid. Rf = 0.82 (DCM/MeCN = 5:1). HPLC: tR = 7.32 min, eluent E1. IR (KBr) ν (cm-1): 1592, 1506, 1332, 1246, 1157, 1091, 995, 944, 854, 757, 685. 1H-NMR (500 MHz, CDCl3) δ (ppm): 9.13 (s, 1H, H-C(triazole)), 8.15 (s, 1H, H-C(8)), 7.87 (d, 2H, 
3J = 8.1 Hz, 2×H-C(Ar)), 7.57 (t, 2H, 3J = 8.1 Hz, 2×H-C(Ar)), 7.49 (t, 1H, 3J = 8.1 Hz, H-C(Ar)), 4.29 (t, 2H, 3J = 7.5 Hz, (-CH2-)), 1.98–1.89 (m, 2H, (-CH2-)), 1.40–1.32 (m, 4H, 
2×(-CH2-)), 1.32–1.22 (m, 4H, 2×(-CH2-)), 0.87 (t, 3H, 3J = 7.5 Hz, (-CH3)). 13C-NMR (126 MHz, CDCl3) δ (ppm): 154.6, 154.2, 149.0, 145.8, 144.0, 136.8, 130.0, 129.4, 129.1, 125.0, 121.0, 44.4, 31.7, 30.0, 28.8, 26.0, 22.6, 14.1. HRMS (ESI) m/z: [M+H]+Calcd for C20H23ClN7 396.1698; Found 396.1684 (3.5 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 5e:

13C-NMR (126 MHz, CDCl3) spectrum of compound 5e:

## 2-Chloro-9-heptyl-6-[1-(4-methoxyphenyl)-1H-1,2,3-triazol-4-yl]-9H-purine (5f)

Prepared according to general method B: Compound 3b (835 mg, 2.39 mmol, 1.0 eq.), CuI (73 mg, 0.38 mmol, 0.16 eq.), AcOH (0.15 mL, ρ = 1.05 g/cm3, 2.64 mmol, 1.1 eq.), Et3N (0.37 mL, ρ = 0.73 g/cm3, 2.64 mmol, 1.1 eq.) and 1-azido-4-methoxybenzene [4] (12.8 mL, C = 0.28 M (in DCM), 3.59 mmol, 1.5 eq.), DCM (16 mL), 25 °C, 3 h. Silica gel column chromatography (DCM/MeCN, gradient 0% → 9%) provided product 5f (yield: 635 mg, 91%) as a pale brown amorphous solid. Rf = 0.86 (DCM/MeCN = 5:1). HPLC: tR = 7.22 min, eluent E1. IR (KBr) ν (cm-1): 1592, 1519, 1334, 1246, 1156, 1036, 942, 854, 824, 800, 641. 1H-NMR 
(500 MHz, CDCl3) δ (ppm): 9.02 (s, 1H, H-C(triazole)), 8.10 (s, 1H, H-C(8)), 7.73 (d, 2H, 
3J = 8.9 Hz, 2×H-C(Ar)), 7.03 (d, 2H, 3J = 8.9 Hz, 2×H-C(Ar)), 4.27 (t, 2H, 3J = 7.3 Hz, (-CH2-)), 3.87 (s, 3H, -(CH3)), 1.96–1.87 (m, 2H, (-CH2-)), 1.37–1.30 (m, 4H, 2×(-CH2-)), 1.30–1.20 (m, 4H, 2×(-CH2-)), 0.85 (t, 3H, 3J = 7.3 Hz, (-CH3)). 13C-NMR (126 MHz, CDCl3) δ (ppm): 160.3, 154.6, 154.1, 149.0, 145.8, 143.7, 130.1, 129.0, 125.0, 122.5, 114.9, 55.8, 44.3, 31.7, 29.9, 28.7, 26.7, 22.6, 14.1. HRMS (ESI) m/z: [M+H]+Calcd for C21H25ClN7O 426.1804; Found 426.1803 (0.23 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 5f:

13C-NMR (126 MHz, CDCl3) spectrum of compound 5f:

## 2-Chloro-9-heptyl-6-[1-(4-nitrophenyl)-1H-1,2,3-triazol-4-yl]-9H-purine (5g)

Prepared according to general method B: Compound 3b (900 mg, 2.58 mmol, 1.0 eq.), CuI (79 mg, 0.41 mmol, 0.16 eq.), AcOH (0.16 mL, ρ = 1.05 g/cm3, 2.84 mmol, 1.1 eq.), Et3N (0.39 mL, ρ = 0.73 g/cm3, 2.84 mmol, 1.1 eq.) and 1-azido-4-nitrobenzene [4] (634 mg, 3.87 mmol, 1.5 eq.), DCM (18 mL), 25 °C, 1 h. Silica gel column chromatography (DCM/MeCN, gradient 0% → 10%) provided product 5g (yield: 780 mg, 69%) as a brown amorphous solid. Rf = 0.75 (DCM/MeCN = 10:1). HPLC: tR = 7.05 min, eluent E1. IR (KBr) ν (cm-1): 1593, 1541, 1498, 1346, 1244, 1157, 1090, 994, 855, 847, 747. 1H-NMR (500 MHz, CDCl3) δ (ppm): 9.26 (s, 1H, H-C(triazole)), 8.46 (d, 2H, 3J = 9.0 Hz, 2×H-C(Ar)), 8.17 (s, 1H, H-C(8)), 8.14 (d, 2H, 3J = 9.0 Hz, 2×H-C(Ar)), 4.30 (t, 2H, 3J = 7.3 Hz, (-CH2-)), 2.00–1.91 (m, 2H, (-CH2-)), 1.40–1.32 (m, 4H, 2×(-CH2-)), 1.32–1.22 (m, 4H, 2×(-CH2-)), 0.87 (t, 3H, 3J = 7.3 Hz, (-CH3)). 13C-NMR (126 MHz, CDCl3) δ (ppm): 154.7, 154.3, 148.2, 147.7, 146.1, 144.8, 140.9, 129.2, 125.8, 124.8, 121.0, 44.4, 31.7, 30.0, 28.8, 26.7, 22.6, 14.1. HRMS (ESI) m/z: [M+H]+Calcd for C20H22ClN8O2 441.1549; Found 441.1548 (0.23 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 5g:

13C-NMR (126 MHz, CDCl3) spectrum of compound 5g:

## 9-[2-(Tert-butyldimethylsilaniloxy)-1-(tert-butyldimethylsilaniloxymethyl)ethyl]-2-chloro-6-[1-(4-methoxyphenyl)-1H-1,2,3-triazol-4-yl]-9H-purine (5h)

Prepared according to general method B: Compound 3c (1.87 g, 3.38 mmol, 1.0 eq.), CuI (103 mg, 0.54 mmol, 0.16 eq.), AcOH (0.21 mL, ρ = 1.05 g/cm3, 3.71 mmol, 1.1 eq.), Et3N (0.52 mL, ρ = 0.73 g/cm3, 3.71 mmol, 1.1 eq.) and 1-azido-4-methoxybenzene [4] (6.84 mL, C = 0.74 M (in DCM), 5.06 mmol, 1.5 eq.), DCM (37 mL), 25 °C, 2 h. Silica gel column chromatography (DCM/MeCN, gradient 0% → 15%) provided product 5h (yield: 1.89 g, 89%) as a brown amorphous solid. Rf = 0.78 (DCM/MeCN = 5:1). HPLC: tR = 5.46 min, eluent E2. IR (KBr) ν (cm-1): 1592, 1519, 1329, 1253, 1109, 1090, 1031, 939, 831, 776. 1H-NMR (500 MHz, CDCl3) δ (ppm): 9.06 (s, 1H, H-C(triazole)), 8.37 (s, 1H, H-C(8)), 7.77 (d, 2H, 3J = 8.5 Hz, 2×H-C(Ar)), 7.05 (d, 2H, 3J = 8.5 Hz, 2×H-C(Ar)), 4.87 (quintet, 1H, 3J = 5.3 Hz, (-CH-)), 4.10 (dd, 2H, 2J = 10.5 Hz, 3J = 5.3 Hz, 2×(Ha-C)), 4.02 (dd, 2H, 2J = 10.5 Hz, 3J = 5.3 Hz, 2×(Hb-C)), 3.89 (s, 3H, (-CH3)), 0.88 (s, 18H, 2×C(CH3)3), 0.02 (s, 6H, 2×Si-(CH3)), 0.01 (s, 6H, Si-(CH3)2). 13C-NMR (126 MHz, CDCl3) δ (ppm): 160.3, 154.41, 154.38, 148.9, 145.8, 143.8, 130.3, 128.7, 125.1, 122.7, 115.0, 61.2 (2C),1 58.0, 55.8, 25.9, 18.2, -5.4, -5.5. HRMS (ESI) m/z: [M+H]+Calcd for C29H45ClN7O3Si3 630.2805; Found 630.2794 (1.7 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 5h:

13C-NMR (126 MHz, CDCl3) spectrum of compound 5h:

## 2-{2-Chloro-6-[1-(cyanomethyl)-1H-1,2,3-triazol-4-yl]-9H-purin-9-yl}ethyl 3,3,3-triphenylpropanoate (5i)

Prepared according to general method B: Compound 3a (300 mg, 0.53 mmol, 1.0 eq.), CuI (15 mg, 0.08 mmol, 0.15 eq.), AcOH (35 µL, ρ = 1.05 g/cm3, 0.58 mmol, 1.1 eq.), Et3N (80 µL, ρ = 0.73 g/cm3, 0.58 mmol, 1.1 eq.), 
2-azidoacetonitrile [6] (65 mg, 0.80 mmol, 1.5 eq.), DCM (5 mL), 1 h, 20 °C. For workup of this compound saturated EDTA solution (3×10 mL) was used instead of NaHS. Silica gel column chromatography (DCM/MeCN, gradient 0% → 15%) provided product 5i (yield: 184 mg, 59%), as a colorless solid. Rf = 0.28 (DCM/MeCN = 5:1). HPLC: tR = 6.33 min, eluent E1. IR (KBr) ν (cm-1): 3106, 3000, 2251, 1733, 1595, 1325, 1210, 1043. 
1H-NMR (500 MHz, DMSO-d6) δ (ppm): 9.38 (s, 1H, H-C(triazole)), 8.56 (s, 1H, H-C(8)), 
7.19‒7.03 (m, 15H, 15×H-C(Ar)), 6.00 (s, 2H, (-CH2-)), 4.34 (t, 2H, 3J = 4.9 Hz, (-CH2-)), 4.15 (t, 2H, 3J = 4.9 Hz, (-CH2-)), 3.75 (s, 2H, (-CH2-)). 13C-NMR (126 MHz, DMSO-d6) δ (ppm): 169.9, 153.8, 152.8, 147.9, 147.4, 146.2, 141.6, 129.6, 128.7 (2C),2 127.6, 125.9, 114.9, 61.5, 55.1, 45.0, 42.6, 37.7. HRMS(ESI) m/z: [M+H]+Calcd for C32H26ClN8O2 589.1862; Found 589.1857 (0.85 ppm).

1H-NMR (500 MHz, DMSO-d6) spectrum of compound 5i:

13C-NMR (126 MHz, DMSO-d6) spectrum of compound 5i:

## 2-{2-Chloro-6-[1-(2-methoxy-2-oxoethyl)-1H-1,2,3-triazol-4-yl]-9H-purin-9-yl}ethyl 3,3,3-triphenylpropanoate (5j)

Prepared according to general method B: Compound 3a (600 mg, 1.06 mmol, 1.0 eq.), CuI (30 mg, 0.16 mmol, 0.15 eq.), AcOH (70 µL, ρ = 1.05 g/cm3, 1.17 mmol, 1.1 eq.), Et3N (162 µL, ρ = 0.73 g/cm3, 1.17 mmol, 1.1 eq.) and methyl 
2-azidoacetate [7] (184 mg, 1.60 mmol, 1.5 eq.), DCM (10 mL), 20 °C, 1h. Silica gel column chromatography (DCM/MeCN, gradient 0% → 20%) provided product 5j (yield: 486 mg, 74%) as a brown solid. Rf = 0.31 (DCM/MeCN = 5:1). HPLC: tR = 6.35 min, eluent E1. IR (KBr) ν (cm-1): 3054, 2937, 1753, 1732, 1594, 1325, 1206, 1137. 1H-NMR (500 MHz, CDCl3) δ (ppm): 8.86 (s, 1H, H-C(triazole)), 7.78 (s, 1H, H-C(8)), 7.26‒7.13 (m, 15H, 15×H-C(Ar)), 5.32 (s, 2H, (-CH2-)), 
4.23‒4.18 (m, 2H, (-CH2-)), 4.18‒4.13 (m, 2H, (-CH2-)), 3.83 (s, 3H, (-CH3)), 3.71 (s, 2H, 
(-CH2-)). 13C-NMR (126 MHz, CDCl3) δ (ppm): 170.5, 166.4, 154.7, 153.9, 149.1, 146.2, 146.0, 143.7, 129.1, 128.9, 128.7, 128.0, 126.5, 61.8, 55.9, 53.4, 51.0, 46.0, 42.8. HRMS (ESI) m/z: [M+H]+Calcd for C33H29ClN7O4 622.1964; Found 622.1971 (1.13 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 5j:

13C-NMR (126 MHz, CDCl3) spectrum of compound 5j:

## 2-[2-Chloro-6-(1-cyclohexyl-1H-1,2,3-triazol-4-yl)-9H-purin-9-yl]ethyl 3,3,3-triphenylpropanoate (5k)

Prepared according to general method A: Compound 3a (500 mg, 0.88 mmol, 1.0 eq.), CuI (25 mg, 0.13 mmol, 0.15 eq.), AcOH (58 µL, ρ = 1.05 g/cm3, 0.97 mmol, 1.1 eq.), Et3N (135 µL, ρ = 0.73 g/cm3, 0.97 mmol, 1.1 eq.), azidocyclohexane [8] (166 mg, 1.33 mmol, 1.5 eq.), DCM (10 mL), 4 h, 20 °C. Silica gel column chromatography (DCM/MeCN, gradient 0% → 15%) provided product 5k (yield: 429 mg, 77%) as a pale yellow solid. Rf = 0.20 (DCM/MeCN = 10/1). HPLC: tR = 7.47 min, eluent E1. IR (KBr) ν (cm-1): 2936, 2858, 1741, 1591, 1447, 1324, 1143, 880. 1H-NMR (500 MHz, CDCl3) δ (ppm): 8.68 (s, 1H, 
H-C(triazole)), 7.79 (s, 1H, H-C(8)), 7.26‒7.14 (m, 15H, 15×H-C(Ar)), 4.64 (tt, 1H, 3J = 11.8 Hz, 3J = 3.6 Hz, (-CH-)), 4.23‒4.17 (m, 2H, (-CH2-)), 4.17‒4.11 (m, 2H, (-CH2-)), 3.70 (s, 2H, (-CH2-)), 2.32 (d, 2H,3J = 11.8 Hz, 2×(Hax-CH-)), 1.97 (d, 2H, 2J = 13.8 Hz, 2×(Heq-CH-)), 1.88‒1.77 (m, 3H, 3×(Heq-CH-)), 1.51 (qt, 2H, 2J = 3J = 12.9 Hz,
 3J = 3.7 Hz, 2×(Hax-CH-)), 1.33 (qt, 1H, 2J = 3J = 12.9 Hz, 3J = 3.7 Hz, (Hax-CH-)). 13C-NMR (126 MHz, CDCl3) δ (ppm): 170.4, 154.6, 153.8, 149.6, 146.2, 145.8, 142.9, 129.1, 128.7, 128.0, 126.5, 124.7, 61.8, 60.5, 55.9, 46.0, 42.8, 33.7, 25.2 (2C).2 HRMS(ESI) m/z: [M+H]+Calcd for C36H35ClN7O2 632.2535; Found 632.2515 (3.16 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 5k:

13C-NMR (126 MHz, CDCl3) spectrum of compound 5k:

## 2-[2-Chloro-6-(1-decyl-1H-1,2,3-triazol-4-yl)-9H-purin-9-yl]ethyl 3,3,3-triphenylpropanoate (5l)

Prepared according to the general method B: Compound 3a (500 mg, 0.88 mmol, 1.0 eq.), CuI (25 mg, 0.13 mmol, 0.15 eq.), AcOH (58 µL, ρ = 1.05 g/cm3, 0.97 mmol, 1.1 eq.), Et3N (135 µL, ρ = 0.73 g/cm3, 0.97 mmol, 1.1 eq.), 
1-azidodecane [8] (243 mg, 1.33 mmol, 1.5 eq.), DCM (10 mL), 1 h, 20 °C. Silica gel column chromatography (DCM/MeCN, gradient 0% → 10%) provided product 5l (yield: 532 mg, 88%) as a pale yellow solid. Rf= 0.26 (DCM/MeCN = 10/1). m. p. = 58‒64°C. HPLC: tR = 9.41 min, eluent E1. IR (KBr) ν (cm-1): 2926, 2855, 1741, 1594, 1446, 1325, 1144, 1041. 1H-NMR (500 MHz, CDCl3) δ (ppm): 8.67 (s, 1H, H-C(triazole)), 7.78 (s, 1H, H-C(8)), 7.26‒7.12 (m, 15H, 15×H-C(Ar)), 4.50 (t, 2H, 3J = 7.1 Hz, (-CH2-)), 4.24‒4.18 (m, 2H, (-CH2-)), 4.18‒4.12 (m, 2H, (-CH2-)), 3.71 (s, 2H, (-CH2-)), 2.00 (quintet, 2H, 3J = 7.1 Hz, 
(-CH2-)), 1.41‒1.32 (m, 4H, 2×(-CH2-)), 1.32‒1.20 (m, 10H, 5×(-CH2-)), 0.87 (t, 3H, 3J = 6.6 Hz, (-CH3)). 13C-NMR (126 MHz, CDCl3) δ (ppm): 170.4, 154.6, 153.8, 149.5, 146.2, 145.8, 143.2, 129.1, 128.7, 128.0, 126.9, 126.5, 61.8, 55.9, 50.8, 46.0, 42.8, 31.9, 30.4, 29.5, 29.4, 29.3, 29.1, 26.5, 22.7, 14.2. HRMS(ESI) m/z: [M+H]+Calcd for C40H45ClN7O2 690.3318; Found 690.3316 (0.29 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 5l:

13C-NMR (126 MHz, CDCl3) spectrum of compound 5l:

## 2-[6-(1-Benzyl-1H-1,2,3-triazol-4-yl)-2-chloro-9H-purin-9-yl]ethyl 3,3,3-triphenylpropanoate (5m)

Prepared according to general method B: Compound 3a (1.0 g, 1.73 mmol, 1.0 eq.), CuI (53 mg, 0.28 mmol, 0.16 eq.), AcOH (0.11 mL, ρ = 1.05 g/cm3, 1.90 mmol, 1.1 eq.), Et3N (0.26 mL, ρ = 0.73 g/cm3, 1.90 mmol, 1.1 eq.) and (azidomethyl)benzene [8] (3.65 mL, C = 0.71 M (in DCM), 2.60 mmol, 1.5 eq.), DCM (20 mL), 25 °C, 2 h. Silica gel column chromatography (DCM/MeCN, gradient 0% → 30%) provided product 5m (yield: 984 mg, 83%) as a gray amorphous solid. Rf = 0.52 (DCM/MeOH = 20:1). HPLC: tR = 7.17 min, eluent E1. IR (KBr) ν (cm-1): 1736, 1593, 1496, 1325, 1236, 1145, 1042, 938, 857, 701. 1H-NMR (500 MHz, CDCl3) δ (ppm): 8.57 (s, 1H, H-C(triazole)), 7.76 (s, 1H, H-C(8)),  
7.44–7.37 (m, 3H, 3×H-C(Ph)), 7.37–7.32 (m, 2H, 2×H-C(Ph)), 7.25–7.14 (m, 15H, 15×H-C(Ph)), 5.68 (s, 2H, (-CH2-)), 4.21–4.16 (m, 2H, (-CH2-)), 4.16–4.12 (m, 2H, (-CH2-)), 3.69 (s, 2H, 
(-CH2-)). 13C-NMR (126 MHz, CDCl3) δ (ppm): 170.5, 154.6, 153.9, 149.4, 146.2, 146.0, 143.9, 134.3, 129.4, 129.1 (2C),1 128.8, 128.3, 128.0, 126.9, 126.5, 61.8, 55.9, 54.6, 46.0, 42.8. HRMS (ESI) m/z: [M+H]+Calcd for C37H31ClN7O2 640.2222; Found 640.2228 (0.94 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 5m:

13C-NMR (126 MHz, CDCl3) spectrum of compound 5m:

# 4. Synthesis of 2,6-bistriazolylpurines

## 2-[2,6-Bis(1-phenyl-1H-1,2,3-triazol-4-yl)-9H-purin-9-yl]ethyl 3,3,3-triphenylpropanoate (6a)

Prepared according to general method B: Compound 4a (235 mg, 0.37 mmol, 1.0 eq.), CuI (23 mg, 0.12 mmol, 0.32 eq.), AcOH (23 µL, ρ = 1.05 g/cm3, 0.40 mmol, 1.1 eq.), Et3N (46 µL, ρ = 0.73 g/cm3, 0.40 mmol, 1.1 eq.) and azidobenzene [4] (2.9 mL, C = 0.38 M (in DCM), 1.10 mmol, 3.0 eq.), DMF (20 mL), 50 °C, 30 min. Silica gel column chromatography (EtOAc/EtOH, gradient 0% → 10%) provided product 6a (yield: 161 mg, 60%) as a brown amorphous solid. Rf = 0.62 (EtOAc/EtOH = 20:1). HPLC: tR = 7.03 min, eluent E1. IR (KBr) ν (cm-1): 1742, 1593, 1566, 1503, 1334, 1210, 1142, 1033, 758, 701. 1H-NMR (500 MHz, CDCl3) δ (ppm): 9.30 (s, 1H, H-C(triazole)), 8.97 (s, 1H, H-C(triazole)), 7.84 (d, 2H, 3J = 7.9 Hz, 2×H-C(Ph)), 7.81 (d, 2H, 3J = 7.9 Hz, 2×H-C(Ph)), 7.84 (s, 1H, H-C(8)), 7.55–7.45 (m, 4H, 4×H-C(Ph)), 7.45–7.36 (m, 2H, 2×H-C(Ph)), 7.23–7.20 (m, 12H, 12×H-C(Ph)), 7.20–7.14 (m, 3H, 3×H-C(Ph)), 4.37–4.29 (m, 2H, (-CH2-)), 4.20–4.15 (m, 2H, (-CH2-)), 3.74 (s, 2H, 
(-CH2-)). 13C-NMR (126 MHz, CDCl3) δ (ppm): 170.5, 153.6, 152.9, 148.3, 147.6, 146.3, 145.8, 144.3, 137.1, 137.0, 130.01, 129.96, 129.4, 129.2, 129.1, 129.0, 128.0, 126.5, 125.3, 123.7, 121.0, 120.9, 62.3, 56.0, 46.2, 42.7. HRMS (ESI) m/z: [M+H]+Calcd for C44H35N10O2 735.2939; Found 735.2921 (2.45 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 6a:

13C-NMR (126 MHz, CDCl3) spectrum of compound 6a:

## 2-{2,6-Bis[1-(4-cyanophenyl)-1H-1,2,3-triazol-4-yl]-9H-purin-9-yl}ethyl 3,3,3-triphenylpropanoate (6b)

Prepared according to general method B: Compound 4a (200 mg, 0.31 mmol, 1.0 eq.), CuI (19 mg, 0.10 mmol, 0.32 eq.), AcOH (20 µL, ρ = 1.05 g/cm3, 0.34 mmol, 1.1 eq.), Et3N (48 µL, ρ = 0.73 g/cm3, 0.34 mmol, 1.1 eq.) and 
4-azidobenzonitrile [4] (3.23 mL, C = 0.29 M (in DCM), 0.94 mmol, 3.0 eq.), DMF (4 mL), 50 °C, 30 min. Silica gel column chromatography (EtOAc/EtOH, gradient 0% → 5%) provided product 6b (yield: 122 mg, 50%) as a brown amorphous solid. Rf = 0.51 (EtOAc/EtOH = 20:1). HPLC: tR = 6.75 min, eluent E1. IR (KBr) ν (cm-1): 1736, 1601, 1518, 1340, 1204, 1036, 841, 760, 702, 553. 1H-NMR (500 MHz, CDCl3) δ (ppm): 9.43 (s, 1H, H-C(triazole)), 9.04 (s, 1H, 
H-C(triazole)), 8.13 (d, 2H, 3J = 8.6 Hz, 2×H-C(Ar)), 8.07 (d, 2H, 3J = 8.6 Hz, 2×H-C(Ar)), 7.92 (d, 2H, 3J = 8.6 Hz, 2×H-C(Ar)), 7.90 (d, 2H, 3J = 8.6 Hz, 2×H-C(Ar)), 7.86 (s, 1H, H-C(8)), 7.22–7.15 (m, 15H, 15×H-C(Ph)), 4.40 (t, 2H, 3J = 4.6 Hz, (-CH2-)), 4.26 (t, 2H, 3J = 4.6 Hz, 
(-CH2-)), 3.74 (s, 2H, (-CH2-)). 13C-NMR (126 MHz, CDCl3) δ (ppm): 170.5, 153.2, 152.9, 148.7, 146.9, 146.24, 146.19, 144.6, 139.7, 139.6, 134.2, 134.1, 129.1 (2C),3 128.0, 126.5, 125.0, 123.4, 121.0, 120.8, 117.8, 117.7, 113.1, 112.8, 62.2, 55.9, 46.1, 42.9. HRMS (ESI) m/z: [M+H]+Calcd for C46H33N12O2 785.2844; Found 785.2839 (0.64 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 6b:

13C-NMR (126 MHz, CDCl3) spectrum of compound 6b:

## 2-{2,6-Bis[1-(4-methoxyphenyl)-1H-1,2,3-triazol-4-yl]-9H-purin-9-yl}ethyl 3,3,3-triphenylpropanoate (6c)

Prepared according to general method B: Compound 4a (300 mg, 0.47 mmol, 1.0 eq.), CuI (29 mg, 0.15 mmol, 0.32 eq.), AcOH (30 µL, ρ = 1.05 g/cm3, 0.52 mmol, 1.1 eq.), Et3N (72 µL, ρ = 0.73 g/cm3, 0.52 mmol, 1.1 eq.) and 1-azido-4-methoxybenzene [4] (5.04 mL, C = 0.28 M (in DCM), 1.41 mmol, 3.0 eq.), DMF (6 mL), 50 °C, 30 min. Silica gel column chromatography (EtOAc/EtOH, gradient 0% → 6%) provided product 6c (yield: 224 mg, 60%) as a brown amorphous solid. Rf = 0.43 (EtOAc/EtOH = 20:1). HPLC: tR = 6.90 min, eluent E1. IR (KBr) ν (cm-1): 2959, 1736, 1592, 1517, 1257, 1030, 829, 801, 730, 701. 1H-NMR (500 MHz, CDCl3) δ (ppm): 9.21 (s, 1H, 
H-C(triazole)), 8.86 (s, 1H, H-C(triazole)), 7.87 (s, 1H, H-C(8)), 7.78 (d, 2H, 3J = 8.6 Hz, 
2×H-C(Ar)), 7.74 (d, 2H, 3J = 8.6 Hz, 2×H-C(Ar)), 7.23–7.17 (m, 12H, 12×H-C(Ph)), 7.17–7.12 (m, 3H, 3×H-C(Ph)), 7.04 (d, 2H, 3J = 7.2 Hz, 2×H-C(Ar)), 7.03 (d, 2H, 3J = 7.2 Hz, 
2×H-C(Ar)), 4.40–4.35 (m, 2H, (-CH2-)), 4.25–4.20 (m, 2H, (-CH2-)), 3.87–3.85 (m, 6H, 
2×(-CH3)), 3.73 (s, 2H, (-CH2-)). 13C-NMR (126 MHz, CDCl3) δ (ppm): 170.5, 160.2, 160.0, 153.6, 152.7, 148.0, 147.5, 146.2, 145.7, 144.0, 130.4, 130.2, 129.1, 128.6, 128.0, 126.5, 125.2, 123.8, 122.5, 122.3, 114.92, 114.88, 62.3, 55.9, 55.8, 55.7, 46.1, 42.7. HRMS (ESI) m/z: [M+H]+Calcd for C46H39N10O4 795.3150; Found 795.3124 (3.27 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 6c:

13C-NMR (126 MHz, CDCl3) spectrum of compound 6c:

## 9-Heptyl-2,6-bis[1-(4-methoxyphenyl)-1H-1,2,3-triazol-4-yl]-9H-purine (6d)

Prepared according to general method B: Compound 4b (300 mg, 0.718 mmol, 1.0 eq.), CuI (44 mg, 0.23 mmol, 0.32 eq.), AcOH (45 µL, ρ = 0.79 g/cm3, 0.79 mmol, 1.1 eq.), Et3N (110 µL, ρ = 0.73 g/cm3, 0.79 mmol, 1.1 eq.) and 1-azido-4-methoxybenzene [4] (7.69 mL, C = 0.28 M (in DCM), 2.154 mmol, 3.0 eq.), DMF (6 mL), 50 °C, 30 min. Silica gel column chromatography (EtOAc/EtOH, gradient 0% → 4%) provided product 6d (yield: 178 mg, 44%) as a white amorphous solid. Rf = 0.48 (EtOAc/EtOH = 20:1). HPLC: tR = 7.07 min, eluent E1. IR (KBr) ν (cm-1): 1594, 1518, 1372, 1305, 1254, 1170, 1033, 829, 803, 638. 1H-NMR (500 MHz, CDCl3) δ (ppm): 9.22 (s, 1H, H-C(triazole)), 8.89 (s, 1H, H-C(triazole)), 8.18 (s, 1H, H-C(8)), 7.80 (d, 2H, 3J = 8.4 Hz, 2×H-C(Ar)), 7.77 (d, 2H, 3J = 8.4 Hz, 2×H-C(Ar)), 7.06 (d, 4H, 3J = 8.4 Hz, 4×H-C(Ar)), 4.44 (t, 2H, 3J = 7.2 Hz, (-CH2-)), 3.89 (s, 6H, 2×(-CH3)), 2.02 (quintet, 2H, 3J = 7.2 Hz, (-CH2-)), 1.45–1.33 (m, 4H, 2×(-CH2-)), 1.32–1.22 (m, 4H, 2×(-CH2-)), 0.87 (t, 3H, 3J = 7.2 Hz, (-CH3)). 13C-NMR (126 MHz, CDCl3) δ (ppm): 160.3, 160.1, 153.7, 153.1, 148.3, 147.6, 145.3, 144.2, 130.6, 130.4, 128.8, 125.3, 123.9, 122.7, 122.5, 114.99, 114.97, 55.83, 55.81, 44.2, 31.8, 30.2, 28.9, 26.8, 22.7, 14.2. HRMS (ESI) m/z: [M+H]+Calcd for C30H33N10O2 565.2782; Found 565.2777 (0.9 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 6d:

13C-NMR (126 MHz, CDCl3) spectrum of compound 6d:

## 9-[2-(Tert-butyldimethylsilaniloxy)-1-(tert-butyldimethylsilaniloxymethyl)ethyl]-2,6-bis[1-(4-methoxyphenyl)-1H-1,2,3-triazol-4-yl]-9H-purine (6e)

Prepared according to general method B: Compound 4c (1.53 mg, 2.49 mmol, 1.0 eq.), CuI (152 mg, 0.80 mmol, 0.32 eq.), AcOH (0.16 mL, ρ = 0.79 g/cm3, 2.74 mmol, 1.1 eq.), Et3N (0.38 mL, ρ = 0.73 g/cm3, 2.74 mmol, 1.1 eq.) and 1-azido-4-methoxybenzene [4] (13.3 mL, C = 0.56 M (in DCM), 7.47 mmol, 3.0 eq.), DMF (31 mL), 25 °C, 40 min. Reverse phase silica gel column chromatography (MeOH/H2O, gradient 70% → 99%) provided product 6e (yield: 730 mg, 38%) as a beige amorphous solid. Rf = 0.52 (DCM/MeOH = 20:1). HPLC: tR = 4.33 min, eluent E2. IR (KBr) ν (cm-1): 1593, 1519, 1399, 1255, 1105, 1254, 1035, 888, 831, 773. 1H-NMR (500 MHz, CDCl3) δ (ppm): 9.23 (s, 1H, H-C(triazole)), 8.90 (s, 1H, H-C(triazole)), 8.39 (s, 1H, H-C(8)), 7.81 (d, 2H, 3J = 8.7 Hz, 2×H-C(Ar)), 7.78 (d, 2H, 3J = 8.7 Hz, 2×H-C(Ar)), 7.07 (d, 4H, 3J = 8.7 Hz, 4×H-C(Ar)), 5.19 (quintet, 1H, 3J = 5.3 Hz, (-CH-)), 4.15 (dd, 2H, 2J  = 10.3 Hz, 
3J = 5.3 Hz, 2×Ha-C), 4.08 (dd, 2H, 2J = 10.3 Hz, 3J = 5.3 Hz, 2×Hb-C), 3.89 (s, 6H, 2×(CH3)), 0.86 (s, 18H, 2×C(CH3)3), 0.03 (s, 6H, Si-(CH3)2), 0.025 (s, 6H, Si-(CH3)2). 13C-NMR (126 MHz, CDCl3) δ (ppm): 160.3, 160.1, 153.4, 153.3, 148.4, 147.3, 145.5, 144.3, 130.6, 130.4, 128.7, 125.3, 123.8, 122.7, 122.5, 115.0 (2C),1 61.2 (2C),1 57.1, 55.82, 55.81, 25.9, 18.3, -5.4, 
-5.5. HRMS (ESI) m/z: [M+H]+Calcd for C38H53N10O4Si2 769.3784; Found 769.3784 (0 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 6e:

13C-NMR (126 MHz, CDCl3) spectrum of compound 6e:

## 2-{2,6-Bis[1-(cyanomethyl)-1H-1,2,3-triazol-4-yl]-9H-purin-9-yl}ethyl 3,3,3-triphenylpropanoate (6f)

Prepared according to general method B: Compound 4a (300 mg, 0.47 mmol, 1.0 eq.), CuI (27 mg, 0.14 mmol, 0.30 eq.), AcOH (62 µL, ρ = 1.05 g/cm3, 1.03 mmol, 2.2 eq.), Et3N (142 µL, ρ = 0.73 g/cm3, 1.03 mmol, 2.2 eq.), 
2-azidoacetonitrile [6] (115 mg, 1.40 mmol, 3.0 eq.), DMF (5 mL), 1 h, 50 °C. For workup of this compound saturated EDTA solution (3×10 mL) was used instead of NaHS. Silica gel column chromatography (DCM/EtOH, gradient 0% → 4%) provided product 6f (yield: 193 mg, 62%) as a pale brown solid. Rf = 0.20 (DCM/EtOH = 20/1). HPLC: tR = 5.60 min, eluent E1. IR (KBr) ν (cm-1): 3158, 2991, 2261, 1718, 1599, 1443, 1247, 1152, 1044. 1H-NMR (500 MHz, DMSO-d6) δ (ppm): 9.41 (s, 1H, 
H-C(triazole)), 9.00 (s, 1H, H-C(triazole)), 8.54 (s, 1H, H-C(8)), 7.18‒6.98 (m, 15H, 
15×H-C(Ar)), 6.03 (s, 2H, (-CH2-)), 5.93 (s, 2H, (-CH2-)), 4.50‒4.38 (m, 2H, (-CH2-)), 4.26‒4.16 (m, 2H, (-CH2-)), 3.74 (s, 2H, (-CH2-)). 13C-NMR (126 MHz, DMF-d7) δ (ppm): 171.3, 154.2, 153.8, 149.1, 148.5, 147.7 (2C),2 144.3, 130.4, 130.0 (2C),2 128.7, 128.3, 127.0, 116.0 (2C),2 63.0, 56.6, 46.5, 43.8, 38.8, 38.6. HRMS (ESI) m/z: [M+H]+Calcd for C36H29N12O2 661.2531; Found 661.2529 (0.30 ppm).

1H-NMR (500 MHz, DMSO-d6) spectrum of compound 6f:

13C-NMR (126 MHz, DMF-d7) spectrum of compound 6f:

## Dimethyl 2,2'-[(9-{2-[(3,3,3-triphenylpropanoyl)oxy]ethyl}-9H-purine-2,6-diyl)bis(1H-1,2,3-triazole-4,1-diyl)]diacetate (6g)

Prepared according to general method B: Compound 4a (320 mg, 0.50 mmol, 1.0 eq.), CuI (29 mg, 0.15 mmol, 0.30 eq.), AcOH (66 µL, ρ = 1.05 g/cm3, 1.10 mmol, 2.2 eq.), Et3N (152 µL, ρ = 0.73 g/cm3, 1.10 mmol, 2.2 eq.), methyl 2-azidoacetate [7] (156 μL, ρ = 1.18 g/cm3, 1.60 mmol, 3.0 eq.), DMF (5 mL), 1 h, 50 °C. Silica gel column chromatography (DCM/EtOH, gradient 0% → 5%) provided product 6g (yield: 243 mg, 67%) as a brown solid. Rf = 0.35 (DCM/EtOH = 20/1). HPLC: tR = 5.65 min, eluent E1. IR (KBr) ν (cm-1): 2957, 1753, 1727, 1595, 1330, 1228, 1047. 1H-NMR (500 MHz, CDCl3) δ (ppm): 8.94 (s, 1H, H-C(triazole)), 8.59 (s, 1H, H-C(triazole)), 7.80 (s, 1H, H-C(8)), 7.24‒7.11 (m, 15H, 15×H-C(Ar)), 5.33 (s, 2H, (-CH2-)), 5.26 (s, 2H, (-CH2-)), 4.31 
(t, 2H, 3J = 4.7 Hz, (-CH2-)), 4.19 (t, 2H, 3J = 4.7 Hz, (-CH2-)), 3.81 (s, 3H, (-CH3)), 3.79 (s, 3H, (-CH3)), 3.71 (s, 2H, (-CH2-)). 13C-NMR (126 MHz, CDCl3) δ (ppm): 170.5, 166.6, 166.5, 153.4, 152.8, 148.2, 147.5, 146.3, 145.8, 144.3, 129.1, 128.8, 128.6, 128.0, 127.2, 126.5, 62.3, 55.9, 53.3, 53.2, 51.0 (2C),2 46.1, 42.6. HRMS (ESI) m/z: [M+H]+Calcd for C38H35N10O6 727.2736; Found 727.2716 (2.75 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 6g:

13C-NMR (126 MHz, CDCl3) spectrum of compound 6g:

## 2-[2,6-Bis(1-cyclohexyl-1H-1,2,3-triazol-4-yl)-9H-purin-9-yl]ethyl 3,3,3-triphenylpropanoate (6h)

Prepared according to general method B: Compound 4a (250 mg, 0.39 mmol, 1.0 eq.), CuI (22 mg, 0.12 mmol, 0.30 eq.), AcOH (51 µL, ρ = 1.05 g/cm3, 0.86 mmol, 2.2 eq.), Et3N (118 µL, ρ = 0.73 g/cm3, 0.86 mmol, 2.2 eq.), azidocyclohexane [8] (146 mg, 1.17 mmol, 3.0 eq.), DMF (5 mL), 1 h, 50 °C. Silica gel column chromatography (DCM/EtOH, gradient 0% → 4%) provided product 6h (yield: 235 mg, 81%) as a brown solid. Rf = 0.42 (DCM/EtOH = 20/1). HPLC: tR = 7.55 min, eluent E1. IR (KBr) ν (cm-1): 2934, 2855, 1740, 1586, 1516, 1446, 1256, 1141. 1H-NMR (500 MHz, CDCl3) δ (ppm): 8.83 (s, 1H, H-C(triazole)), 8.51 (s, 1H, H-C(triazole)), 7.79 (s, 1H, H-C(8)), 7.26‒7.14 (m, 15H, 15×H-C(Ar)), 4.65 (tt, 1H, 3J = 11.8 Hz, 3J = 3.6 Hz, (-CH-)), 4.59 (tt, 1H, 3J = 11.8 Hz, 3J = 3.6 Hz, 
(-CH-)), 4.34 (t, 2H, 3J = 4.9 Hz, (-CH2-)), 4.20 (t, 2H, 3J = 4.9 Hz, (-CH2-)), 3.72 (s, 2H, 
(-CH2-)), 2.33, 2.28 (2d, 4H, 3J = 11.8 Hz, 4×(Hax-CH-)), 2.01‒1.93 (m, 4H, 4×(Heq-CH-)), 1.93‒1.75 (m, 6H, 6×(Heq-CH-)), 1.58‒1.43 (m, 4H, 4×(Hax-CH-)), 1.40‒1.26 (m, 2H, 
2×(Hax-CH-)). 13C-NMR (126 MHz, CDCl3) δ (ppm): 170.5, 154.1, 152.8, 148.1, 147.4, 146.3, 145.4, 143.3, 129.2, 128.6, 128.0, 126.5, 124.9, 123.4, 62.4, 60.6, 60.5, 56.0, 46.2, 42.5, 33.8 (2C),2 25.4, 25.3 (3C).2 HRMS (ESI) m/z: [M+H]+Calcd for C44H47N10O2 747.3878; Found 747.3878 (0 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 6h:

13C-NMR (126 MHz, CDCl3) spectrum of compound 6h:

## 2-[2,6-Bis(1-decyl-1H-1,2,3-triazol-4-yl)-9H-purin-9-yl]ethyl 3,3,3-triphenylpropanoate (6i)

Prepared according to general method B: Compound 4a (250 mg, 0.39 mmol, 1.0 eq.), CuI (22 mg, 0.12 mmol, 0.30 eq.), AcOH (51 µL, ρ = 1.05 g/cm3, 0.86 mmol, 2.2 eq.), Et3N (118 µL, ρ = 0.73 g/cm3, 0.86 mmol, 2.2 eq.), 
1-azidodecane [8] (214 mg,1.17 mmol, 3.0 eq.), DMF (5 mL), 1 h, 50 °C. Silica gel column chromatography (DCM/MeCN, gradient 0% → 40%) provided product 6i (yield: 152 mg, 45%) as a brown solid. Rf = 0.38 (DCM/EtOH = 20/1). HPLC: tR = 14.44 min, eluent E3. IR (KBr) ν (cm-1): 2925, 2854, 1741, 1595, 1447, 1328, 1207, 1143, 1043. 1H-NMR (500 MHz, CDCl3) δ (ppm): 8.83 (s, 1H, H-C(triazole)), 8.50 (s, 1H, H-C(triazole)), 7.79 (s, 1H, H-C(8)), 7.26‒7.12 (m, 15H, 15×H-C(Ar)), 4.52 (t, 2H, 3J = 7.2 Hz, (-CH2-)), 4.44 (t, 2H, 3J = 7.1 Hz, 
(-CH2-)), 4.35 (t, 2H, 3J = 4.9 Hz, (-CH2-)), 4.21 (t, 2H, 3J = 4.9 Hz, (-CH2-)), 3.72 (s, 2H, 
(-CH2-)), 2.01 (quintet, 2H, 3J = 7.1 Hz, (-CH2-)), 1.97 (quintet, 2H, 3J = 7.1 Hz, (-CH2-)), 1.42‒1.18 (m, 28H, 14×(-CH2-)), 0.86 (t, 6H, 3J = 6.7 Hz, 2×(-CH3)). 13C-NMR (126 MHz, CDCl3) 
δ (ppm): 170.5, 154.0, 152.8, 147.9, 147.7, 146.3, 145.4, 143.6, 129.2, 128.7, 128.0, 127.0, 126.5, 125.5, 62.4, 56.0, 50.8, 50.7, 46.1, 42.5, 32.0 (2C), 30.5 (2C), 29.6 (2C), 29.5 (2C), 29.4 (2C), 29.1 (2C), 26.6 (2C), 22.8 (2C), 14.2 (2C). HRMS (ESI) m/z: [M+H]+Calcd for C52H67N10O2 863.5443; Found 863.5440 (0.35 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 6i:

13C-NMR (126 MHz, CDCl3) spectrum of compound 6i:

## 2-[2,6-Bis(1-benzyl-1H-1,2,3-triazol-4-yl)-9H-purin-9-yl]ethyl 3,3,3-triphenylpropanoate (6j)

Prepared according to general method B: Compound 4a (20 mg, 0.03 mmol, 1.0 eq.), CuI (2 mg, 0.01 mmol, 0.32 eq.), AcOH (2 µL, ρ = 0.79 g/cm3, 0.03 mmol, 1.1 eq.), Et3N (5 µL, ρ = 0.73 g/cm3, 0.03 mmol, 1.1 eq.) and (azidomethyl)benzene [8] (0.21 mL, C = 0.45 M (in DCM), 0.09 mmol, 3.0 eq.), DMF (3 mL), 50 °C, 30 min. Silica gel column chromatography (EtOAc/EtOH, gradient 0% → 3%) provided product 6j (yield: 20 mg, 85%) as a brown amorphous solid. Rf = 0.55 (EtOAc/EtOH = 20:1). HPLC: tR = 6.75 min, eluent E1. IR (KBr) ν (cm-1): 1729, 1594, 1448, 1365, 1329, 1203, 1147, 1046, 718, 703. 1H-NMR (500 MHz, DMSO-d6) δ (ppm): 9.24 (s, 1H, H-C(triazole)), 8.87 (s, 1H, H-C(triazole)), 8.48 (s, 1H, H-C(8)), 7.48–7.29 (m, 10H, 10×H-C(Ph)), 7.11–7.05 (m, 6H, 6×H-C(Ph)), 7.05–6.98 (m, 9H, 9×H-C(Ph)), 5.84 (s, 2H, (-CH2-)), 5.73 (s, 2H, (-CH2-)), 4.41 (t, 2H, 3J = 4.9 Hz, (-CH2-)), 4.19 (t, 2H, 3J = 4.9 Hz, (-CH2-)), 3.71 (s, 2H, (-CH2-)). 13C-NMR (126 MHz, DMSO-d6) δ (ppm): 170.5, 153.7, 152.7, 148.1, 147.7, 146.2, 145.6, 144.2, 134.5, 134.4, 129.3 (2C),3 129.1, 128.98, 128.97, 128.7, 128.3, 128.1, 128.0, 127.1, 126.5, 125.6, 62.3, 55.9, 54.5 (2C),1 46.1, 42.5. HRMS (ESI) m/z: [M+H]+Calcd for C46H39N10O2 763.3252; Found 763.3282 (3.93 ppm).

1H-NMR (500 MHz, DMSO-d6) spectrum of compound 6j:

13C-NMR (126 MHz, DMSO-d6) spectrum of compound 6j:

# 5. Synthesis of 2-piperidinyl-6-triazolylpurines

## 2-[6-(1-Phenyl-1H-1,2,3-triazol-4-yl)-2-(piperidin-1-yl)-9H-purin-9-yl]ethyl 3,3,3-triphenylpropanoate (7a)

General method C for preparation of piperidinylpurines: To a solution of compound 5a (100 mg, 0.16 mmol, 1.0 eq.) in DMF (1 mL) piperidine (48 µL, ρ = 0.86 g/cm3, 0.48 mmol, 3.0 eq.) was added and the mixture was stirred for 1.5 h at 100 °C. Then it was evaporated and dried in vacuum. Silica gel column chromatography (DCM/MeOH, gradient 0% → 4%) provided product 7a (yield: 72 mg, 67%) as a white amorphous solid. Rf = 0.50 (DCM/MeOH = 20:1). tR = 7.47 min, eluent E1. IR (KBr) ν (cm-1): 2937, 2846, 1738, 1604, 1589, 1523, 1493, 1257, 1197, 1148, 1037. 1H-NMR (500 MHz, CDCl3) 
δ (ppm): 9.09 (s, 1H, H-C(triazole)), 7.89 (d, 2H, 3J = 7.7 Hz, 2×H-C(Ph)), 7.56 (t, 2H, 3J = 7.7 Hz, 2×H-C(Ph)), 7.51–7.43 (m, 2H, H-C(Ph), H-(C8)), 7.51–7.43 (m, 15H, 15×H-C(Ph)), 4.14 (t, 2H, 3J = 5.1 Hz, (-CH2-)), 4.06 (t, 2H, 3J = 5.1 Hz, (-CH2-)), 3.95–3.91 (m, 4H, 2×(-CH2-)), 3.71 (s, 2H, (-CH2-)), 1.69–1.65 (m, 6H, 3×(-CH2-)). 13C-NMR (126 MHz, CDCl3) δ (ppm): 170.7, 159.4, 154.2, 147.4, 146.3, 145.3, 141.8, 137.1, 129.9, 129.2, 129.1, 128.0, 126.5, 124.4, 123.1, 121.0, 62.1, 55.9, 46.2, 45.6, 41.9, 26.0, 25.1. HRMS (ESI) m/z: [M+H]+Calcd for C41H39N8O2 675.3190; Found 675.3198 (1.18 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 7a:

13C-NMR (126 MHz, CDCl3) spectrum of compound 7a:

## 2-{6-[1-(4-Cyanophenyl)-1H-1,2,3-triazol-4-yl]-2-[piperidin-1-yl]-9H-purin-9-yl}ethyl 3,3,3-triphenylpropanoate (7b)

Prepared according to general method C: Compound 5b (350 mg, 0.54 mmol, 1.0 eq.), piperidine (0.17 mL, ρ = 0.86 g/cm3, 1.62 mmol, 3.0 eq.), DMF (10 mL), 1 h, 100 °C. Silica gel column chromatography (DCM/MeOH, gradient 0% → 3%) provided compound 7b (yield: 284 mg, 76%) as a yellow amorphous solid. Rf = 0.68 (DCM/MeOH = 20:1). HPLC: tR = 7.18 min, eluent E1. IR (KBr) ν (cm-1): 1742, 1607, 1529, 1445, 1200, 1153, 1025, 913, 767, 700. 1H-NMR (500 MHz, CDCl3) δ (ppm): 9.18 (s, 1H, H-C(triazole)), 7.53 (s, 1H, H-C(8)), 8.06 (d, 2H, 3J = 8.7 Hz, 2×H-C(Ar)), 7.85 (d, 2H, 
3J = 8.7 Hz, 2×H-C(Ar)), 7.22–7.17 (m, 15H, 
15×H-C(Ph)), 4.14 (t, 2H, 3J = 5.0 Hz, (-CH2-)), 4.06 (t, 2H, 3J = 5.0 Hz, (-CH2-)), 3.94–3.89 (m, 4H, 2×(-CH2-)), 3.71 (s, 2H, (-CH2-)), 1.74–1.60 (m, 6H, 3×(-CH2-)). 13C-NMR (126 MHz, CDCl3) δ (ppm): 170.6, 159.4, 154.2, 146.7, 146.3, 145.9, 141.9, 139.8, 134.0, 129.2, 128.0, 126.5, 124.0, 122.8, 121.0, 117.9, 112.7, 62.0, 55.9, 46.2, 45.6, 42.0, 26.0, 25.0. HRMS (ESI) m/z: [M+H]+Calcd for C42H38N9O2 700.3143; Found 700.3145 (0.29 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 7b:

13C-NMR (126 MHz, CDCl3) spectrum of compound 7b:

## 2-{6-[1-(4-{Dimethylamino}phenyl)-1H-1,2,3-triazol-4-yl]-2-[piperidin-1-yl]-9H-purin-9-yl}ethyl 3,3,3-triphenylpropanoate (7c)

Prepared according to general method C: Compound 5c (250 mg, 0.37 mmol, 1.0 eq.), piperidine (0.11 mL, ρ = 0.86 g/cm3, 1.12 mmol, 3.0 eq.), DMF (5 mL), 1 h, 100 °C. Silica gel column chromatography (DCM/MeOH, gradient 0% → 4%) provided compound 7c (yield: 109 mg, 41%) as a yellow amorphous solid. Rf = 0.60 (DCM/MeOH = 20:1). HPLC: tR = 7.58 min, eluent E1. IR (KBr) ν (cm-1): 1737, 1608, 1523, 1446, 1210, 1141, 1038, 908, 816, 749, 701. 1H-NMR (500 MHz, CDCl3) δ (ppm): 9.00 (s, 1H, H-C(triazole)), 7.69 (d, 2H, 
3J = 9.1 Hz, 2×H-C(Ph)), 7.50 (s, 1H, H-C(8)),  7.25–7.15 (m, 15H, 15×H-C(Ph)), 6.78 (d, 2H, 3J = 9.1 Hz, 2×H-C(Ph)), 4.14 (t, 2H, 3J = 5.0 Hz, (-CH2-)), 4.06 (t, 2H, 3J = 5.0 Hz, (-CH2-)), 3.94–3.90 (m, 4H, 2×(-CH2-)), 3.71 (s, 2H, (-CH2-)), 3.04 (s, 6H, 2×(-CH3), 1.67–1.62 (m, 6H, 3×(-CH2-)). 
13C-NMR (126 MHz, CDCl3) δ (ppm): 170.7, 159.5, 154.1, 150.8, 147.8, 146.3, 144.7, 141.6, 129.2, 128.0, 126.9, 126.5, 124.4, 122.6, 122.3, 112.5, 62.1, 56.0, 46.2, 45.6, 42.0, 40.7, 26.0, 25.1. HRMS (ESI) m/z: [M+H]+Calcd for C43H44N9O2 718.3612; Found 718.3600 (1.67 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 7c:

13C-NMR (126 MHz, CDCl3) spectrum of compound 7c:

## 2-{6-[1-(4-Methoxyphenyl)-1H-1,2,3-triazol-4-yl]-2-[piperidin-1-yl]-9H-purin-9-yl}ethyl 3,3,3-triphenylpropanoate (7d)

Prepared according to general method C: Compound 5d (150 mg, 0.23 mmol, 1.0 eq.), piperidine (68 µL, ρ = 0.86 g/cm3, 0.69 mmol, 3.0 eq.), DMF (5 mL), 1 h, 100 °C. Silica gel column chromatography (Tol/iPrOH, gradient 0% → 15%) provided compound 7d (yield: 110 mg, 67%) as an orange amorphous solid. Rf = 0.32 (Tol/iPrOH = 10:1). HPLC: tR = 7.31 min, eluent E1. IR (KBr) ν (cm-1): 2933, 1740, 1588, 1517, 1446, 1255, 1142, 1030, 831, 795, 700. 1H-NMR (500 MHz, CDCl3) δ (ppm): 9.01 (s, 1H, H-C(triazole)), 7.76 (d, 2H, 
3J = 8.9 Hz, 2×H-C(Ar)), 7.49 (s, 1H, H-C(8)), 7.25–7.15 (m, 15H, 15×H-C(Ph)), 7.04 (d, 2H, 3J = 8.9 Hz, 2×H-C(Ar)), 4.14 (t, 2H, 3J = 4.9 Hz, 
2×(-CH2-)), 4.06 (t, 2H, 3J = 4.9 Hz, 2×(-CH2-)), 3.95–3.90 (m, 4H, 4×(-CH2-)), 3.88 (s, 3H, 
(-CH3)), 3.71 (s, 2H, (-CH2-)), 1.70–1.62 (m, 6H, 3×(-CH2-)). 13C-NMR (126 MHz, CDCl3) 
δ (ppm): 170.6, 160.0, 159.3, 154.0, 147.4, 146.2, 144.9, 141.6, 130.4, 129.1, 127.9, 126.4, 124.5, 122.7, 122.5, 114.8, 61.9, 55.8, 55.7, 46.1, 45.5, 41.8, 25.9, 24.9. HRMS (ESI) m/z: [M+H]+Calcd for C42H41N8O3 705.3296; Found 705.3300 (0.57 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 7d:

13C-NMR (126 MHz, CDCl3) spectrum of compound 7d:

## 9-Heptyl-6-(1-phenyl-1H-1,2,3-triazol-4-yl)-2-(piperidin-1-yl)-9H-purine (7e)

Prepared according to general method C: Compound 5e (200 mg, 0.51 mmol, 1.0 eq.), piperidine (0.15 mL, ρ = 0.86 g/cm3, 1.52 mmol, 3.0 eq.), DMF (10 mL), 2 h, 100 °C. Silica gel column chromatography (DCM/MeOH, gradient 0% → 1%) provided compound 7e (yield: 173 mg, 77%) as a white amorphous solid. Rf = 0.52 (DCM/MeOH = 20:1). HPLC: tR = 7.57 min, eluent E1. IR (KBr) ν (cm-1): 1607, 1524, 1486, 1408, 1304, 1201, 1029, 911, 792, 751, 686. 1H-NMR (500 MHz, CDCl3) δ (ppm): 9.09 (s, 1H, H-C(triazole)), 7.87 (d, 2H, 3J = 7.9 Hz, 2×H-C(Ph)), 7.75 (s, 1H, 
H-C(8)), 7.54 (t, 2H, 3J = 7.9 Hz, 2×H-C(Ph)), 7.45 (t, 1H, 3J = 7.9 Hz, 
H-C(Ph)), 4.12 (t, 2H, 3J = 7.1 Hz, (-CH2-)), 3.98–3.92 (m, 4H, 2×(-CH2-)), 1.94–1.85 (m, 2H, 
(-CH2-)), 1.73–1.64 (m, 6H, 3×(-CH2-)), 1.40–1.32 (m, 4H, 2×(-CH2-)), 1.32–1.21 (m, 4H, 
2×(-CH2-)), 0.87 (t, 3H, 3J = 7.1 Hz, (-CH3)). 13C-NMR (126 MHz, CDCl3) δ (ppm): 159.5, 154.5, 147.2, 145.4, 141.6, 137.2, 129.8, 129.0, 124.3, 123.2, 121.0, 45.6, 43.3, 31.7, 29.8, 28.8, 26.7, 26.0, 25.1, 22.7, 14.2. HRMS (ESI) m/z: [M+H]+Calcd for C25H33N8 444.2823; Found 444.2837 (3.14 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 7e:

13C-NMR (126 MHz, CDCl3) spectrum of compound 7e:

## 9-Heptyl-6-[1-(4-methoxyphenyl)-1H-1,2,3-triazol-4-yl]-2-[piperidin-1-yl]-9H-purine (7f)

Prepared according to general method C: Compound 5f (200 mg, 0.47 mmol, 1.0 eq.), piperidine (0.14 mL, ρ = 0.86 g/cm3, 1.41 mmol, 3.0 eq.), DMF (10 mL), 1 h, 100 °C. Silica gel column chromatography (DCM/MeOH, gradient 0% → 3%) provided compound 7f (yield: 181 mg, 81%) as a pale orange amorphous solid. Rf = 0.72 (DCM/MeOH = 20:1). HPLC: tR = 7.69 min, eluent E1. IR (KBr) ν (cm-1): 1606, 1586, 1376, 1255, 1246, 1131, 1030, 906, 825, 794, 635. 1H-NMR (500 MHz, CDCl3) δ (ppm): 9.00 (s, 1H, H-C(triazole)), 7.78–7.72 (m, 3H, 2×H-C(Ph), H-C(8)),1 7.05–7.01 (m, 2H, 2×H-C(Ph)), 4.12 (t, 2H, 3J = 6.7 Hz, (-CH2-)), 3.97–3.93 (m, 4H, 2×(-CH2-)), 3.87 (s, 3H, -(CH3)), 1.91–1.86 (m, 2H, (-CH2-)), 1.72–1.63 (m, 6H, 3×(-CH2-)), 1.37–1.32 (m, 4H, 2×(-CH2-)), 1.32–1.24 (m, 4H, 2×(-CH2-)), 0.87 (t, 3H, 3J = 7.0 Hz, (-CH3)). 13C-NMR (126 MHz, CDCl3) δ (ppm): 160.1, 159.5, 154.5, 147.3, 145.2, 141.6, 130.6, 124.5, 123.1, 122.6, 114.9, 55.8, 45.6, 43.3, 31.7, 29.8, 28.8, 26.7, 26.0, 25.1, 22.7, 14.2. HRMS (ESI) m/z: [M+H]+Calcd for C26H35N8O 475.2928; Found 475.2946 (3.78 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 7f:

13C-NMR (126 MHz, CDCl3) spectrum of compound 7f:

## 9-Heptyl-6-[1-(4-nitrophenyl)-1H-1,2,3-triazol-4-yl]-2-[piperidin-1-yl]-9H-purine (7g)

Prepared according to general method C: Compound 5g (100 mg, 0.22 mmol, 1.0 eq.), piperidine (0.07 mL, ρ = 0.86 g/cm3, 0.66 mmol, 3.0 eq.), DMF (2 mL), 1 h, 100 °C. Silica gel column chromatography (DCM/EtOH, gradient 0% → 5%) provided compound 7g (yield: 79 mg, 71%) as an orange amorphous solid. Rf = 0.71 (DCM/EtOH = 20:1). HPLC: tR = 7.08 min, eluent E1. IR (KBr) ν (cm-1): 1600, 1588, 1526, 1487, 1343, 1251, 1129, 1036, 987, 853, 792. 1H-NMR (500 MHz, CDCl3) δ (ppm): 9.13 (s, 1H, H-C(triazols)), 8.35 (d, 2H, 3J = 8.9 Hz, 2×H-C(Ph)) 8.06 (d, 2H, 3J = 8.9 Hz, 2×H-C(Ph)), 7.75 (s, 1H, H-C(8)), 4.10 (t, 2H, 3J = 7.0 Hz, (-CH2-)), 3.96–3.87 (m, 4H, 2×(-CH2-)), 1.92–1.84 (m, 2H, (-CH2-)), 1.72–1.61 (m, 6H, 3×(-CH2-)), 1.38–1.30 (m, 4H, 2×(-CH2-)), 1.30–1.17 (m, 4H, 2×(-CH2-)), 0.85 (t, 3H, 3J = 7.0 Hz, (-CH3)). 13C-NMR (126 MHz, CDCl3) δ (ppm): 159.5, 154.7, 147.4, 146.4, 146.2, 142.0, 141.3, 125.6, 124.0, 123.4, 120.9, 45.6, 43.3, 31.8, 29.8, 28.8, 26.7, 26.0, 25.1, 22.7, 14.2. HRMS (ESI) m/z: [M+H]+Calcd for C25H32N9O2 490.2673; Found 490.2688 (3.06 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 7g:

13C-NMR (126 MHz, CDCl3) spectrum of compound 7g:

## 9-[2-(Tert-butyldimethylsilaniloxy)-1-(tert-butyldimethylsilaniloxymethyl)ethyl]-6-[1-(4-methoxyphenyl)-2-(piperidin-1-yl)-1H-1,2,3-triazol-4-yl]-9H-purine (7h)

Prepared according to general method C: Compound 5h (1.87 g, 2.97 mmol, 1.0 eq.), piperidine (0.88 mL, ρ = 0.86 g/cm3, 8.91 mmol, 3.0 eq.), DMF (35 mL), 6 h, 100 °C. Silica gel column chromatography (DCM/MeCN, gradient 0% → 15%) provided compound 7h (yield: 1.52 g, 75%) as an orange amorphous solid. Rf = 0.58 (DCM/MeCN = 10:1). HPLC: tR = 5.00 min, eluent E2. IR (KBr) ν (cm-1): 1594, 1517, 1404, 1253, 1133, 1092, 1007, 910, 832, 778. 1H-NMR (500 MHz, CDCl3) δ (ppm): 9.01 (s, 1H, 
H-C(triazole)), 8.00 (s, 1H,H-C(8)), 7.76 (d, 2H, 3J = 8.7 Hz, 
2×H-C(Ar)), 7.03 (d, 2H, 3J = 8.7 Hz, 2×H-C(Ar)), 4.64 (quintet, 1H, 3J = 5.5 Hz, (-CH-)), 4.09 (dd, 2H, 2J = 10.3 Hz, 3J = 5.5 Hz, 2×(Ha-C)), 4.03 (dd, 2H, 2J = 10.3 Hz, 3J = 5.5 Hz, 2×(Hb-C)), 3.97–3.90 (m, 4H, 2×(-CH2-)), 3.88 (s, 3H, (-CH3)), 1.68–1.63 (m, 6H, 3×(-CH2-)), 0.87 (s, 18H, 2×C(CH3)3), 0.032 (s, 6H, 
2×Si-(CH3)), 0.027 (s, 6H, Si-(CH3)2). 13C-NMR (126 MHz, CDCl3) δ (ppm): 160.1, 159.3, 154.5, 147.2, 145.1, 141.6, 130.6, 124.6, 122.9, 122.7, 114.8, 61.1 (2C),1 57.2, 55.8, 45.6, 26.0, 25.9, 25.1, 18.3, -5.37, -5.44. HRMS (ESI) m/z: [M+H]+Calcd for C34H55N8O3Si2 679.3930; Found 679.3922 (1.2 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 7h:

13C-NMR (126 MHz, CDCl3) spectrum of compound 7h:

## 2-{6-[1-(Cyanomethyl)-1H-1,2,3-triazol-4-yl]-2-(piperidin-1-yl)-9H-purin-9-yl}ethyl 3,3,3-triphenylpropanoate (7i)

Prepared according to general method C: Compound 5i (160 mg, 0.27 mmol, 1.0 eq.), piperidine (80 μL, ρ = 0.86 g/cm3, 0.81 mmol, 3.0 eq.), DMF (5 mL), 14 h, 50 °C. Silica gel column chromatography (DCM/EtOH, gradient 0% → 2%) provided compound 7i (yield: 129 mg, 75%) as a colorless solid. Rf= 0.41 (DCM/EtOH = 20/1). HPLC: tR = 6.51 min, eluent E1. IR (KBr) ν 
(cm-1): 3057, 2930, 2262, 1734, 1590, 1446, 1141, 1039. 
1H-NMR (500 MHz, CDCl3) δ (ppm): 8.88 (s, 1H, 
H-C(triazole)), 7.46 (s, 1H, H-C(8)), 7.26‒7.13 (m, 15H, 15×H-C(Ar)), 5.46 (s, 2H, (-CH2-)), 4.16‒4.10 (m, 2H, (-CH2-)), 4.08‒4.02 (m, 2H, 
(-CH2-)), 3.93‒3.86 (m, 4H, 2×(-CH2-)), 3.71 (s, 2H, (-CH2-)), 1.71‒1.60 (m, 6H, 3×(-CH2-)). 
13C-NMR (126 MHz, CDCl3) δ (ppm): 170.7, 159.3, 154.4, 146.5, 146.3, 146.2, 142.1, 129.2, 128.0, 126.5, 126.4, 123.1, 112.6, 62.0, 55.9, 46.2, 45.6, 42.0, 37.7, 25.9, 25.0. HRMS (ESI) m/z: [M+H]+Calcd for C37H36N9O2 638.2986; Found 638.2993 (1.10 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 7i:

13C-NMR (126 MHz, CDCl3) spectrum of compound 7i:

## 2-(6-{1-[2-Oxo-2-(piperidin-1-yl)ethyl]-1H-1,2,3-triazol-4-yl}-2-(piperidin-1-yl)-9H-purin-9-yl)ethyl 3,3,3-triphenylpropanoate (7j)

Prepared according to general method C: Compound 5j (300 mg, 0.48 mmol, 1.0 eq.), piperidine (0.30 mL, ρ = 0.86 g/cm3, 2.88 mmol, 6.0 eq.), DMF (10 mL), 14 h, 20 °C. Silica gel column chromatography (DCM/MeCN, gradient 0% → 10%) provided product 5 (yield: 261 mg, 75%) as a pale orange solid. Rf = 0.38 (DCM/EtOH = 20/1). HPLC: tR = 6.70 min, eluent E1. IR (KBr) ν 
(cm-1): 2935, 1740, 1655, 1588, 1445, 1253, 1139, 1045. 1H-NMR (500 MHz, CDCl3) δ (ppm): 8.81 (s, 1H, 
H-C(triazole)), 7.45 (s, 1H, H-C(8)), 7.25‒7.13 (m, 15H, 15×H-C(Ar)), 5.33 (s, 2H, (-CH2-)), 4.12 (t, 2H, 3J = 5.4 Hz, (-CH2-)), 4.03 (t, 2H, 3J = 5.4 Hz, (-CH2-)), 3.92‒3.85 (m, 4H, 2×(-CH2-)), 3.70 (s, 2H, 
(-CH2-)), 3.58 (t, 2H, 3J = 5.2 Hz, (-CH2-)), 3.50 (t, 2H, 3J = 5.2 Hz, (-CH2-)), 1.70‒1.52 (m, 12H, 6×(-CH2-)). 13C-NMR (126 MHz, CDCl3) δ (ppm): 170.7, 163.0, 159.3, 154.2, 147.7, 146.3, 145.4, 141.8, 129.2, 128.0, 127.8, 126.5, 123.0, 62.0, 55.9, 51.5, 46.7, 46.2, 45.5, 43.6, 41.9, 26.4, 26.0, 25.5, 25.0, 24.3. HRMS (ESI) m/z: [M+H]+Calcd for C42H46N9O3 724.3718; Found 724.3706 (1.66 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 7j:

13C-NMR (126 MHz, CDCl3) spectrum of compound 7j:

## 2-[6-(1-Cyclohexyl-1H-1,2,3-triazol-4-yl)-2-(piperidin-1-yl)-9H-purin-9-yl]ethyl 3,3,3-triphenylpropanoate (7k)

Prepared according to general method C: Compound 5k (300 mg, 0.47 mmol, 1.0 eq.), piperidine (0.14 mL, ρ = 0.86 g/cm3, 1.42 mmol, 3.0 eq.), DMF (10 mL), 14 h, 50 °C. Silica gel column chromatography (DCM/EtOH, gradient 0% → 2%) provided product 7k (yield: 211 mg, 66%) as a colorless solid. Rf = 0.42 (DCM/EtOH = 20:1). HPLC: tR = 7.42 min, eluent E1. IR (KBr) ν (cm-1): 2933, 2856, 1740, 1586, 1516, 1445, 1256, 1141, 1041. 1H-NMR (500 MHz, CDCl3) δ (ppm): 8.64 (s, 1H, H-C(triazole)), 7.46 (s, 1H, H-C(8)), 7.26‒7.10 (m, 15H, 15×H-C(Ar)), 4.61 (tt, 1H, 3J = 11.8 Hz, 3J = 3.8 Hz, 
(-CH-)), 4.13 (t, 2H, 3J = 5.1 Hz, (-CH2-)), 4.04 (t, 2H,
 3J = 5.1 Hz, (-CH2-)), 3.96‒3.85 (m, 4H, 2×(-CH2-)), 3.70 (s, 2H, (-CH2-)), 2.29 (d, 2H,3J = 11.8 Hz, 2×(Hax-CH-)), 1.95 (d, 2H, 2J = 13.7 Hz, 2×(Heq-CH-)), 1.91‒1.74 (m, 3H, 3×(Heq-CH-)), 1.71‒1.58 (m, 6H, 3×(-CH2-)), 1.49 (qt, 2H, 2J = 3J = 13.0 Hz, 3J = 3.5 Hz, 2×(Hax-CH-)), 1.32 (qt, 1H, 2J = 3J = 13.0 Hz, 3J = 3.5 Hz, (Hax-CH-)). 13C-NMR (126 MHz, CDCl3) δ (ppm): 170.6, 159.4, 154.1, 148.0, 146.3, 144.2, 141.5, 129.2, 128.0, 126.5, 124.0, 122.9, 62.0, 60.3, 55.9, 46.2, 45.5, 41.9, 33.7, 26.0, 25.3, 25.2, 25.0. HRMS (ESI) m/z: [M+H]+Calcd for C41H45N8O2 681.3660; Found 681.3645 (2.20 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 7k:

13C-NMR (126 MHz, CDCl3) spectrum of compound 7k:

## 2-[6-(1-Decyl-1H-1,2,3-triazol-4-yl)-2-(piperidin-1-yl)-9H-purin-9-yl]ethyl 3,3,3-triphenylpropanoate (7l)

Prepared according to general method C: Compound 5l (300 mg, 0.43 mmol, 1.0 eq.), piperidine (0.13 mL, ρ = 0.86 g/cm3, 1.30 mmol, 3.0 eq.), DMF (10 mL), 14 h, 50 °C. Silica gel column chromatography (DCM/EtOH, gradient 0% → 2%) provided compound 7l (yield: 283 mg, 89%) as a pale yellow oil. Rf = 0.54 (DCM/EtOH = 20:1). HPLC: tR = 8.66 min, eluent E1. IR (KBr) ν (cm-1): 2926, 2854, 1740, 1586, 1516, 1446, 1256, 1141, 1040. 
1H-NMR (500 MHz, CDCl3) δ (ppm): 8.64 (s, 1H, 
H-C(triazole)), 7.46 (s, 1H, H-C(8)), 7.26‒7.12 (m, 15H, 15×H-C(Ar)), 4.47 (t, 2H, 3J = 7.2 Hz, (-CH2-)), 4.16‒4.10 (m, 2H, (-CH2-)), 4.08‒4.02 (m, 2H, 
(-CH2-)), 3.96‒3.86 (m, 4H, 2×(-CH2-)), 3.70 (s, 2H, (-CH2-)), 2.02‒1.92 (m, 2H, (-CH2-)), 1.73‒1.59 (m, 6H, 3×(-CH2-)), 1.41‒1.18 (m, 14H, 7×(-CH2-)), 0.87 (t, 3H, 3J = 6.5 Hz, (-CH3)). 
13C-NMR (126 MHz, CDCl3) δ (ppm): 170.6, 159.4, 154.0, 147.7, 146.3, 144.5, 141.5, 129.1, 127.9, 126.4, 126.2, 122.8, 62.0, 55.9, 50.6, 46.2, 45.5, 41.8, 31.9, 30.5, 29.5, 29.4, 29.3, 29.1, 26.5, 25.9, 25.0, 22.7, 14.2. HRMS (ESI) m/z: [M+H]+Calcd for C45H54N8O2739.4442; Found 739.4416 (2.16 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 7l:

13C-NMR (126 MHz, CDCl3) spectrum of compound 7l:

## 2-[6-(1-Benzyl-1H-1,2,3-triazol-4-yl)-2-(piperidin-1-yl)-9H-purin-9-yl]ethyl 3,3,3-triphenylpropanoate (7m)

Prepared according to general method C: Compound 5m (100 mg, 0.16 mmol, 1.0 eq.), piperidine (46 µL, ρ = 0.86 g/cm3, 0.47 mmol, 3.0 eq.), DMF (2 mL), 1 h, 100 °C. Silica gel column chromatography (DCM/MeOH, gradient 0% → 4%) provided compound 7m (yield: 90 mg, 83%) as a gray amorphous solid. Rf = 0.32 (DCM/MeOH = 20:1). HPLC: tR = 7.13 min, eluent E1. IR (KBr) ν (cm-1): 1736, 1593, 1496, 1447, 1325, 1235, 1145, 1042, 938, 857, 701. 1H-NMR (500 MHz, CDCl3) δ (ppm): 8.58 (s, 1H, H-C(triazole)), 7.43 (s, 1H, H-C(8)), 7.37–7.30 (m, 5H, 5×H-C(Ph)), 7.24–7.13 (m, 15H, 15×H-C(Ph)), 5.66 (s, 2H, (-CH2-)), 4.12 (t, 2H, 3J = 4.9 Hz, (-CH2-)), 4.02 (t, 2H, 3J = 4.9 Hz (-CH2-)), 3.90–3.86 (m, 4H, 2×(-CH2-)), 3.69 (s, 2H, (-CH2-)), 1.68–1.58 (m, 6H, 3×(-CH2-)). 13C-NMR (126 MHz, CDCl3) δ (ppm): 170.7, 159.4, 154.1, 147.6, 146.3, 145.2, 141.7, 134.9, 129.2, 129.2, 128.8, 128.1, 128.0, 126.5, 126.4, 122.9, 62.0, 55.9, 54.4, 46.2, 45.6, 41.9, 26.0, 25.0. HRMS (ESI) m/z: [M+H]+Calcd for C42H41N8O2 689.3347; Found 689.3334 (1.86 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 7m:

13C-NMR (126 MHz, CDCl3) spectrum of compound 7m:

# 6. Synthesis of C-N conjugated triazolylpurines

Scheme S1. Synthesis of C-N boded triazolylpurine derivatives

## 2,6-Diazido-9-[2-(tert-butyldimethylsilaniloxy)-1-(tert-butyldimethylsilaniloxymethyl)ethyl]-9H-purine (10)

To a solution of 2a (3.00 g, 6.10 mmol, 1.0 eq.) in acetone (50 mL) NaN3 (2.38 g, 36.62 mmol, 6.0 eq.) was added and the reaction mixture was stirred isolated from the daylight at 50 oC for 16 h. Then it was evaporated, suspended in H2O (50 ml), filtered and washed with an additional H2O (150 ml). Yield: 3.01 g, 98%, white amorphous solid. Rf = 0.50 (DCM = 100%). HPLC: tR = 5.82 min, eluent E2. IR (KBr) ν (cm-1): 1601, 1576, 1367, 1251, 1214, 1092, 1005, 887, 837, 774. 1H-NMR (500 MHz, CDCl3) δ (ppm): 8.10 (s, 1H, H-C(8)), 4.71 (quintet, 1H, 3J = 5.5 Hz, (-CH-)), 4.04 (dd, 2H, 2J = 10.5 Hz, 3J = 5.5 Hz, 2×Ha-C), 3.97 (dd, 2H, 2J = 10.5 Hz, 3J = 5.5 Hz, 2×Hb-C), 0.84 (s, 18H, 2×C(CH3)3), 0.00 (s, 6H, Si-(CH3)2), -0.01 (s, 6H, Si-(CH3)2). 13C-NMR (126 MHz, CDCl3) δ (ppm): 155.8, 154.2, 153.7, 143.8, 121.2, 61.1 (2C),1 58.2, 25.8, 18.2, -5.4, -5.5. HRMS (ESI) m/z: [M+H]+Calcd for C20H37ClN10O2Si2 505.2634; Found 505.2636 (0.4 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 10:

13C-NMR (126 MHz, CDCl3) spectrum of compound 10:

## 6-Azido-9-[2-(tert-butyldimethylsilaniloxy)-1-(tert-butyldimethylsilaniloxymethyl)ethyl]-2-(piperidin-1-yl)-9H-purine (11)

Prepared according to general method C: Compound 10 (1.86 g, 3.87 mmol, 1.0 eq.), piperidine (1.11 mL, ρ = 0.86 g/cm3, 11.06 mmol, 3.0 eq.), DMF (85 mL), 4 h, 25 °C. Silica gel column chromatography (Hex/EtOAc, gradient 0% → 10%) provided compound 11 (yield: 1.42 g, 70%) as a white amorphous solid. Rf = 0.57 (Hex/EtOAc = 5:1). HPLC: tR = 11.0 min, eluent E2. IR (KBr) ν (cm-1): 1621, 1578, 1462, 1302, 1251, 1106, 1085, 1005, 835, 774. 1H-NMR (500 MHz, CDCl3) δ (ppm): 7.82 (s, 1H, H-C(8)), 4.55 (quintet, 1H, 3J = 5.5 Hz, (-CH-)), 4.02 (dd, 2H, 2J = 10.5 Hz, 3J = 5.5 Hz, 2×Ha-C), 3.97 (dd, 2H, 2J = 10.5 Hz, 3J = 5.5 Hz, 2×Hb-C), 3.81 (t, 4H, 
3J = 5.2 Hz, 2×(-CH2-)), 1.70–1.64 (m, 2H, (-CH2-)), 1.61–1.57 (m, 4H, 2×(-CH2-)), 0.86 (s, 18H, 2×C(CH3)3), 0.012 (s, 6H, Si-(CH3)2), 0.008 (s, 6H, Si-(CH3)2). 13C-NMR (126 MHz, CDCl3) 
δ (ppm): 158.4, 154.9, 152.5, 140.8, 116.8, 61.0 (2C),1 57.5, 45.5, 25.93, 25.86, 25.0, 18.3, -5.4, 
-5.5. HRMS (ESI) m/z: [M+H]+Calcd for C25H47N8O2Si2 547.3355; Found 547.3359 (0.7 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 11:

13C-NMR (126 MHz, CDCl3) spectrum of compound 11:

## 9-[2-(Tert-butyldimethylsilaniloxy)-1-(tert-butyldimethylsilaniloxymethyl)ethyl]-2,6-bis[4-(4-methoxyphenyl)-1H-1,2,3-triazol-1-yl]-9H-purine (12)

Prepared according to general method B: Compound 10 (700 mg, 1.39 mmol, 1.0 eq.), CuI (95 mg, 0.50 mmol, 0.36 eq.), AcOH (0.09 mL, ρ = 0.79 g/cm3, 1.53 mmol, 1.1 eq.), Et3N (0.21 mL, ρ = 0.73 g/cm3, 1.53 mmol, 1.1 eq.) and 
1-ethynyl-4-methoxybenzene (550 mg, 4.16 mmol, 3.0 eq.), DCM (30 mL), 25 °C, 40 min. Crystallization from ethanol (40 mL) provided product 12 (yield: 720 mg, 63%) as a beige amorphous solid. Rf = 0.83 (DCM/MeOH = 20:1). HPLC: tR = 5.30 min, eluent E2. m. p. = 192−193 oC. IR (KBr) ν (cm-1): 1608, 1567, 1469, 1440, 1260, 1219, 1094, 999, 832, 789. 1H-NMR (500 MHz, CDCl3) δ (ppm): 9.27 (s, 1H, H-C(triazole)), 8.87 (s, 1H, H-C(triazole)), 8.55 (s, 1H, H-C(8)), 7.98 (d, 2H, 3J = 8.6 Hz, 2×H-C(Ar)), 7.93 (d, 2H, 3J = 8.6 Hz, 
2×H-C(Ar)), 7.03 (d, 2H, 3J = 8.7 Hz, 2×H-C(Ar)), 7.02 (d, 2H, 3J = 8.7 Hz, 2×H-C(Ar)), 5.03 (quintet, 1H, 3J = 5.4 Hz, (-CH-)), 4.18 (dd, 2H, 2J  = 10.7 Hz, 3J = 5.4 Hz, 2×Ha-C), 4.10 (dd, 2H, 2J = 10.7 Hz, 3J = 5.4 Hz, 2×Hb-C), 3.88 (s, 6H, 2×(CH3)), 0.86 (s, 18H, 2×C(CH3)3), 0.05 (s, 12H, 2×Si-(CH3)2). 13C-NMR (126 MHz, CDCl3) δ (ppm): 160.3, 160.2, 156.2, 148.7, 148.4, 148.1, 147.3, 145.3, 127.8, 127.6, 122.7, 122.4, 121.7, 118.8, 118.2, 114.52, 114.51, 61.3 (2C),1 58.3, 55.5 (2С),1 25.9, 18.2, -5.4, -5.5. HRMS (ESI) m/z: [M+H]+Calcd for C38H53N10O4Si2 769.3784; 769.3779 (0.6 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 12:

13C-NMR (126 MHz, CDCl3) spectrum of compound 12:

## 9-[2-(Tert-butyldimethylsilaniloxy)-1-(tert-butyldimethylsilaniloxymethyl)ethyl]-6-[4-(4-methoxyphenyl)-2-(piperidin-1-yl)-1H-1,2,3-triazol-1-yl]-9H-purine (14)

Prepared according to general method B: Compound 11 (1.37 g, 2.50 mmol, 1.0 eq.), CuI (95 mg, 0.50 mmol, 0.2 eq.), AcOH (0.16 mL, ρ = 1.05 g/cm3, 2.75 mmol, 1.1 eq.), Et3N (0.38 mL, ρ = 0.73 g/cm3, 2.75 mmol, 1.1 eq.) and 1-ethynyl-4-methoxybenzene (660 mg, 5.00 mmol, 2.0 eq.), DMF (50 mL), 25 °C, 1 h. Silica gel column chromatography (DCM/MeOH, gradient 0% → 5%) provided product 14 (yield: 1.24 g, 73%) as a white amorphous solid. Rf = 0.73 (DCM/MeOH = 20:1). HPLC: tR = 9.18 min, eluent E2. IR (KBr) ν (cm-1): 1626, 1561, 1533, 1443, 1251, 1109, 1092, 1019, 835, 778. 1H-NMR (500 MHz, CDCl3) δ (ppm): 9.05 (s, 1H, H-C(triazole)), 8.08 (s, 1H, H-C(8)), 7.93 (d, 2H, 3J = 8.7 Hz, 2×H-C(Ar)), 6.99 (d, 2H, 3J = 8.7 Hz, 2×H-C(Ar)), 4.66 (quintet, 1H, 3J = 5.5 Hz, (-CH-)), 4.08 (dd, 2H, 2J = 10.4 Hz, 3J = 5.5 Hz, 2×(Hb-C)), 4.02 (dd, 2H, 2J = 10.4 Hz, 3J = 5.5 Hz, 2×(Hb-C)), 3.94–3.89 (m, 4H, 
2×(-CH2-)), 3.86 (s, 3H, (-CH3)), 1.74–1.63 (m, 6H, 3×(-CH2-)), 0.88 (s, 18H, 2×C(CH3)3), 0.043 (s, 6H, 2×Si-(CH3)), 0.043 (s, 6H, Si-(CH3)2). 13C-NMR (126 MHz, CDCl3) δ (ppm): 159.9, 158.3, 157.0. 147.5, 145.1, 142.7, 127.7, 123.2, 118.7, 115.3, 114.4, 61.1 (2C),2 57.5, 55.5, 45.7, 25.9 (2C),1 25.0, 18.3, -5.37, -5.44. HRMS (ESI) m/z: [M+H]+Calcd for C34H55N8O3Si2 679.3930; Found 679.3922 (1.2 ppm).

1H-NMR (500 MHz, CDCl3) spectrum of compound 14:

13C-NMR (126 MHz, CDCl3) spectrum of compound 14:

# 7. TBS group cleavage

Scheme S2. TBS group cleavage of compound 6e

## 2-{2,6-Bis[1-(4-methoxyphenyl)-1H-1,2,3-triazol-4-yl]-9H-purin-9-yl}propane-1,3-diol (8b)

General method D for TBS group cleavage: To a solution of 6e (50 mg, 0.09 mmol) in THF (1.5 mL) and H2O (1.5 mL) AcOH was added (2.5 mL) and the reaction mixture was stirred at 50 oC for 14 h. Then it was evaporated and co-evaporated with toluene (20 mL). Precipitate was suspended in Hex/EtOAc mixture (1:1, 20 mL) and filtered to provide product 8b (yield: 30 mg, 86%) as a pale brown amorphous solid. HPLC: tR = 6.60 min, eluent E4. IR (KBr) ν (cm-1): 1593, 1515, 1384, 1326, 1249, 1170, 1045, 989, 927, 835. 1H-NMR (500 MHz, DMSO-d6) 
δ (ppm): 9.57 (s, 1H, H-C(triazole)), 9.38 (s, 1H, H-C(triazole)), 8.72 (s, 1H, H-C(8)), 7.99 (d, 2H, 3J = 9.3 Hz, 2×H-C(Ar)), 7.98 (d, 2H, 3J = 9.3 Hz, 2×H-C(Ar)), 7.21 (d, 2H, 3J = 9.3 Hz, 
2×H-C(Ar)), 7.18 (d, 2H, 3J = 9.3 Hz, 2×H-C(Ar)), 5.14 (t, 2H, 3J = 5.3 Hz, 2×(-OH)), 4.86 (quintet, 1H, 3J = 5.3 Hz, (-CH-)), 4.07–4.01 (m, 2H, 2×Ha-C), 3.98–3.91 (m, 2H, 2×Hb-C), 3.87 (s, 3H, (-CH3)), 3.86 (s, 3H, (-CH3)).  13C-NMR (126 MHz, 
DMSO-d6) δ (ppm): 159.7, 159.5, 153.4, 152.0, 147.7, 146.8, 146.4, 143.8, 129.9, 129.7, 128.6, 125.5, 124.1, 122.4, 122.0, 115.0, 114.9, 59.8 (2C),1 59.4, 55.65, 55.62. HRMS (ESI) m/z: [M+H]+Calcd for C26H25N10O4 541.2055; Found 541.2040 (2.77 ppm).

1H-NMR (500 MHz, DMSO-d6) spectrum of compound 8b:

13C-NMR (126 MHz, DMSO-d6) spectrum of compound 8b:

## 2-(6-(1-(4-Methoxyphenyl)-1H-1,2,3-triazol-4-yl)-2-(piperidin-1-yl)-9H-purin-9-yl)propane-1,3-diol (8a)

Scheme S3. TBS group cleavage of compound 7h

Prepared according to general method D: Compound 7h (1.05 g, 2.33 mmol), THF (30 mL), H2O (30 mL), AcOH (50 mL), 50 °C, 14 h. Yield: 392 mg, 57%, an yellow amorphous solid. HPLC: tR = 6.31 min, eluent E4. IR (KBr) ν (cm-1): 1591, 1518, 1445, 1308, 1251, 1050, 971, 910, 832, 794. 1H-NMR (500 MHz, DMSO-d6) δ (ppm): 9.37 (s, 1H, H-C(triazole)), 8.17 (s, 1H, H-C(8)), 7.94 (d, 2H, 3J = 9.0 Hz, 2×H-C(Ar)), 7.17 (d, 2H, 3J = 9.0 Hz, 2×H-C(Ar)), 5.02 (t, 2H, 
3J = 5.4 Hz, 2×(-OH)), 4.53 (quintet, 1H, 3J = 5.4 Hz, (-CH-)), 3.95–3.80 (m, 11H, 2×(Ha-C), 2×(Hb-C), 2×(-CH2-), (-CH3)), 1.70–1.62 (m, 2H, (-CH2-)), 1.62–1.56 (m, 4H, 2×(-CH2-)). 13C-NMR (126 MHz, DMSO-d6) δ (ppm): 159.5, 158.2, 154.3, 146.4, 144.2, 142.9, 129.8, 125.0, 123.0, 122.3, 114.9, 59.6 (2C),1 58.8, 55.6, 44.9, 25.4, 24.4. HRMS (ESI) m/z: [M+H]+Calcd for C22H27N8O3 451.2201; Found 451.2202 (0.22 ppm).

1H-NMR (500 MHz, DMSO-d6) spectrum of compound 8a:

13C-NMR (126 MHz, DMSO-d6) spectrum of compound 8a:

## 2-{2,6-Bis[4-(4-methoxyphenyl)-1H-1,2,3-triazol-1-yl]-9H-purin-9-yl}propane-1,3-diol (13)

Prepared according to general method D: Compound 12 (500 mg, 0.92 mmol), THF (6 mL), H2O (6 mL), AcOH (9 mL), 50 °C, 14 h. Yield: 275 mg, 78%, a white amorphous solid. HPLC: tR = 6.98 min, eluent E4. IR (KBr) ν (cm-1): 1607, 1582, 1502, 1451, 1417, 1255, 1229, 1015, 1009, 837. 1H-NMR (500 MHz, DMSO-d6) δ (ppm): 9.68 (s, 1H, H-C(triazole)), 9.53 (s, 1H, 
H-C(triazole)), 8.93 (s, 1H, H-C(8)), 8.03 (d, 2H, 3J = 9.2 Hz, 2×H-C(Ar)), 8.01 (d, 2H, 3J = 9.2 Hz, 2×H-C(Ar)), 7.12 (d, 2H, 3J = 9.2 Hz, 2×H-C(Ar)), 7.10 (d, 2H, 3J = 9.2 Hz, 2×H-C(Ar)), 5.20 (s, 2H, 2×(-OH)), 4.95–4.86 (m, 1H, (-CH-)), 4.08–4.02 (m, 2H, 2×Ha-C), 3.98–3.92 (m, 2H,2×Hb-C), 3.84 (s, 3H, (-CH3)), 3.83 (s, 3H, (-CH3)). 13C-NMR (126 MHz, DMSO-d6) δ (ppm): 159.7, 159.6, 156.5, 148.9, 147.4, 147.0, 146.9, 144.2, 127.3, 127.1, 122.31, 122.27, 121.9, 119.5 (2C),2 114.6, 114.5, 60.2, 59.6 (2C),1 55.28, 55.26. HRMS (ESI) m/z: [M+H]+Calcd for C26H25N10O4 541.2055; Found 541.2055 (0 ppm).

1H-NMR (500 MHz, DMSO-d6) spectrum of compound 13:

13C-NMR (126 MHz, DMSO-d6) spectrum of compound 13:

## 2-{6-[4-(4-Methoxyphenyl)-1H-1,2,3-triazol-1-yl]-2-[piperidin-1-yl]-9H-purin-9-yl}propane-1,3-diol (15)

Prepared according to general method D: Compound 13 (1.03 mg, 2.29 mmol), THF (30 mL), H2O (30 mL), AcOH (50 mL), 50 °C, 14 h. Yield: 551 mg, 81%, beige amorphous solid. HPLC: tR = 7.00 min, eluent E4. IR (KBr) ν (cm-1): 1631, 1565, 1489, 1445, 1250, 1231, 1018, 917, 848, 786.  1H-NMR (500 MHz, DMSO-d6) δ (ppm): 9.40 (s, 1H, H-C(triazole)), 8.28 (s, 1H, H-C(8)), 7.98 (d, 2H, 3J = 8.7 Hz, 
2×H-C(Ar)), 7.07 (d, 2H, 3J = 8.7 Hz, 2×H-C(Ar)), 5.04 (t, 2H, 3J = 5.5 Hz, 2×(-OH)), 4.56 (quintet, 1H, 3J = 5.5 Hz, (-CH-)), 3.96–3.89 (m, 2H, 2×(Ha-C)), 3.89–3.83 (m, 6H, 2×(Hb-C), 2×(-CH2-)), 3.82 (s, 3H, (-CH3)), 1.70–1.64 (m, 2H, (-CH2-)), 1.64–1.57 (m, 4H, 2×(-CH2-)). 13C-NMR (126 MHz, DMSO-d6) δ (ppm): 159.5, 157.4, 157.0, 146.5, 144.3, 144.2, 127.1, 122.3, 119.4, 115.4, 114.4, 59.5 (2C),1 59.2, 55.2, 45.0, 25.3, 24.3. HRMS (ESI) m/z: [M+H]+Calcd for C22H27N8O3 451.2201; Found 451.2215 (3.1 ppm).

1H-NMR (500 MHz, DMSO-d6) spectrum of compound 15:

13C-NMR (126 MHz, DMSO-d6) spectrum of compound 15:

# 8. Photophysical data

Figure S1. Absorption spectra of bistriazolylpurine derivatives

Figure S2. Absorption spectra of target compounds 7, 8 and 15

Figure S3. Emission spectra of target compounds 7 in thin layer films

# 9. In vitro cytotoxic experiments

NIH-3T3 (mouse embryo fibroblast), HaCaT (human keratinocytes) and TrampC1 (transgenic adenocarcinoma of the mouse prostate) were maintained in Dulbecco’s modified Eagle’s medium (DMEM) supplemented with 10% fetal bovine serum (FBS), antibiotic-antimycotic (1%), L-glutamine (2 mM) and nonessential amino acids (1%) in 5% CO2 at 37 °C. The in vitro cytotoxicity of the purine derivatives was evaluated using MTT (3-(4,5-dimethylthiazol-2-yl)-2,5-diphenyltetrazolium bromide) test. 7.5 × 103 cells were seeded in 96-well plates and incubated with DMEM containing 10% FBS in a humidified incubator with 5% CO2 at 37 °C for 24 h. After incubation, medium was aspired and the cells were further incubated with DMEM containing 10% FBS and the purine derivatives at different concentrations and further cultured for 72 h. After that, the culture medium was replaced with MTT (50 µg in 100 uL PBS) and incubated for another 1 h at 37 °C. The absorbance at 570 nm was measured using a monochromatic microplate spectrophotometer (Synergy 4 Multi-Mode; Biotek Instruments, Winooski, VT, USA).

The mean and standard deviations are derived from 4 separate experiments.

Compound 5e

NIH3T3	885.8 µM

HaCaT	598.1 µM

TrampC1	919.7 µM

Compound 5f

NIH3T3	1427.5 µM

HaCaT	703.4 µM

TrampC1	1092.0 µM

Compound 5g

NIH3T3	719.2 µM

HaCaT	736.2 µM

TrampC1	206.2 µM

Compound 7e

NIH3T3	875.4 µM

HaCaT	438.6 µM

TrampC1	59.6 µM

Compound 7f

NIH3T3	1212.8 µM

HaCaT	603.6 µM

TrampC1	1124.5 µM

Compound 8a

NIH3T3	1528.7 µM

HaCaT	827.7 µM

TrampC1	1533.0 µM

Compound 15

NIH3T3	172.3 µM

HaCaT	73.0 µM

TrampC1	784.9 µM

Compound 8b

NIH3T3	1104.6 µM

HaCaT	558.9 µM

TrampC1	1179.4 µM

Compound 13

NIH3T3	1012.1 µM

HaCaT	552.4 µM

TrampC1	650.6 µM

# References

[1] Kapilinskis Z, Novosjolova I, Turks M (2018) Purine-Furan and Purine-Thiophene Conjugates Molbank M1024:1–7. https://doi.org/10.3390/M1024

[2] Šišuļins A, Bucevičius J, Tseng YT, Novosjolova I, Traskovskis K, Bizdēna Ē, Chang HT, Tumkevičius S, Turks M (2019) Synthesis and fluorescent properties of N(9)-alkylated 2-amino-6-triazolylpurines and 7-deazapurines. Beilstein J. Org. Chem. 15:474–489. https://doi.org/10.3762/bjoc.15.41

[3] Kim HS, Barak D, Harden TK, Boyer JL, Jacobson KA (2001) Acyclic and Cyclopropyl Analogues of Adenosine Bisphosphate Antagonists of the P2Y1 Receptor: Structure-Activity Relationships and Receptor Docking. J. Med. Chem. 44:3092–3108. https://doi.org/10.1021/jm010082h

[4] Barral K, Moorhouse AD, Moses JE (2007) Efficient Conversion of Aromatic Amines into Azides: A One-Pot Synthesis of Triazole Linkages. Org. Lett. 9:1809–1811. https://doi.org/10.1021/ol070527h

[5] Das J, Patil SN, Awasthi R, Narasimhulu CP, Trehan S (2005) An Easy Access to Aryl Azides from Aryl Amines under Neutral Conditions. Synthesis, 11:1801–1806. https://doi.org/10.1055/s-2005-869974

[6] Verkhozina ON, Kizhnyaev VN, Vereshchagin LI, Rokhin AV, Smirnov AI (2003) Synthesis of Polynuclear Nonfused Azoles. Russ. J. Org. 39:1792-1796. https://doi.org/10.1023/B:RUJO.0000019746.10504.f3

[7] Bonacorso HG, Libero FM, Dal Forno GM, Pittaluga EP, Back DF, Hörner M, Martins MAP, Zanatta N (2016) New regioselective synthesis of polyfunctionalized 3-ferrocenyl-1H-pyrroles under microwave irradiation. Tetrahedron Lett. 57-41:4568-4573. https://doi.org/10.1016/j.tetlet.2016.08.088

[8] Alvarez SG, Alvarez MT (1997) A Practical Procedure for the Synthesis of Alkyl Azides at Ambient Temperature in Dimethyl Sulfoxide in High Purity and Yield. Synthesis 4:413-414.

https://doi.org/10.1055/s-1997-1206

The signal was assigned from 1H-13C HSQC spectra

1 The signal was assigned from 1H-13C HSQC spectra

1 The signal was assigned from 1H-13C HSQC spectra

2 The signal was assigned from 1H-13C HSQC and 1H-13C HMBC spectra.

2 The signal was assigned from 1H-13C HSQC and 1H-13C HMBC spectra.

1 The signal was assigned from 1H-13C HSQC spectra.

3 The signal was assigned from 1H-13C HMBC spectra.

1 The signal was assigned from 1H-13C HSQC spectra.

2 The signal was assigned from 1H-13C HSQC and 1H-13C HMBC spectra.

2 The signal was assigned from 1H-13C HSQC and 1H-13C HMBC spectra.

2 The signal was assigned from 1H-13C HSQC and 1H-13C HMBC spectra.

3 The signal was assigned from 1H-13C HMBC spectra.

1 The signal was assigned from 1H-13C HSQC spectra.

1 The signal was assigned from 1H-13C HSQC spectra.

1 The signal was assigned from 1H-13C HSQC spectra.

1 The signal was assigned from 1H-13C HSQC spectra.

1 The signal was assigned from 1H-13C HSQC spectra.

1 The signal was assigned from 1H-13C HSQC spectra.

2 The signal was assigned from 1H-13C HSQC and 1H-13C HMBC spectra.

1 The signal was assigned from 1H-13C HSQC spectra.

1 The signal was assigned from 1H-13C HSQC spectra.

1 The signal was assigned from 1H-13C HSQC spectra.

2 The signal was assigned from 1H-13C HSQC and 1H-13C HMBC spectra.

1 The signal was assigned from 1H-13C HSQC spectra.