Supplementary

Fig. S1. DMA curves for storage modulus of developed polymer foam samples.

Fig. S2. DMA curves for loss modulus of developed polymer foam samples.

Fig. 3S. DMA curves for loss modulus and tanδ of for EIRTOFA_TMP_AA_ESOA polymer sample.

Equation 1 was used to calculate the cross-link density using the results from the DMA test [1–4]:

| νe = Erubbery'3RT | (1) |
| --- | --- |

where ve is the cross-link density (mol·cm−3); E'rubbery is the storage modulus (MPa) at temperature Tg(DMA)+50 (K); R is the gas constant; T is the temperature that corresponds to the rubbery storage modulus (K).

According to Equation 2, the molecular weight between cross-links Mc (g·mol−1) was found [5].

| Mc=3RTρErubbery' | (2) |
| --- | --- |

References

[1]	T.H. Kim, M. Kim, W. Lee, H.G. Kim, C.S. Lim, B. Seo, Synthesis and characterization of a polyurethane phase separated to nano size in an epoxy polymer, Coatings. 9 (2019). https://doi.org/10.3390/coatings9050319.

[2]	K.K. Jena, K.V.S.N. Raju, Synthesis and characterization of hyperbranched polyurethane hybrids using tetraethoxysilane (TEOS) as cross-linker, Ind. Eng. Chem. Res. 47 (2008) 9214–9224. https://doi.org/10.1021/ie800884y.

[3]	L.W. Hill, Calculation of crosslink density in short chain networks, Prog. Org. Coatings. 31 (1997) 235–243. https://doi.org/10.1016/S0300-9440(97)00081-7.

[4]	C. Zhang, S.A. Madbouly, M.R. Kessler, Biobased polyurethanes prepared from different vegetable oils, ACS Appl. Mater. Interfaces. 7 (2015) 1226–1233. https://doi.org/10.1021/am5071333.

[5]	I.M. Barszczewska-Rybarek, A. Korytkowska-Wałach, M. Kurcok, G. Chladek, J. Kasperski, DMA analysis of the structure of crosslinked poly(methyl methacrylate)s, Acta Bioeng. Biomech. 19 (2017) 47–53. https://doi.org/10.5277/ABB-00590-2016-01.