| Sample | NFC susp. (g) | Xylan solution (g) | Lignin solution (g) | Pectin (g) | Glycerol (g) | CA (g) |
| --- | --- | --- | --- | --- | --- | --- |
| Hemp | 100 | - | - | - | - | - |
| H-CA0.5 | 100 | - | - | - | - | 0.5 |
| H-CA1 | 100 | - | - | - | - | 1 |
| H-CA2.5 | 100 | - | - | - | - | 2.5 |
| H-CA5 | 100 | - | - | - | - | 5 |
| WM | 100 | 11.8 | 32 | - | - | - |
| WM-CA0.5 | 100 | 11.8 | 32 | - | - | 0.5 |
| WM-CA1 | 100 | 11.8 | 32 | - | - | 1 |
| WM-CA2.5 | 100 | 11.8 | 32 | - | - | 2.5 |
| WM-CA5 | 100 | 11.8 | 32 | - | - | 5 |
| H-P0.5-CA0.5 | 100 | - | - | 0.5 | - | 0.5 |
| H-P0.25-CA1 | 100 | - | - | 0.25 | - | 1 |
| H-P0.5-CA1 | 100 | - | - | 0.5 | - | 1 |
| H-P1-CA1 | 100 | - | - | 1 | - | 1 |
| WM-P0.25-CA1 | 100 | 11.8 | 32 | 0.25 | - | 1 |
| WM-P0.5-CA1 | 100 | 11.8 | 32 | 0.5 | - | 1 |
| WM-P1-CA1 | 100 | 11.8 | 32 | 1 | - | 1 |
| H-G0.5-CA1 | 100 | - | - | - | 0.5 | 1 |
| H-G1-CA1 | 100 | - | - | - | 1 | 1 |
| H-G2-CA1 | 100 | - | - | - | 2 | 1 |
| WM-G0.5-CA1 | 100 | 11.8 | 32 | - | 0.5 | 1 |
| WM-G1-CA1 | 100 | 11.8 | 32 | - | 1 | 1 |
| WM-G2-CA1 | 100 | 11.8 | 32 | - | 2 | 1 |
| H-P0.5-G1-CA1 | 100 | - | - | 0.5 | 1 | 1 |
| H-P0.5-G2-CA1 | 100 | - | - | 0.5 | 2 | 1 |
| WM-P0.5-G1-CA1 | 100 | 11.8 | 32 | 0.5 | 1 | 1 |
| WM-P0.5-G2-CA1 | 100 | 11.8 | 32 | 0.5 | 2 | 1 |

Table S1. Summary of all prepared foam compositions and the quantities of each modifier.

Figure S1. FTIR spectra of all remaining samples for (a) Hemp foams and (b) WM foams.

Figure S2. SEM micrographs of selected foam samples shown at 100x magnification.

Figure S3. SEM micrographs of selected foam samples shown at 1000x magnification.

Figure S4. Influence of increasing CA concentrations in H- and WM-foams on compression properties.

Figure S5. Foam recovery capabilities and cycle performance in kerosene.

Figure S6. Thermal properties dependence on moisture content: (a) thermal conductivity, (b) thermal diffusivity, and (c) specific heat.