Phase composition of silver-doped hydroxyapatite depending on silver content

L.Poca1, A.Dubnika2, D.Loca2, L.Berzina-Cimdina1

1Department of General Chemical Engineering, Riga Technical University, Āzenes str. 14/24, Riga, Latvia

2Riga Biomaterials Innovation and Development Center, Riga Technical University, Pulka str. 3/3, Riga, Latvia

lasma.poca@rtu.lv

The antibacterial properties of the silver have been used in different biomedical fields for a long time. It is well known that silver and silver-based compounds are antimicrobial to as many as 16 kinds of bacteria [1]. The combination of silver and hydroxyapatite (HAp/Ag) is used in the biomedical applications, due to their osteoconductivity and bioactivity [2].

In this study modified wet precipitation method was used to synthesize HAp/Ag with various silver contents. The precursors for HAp/Ag synthesis was calcium nitrate, diammonium hydrogen phosphate, ammonia solution, deionized water and silver nitrate. Synthesis was performed at 90oC. Four HAp/Ag complexes with different contents of silver (1%, 2%, 3% and 4%) were synthesized.

X-ray diffraction (XRD, Xpert-Pro Powder Diffractometer) was used to identify various phases in the HAp/Ag complexes. The XRD patterns show that before sintering typical HAp phases was determined. After sintering at 1000oC for 2 h the typical peaks of HAp and AgO phases was detected. For samples contents of 1% and 2% silver β-tricalcium phosphate phase was observed. Scanning electron microscopy was used to evaluate the surface morfphology of all samples.

References

[1] N.Rameshbabu et.al., J of Biomed Mat Res A, 2006, DOI 10.1002

[2] V.Stanic et.al., Applied Surface Science, 2011, 257(9), 4510-4518.